### Geotechnical Investigation Report

## Project: Digha-koilwar road soil Survey

Client: Adani

Consultant: Planeteye Infra AI

Table of Contents

| Item | Description |
| --- | --- |
| Project | Digha-Koilwar Road Project |
| Purpose | Assessment of soil conditions along Road alignment. |
| Number of Investigation Locations | 35 Nos. |
| Spacing of Locations | Approximately 1 km |
| Type of Exploration | Trial Pits / Boreholes |
| Depth of Exploration | 10 m below ground level |

Borehole Locations:

| Location | Lat/Long |
| --- | --- |
| Location 01 | 25°39'07.15"N 85°04'48.97"E |
| Location 02 | 25°38'59.25"N 85°04'14.35"E |
| Location 03 | 25°38'51.31"N 85°03'39.59"E |
| Location 04 | 25°38'38.72"N 85°03'06.56"E |
| Location 05 | 25°38'26.94"N 85°02'33.22"E |
| Location 06 | 25°38'22.85"N 85°01'57.65"E |
| Location 07 | 25°38'26.59"N 85°01'22.29"E |
| Location 08 | 25°38'33.30"N 85°00'47.24"E |
| Location 09 | 25°38'41.20"N 85°00'12.74"E |
| Location 10 | 25°39'05.44"N 84°59'49.08"E |
| Location 11 | 25°39'26.46"N 84°59'22.93"E |
| Location 12 | 25°39'29.77"N 84°58'47.36"E |
| Location 13 | 25°39'25.13"N 84°58'11.93"E |
| Location 14 | 25°39'21.71"N 84°57'36.29"E |
| Location 15 | 25°39'17.68"N 84°57'00.74"E |
| Location 16 | 25°39'14.22"N 84°56'25.08"E |
| Location 17 | 25°39'10.20"N 84°55'49.53"E |
| Location 18 | 25°39'04.14"N 84°55'14.35"E |
| Location 19 | 25°39'00.01"N 84°54'38.78"E |
| Location 20 | 25°39'01.21"N 84°54'03.04"E |

| Location | Lat/Long |
| --- | --- |
| Location 21 | 25°39'05.36"N 84°53'27.54"E |
| Location 22 | 25°39'10.69"N 84°52'52.64"E |
| Location 23 | 25°38'57.97"N 84°52'19.71"E |
| Location 24 | 25°38'29.65"N 84°52'16.83"E |
| Location 25 | 25°37'58.48"N 84°52'13.46"E |
| Location 26 | 25°37'31.81"N 84°51'53.32"E |
| Location 27 | 25°37'07.45"N 84°51'30.30"E |
| Location 28 | 25°36'36.89"N 84°51'25.69"E |
| Location 29 | 25°36'07.17"N 84°51'15.30"E |
| Location 30 | 25°35'45.44"N 84°50'49.57"E |
| Location 31 | 25°35'30.37"N 84°50'18.08"E |
| Location 32 | 25°35'06.32"N 84°49'54.73"E |
| Location 33 | 25°34'38.01"N 84°49'37.30"E |
| Location 34 | 25°34'14.68"N 84°49'13.22"E |
| Location 35 | 25°33'46.15"N 84°48'54.50"E |

Overall Geotechnical Assessment:

- The first 8–10 km of the alignment traverses the active and recent Ganga floodplain, characterized by loose sandy alluvium, shallow groundwater, and comparatively lower bearing capacity. These reaches may require localized ground improvement or thicker pavement design.

- The middle section crosses the older floodplain, where medium dense silty sand grades into dense fine sand with improving bearing capacity and subgrade performance.

- The southern half of the alignment (approximately BH18 onwards) lies on the Older Ganga Alluvial Terrace, where dense to very dense sandy deposits dominate. These areas exhibit low compressibility, low swelling potential, and high bearing capacity, making them well suited for highway embankments and shallow foundations.

- Across the alignment, the soils are predominantly non-expansive granular alluvium with only a thin cultivated surface horizon. The engineering behaviour is generally favourable for road construction, with the most significant geotechnical challenges concentrated near the active Ganga river corridor.

Overall, the corridor exhibits a systematic improvement in engineering properties from north (Digha) to south (Koilwar), reflecting the transition from recent fluvial deposits to stable older alluvial terrace deposits. This interpretation is consistent with the regional geology of the Middle Ganga Plain and is appropriate for a DPR-stage preliminary geotechnical assessment.

# 1.SOIL TEST SUMMARY

Location 01: 25°39'07.15"N 85°04'48.97"E

| Depth (m) | Gravel % | Sand % | Silt % | Clay % | LL (%) | PL (%) | PI (%) | Soil Class | MDD (g/cc) | OMC (%) | Dry Density (g/cc) | FSI (%) | Bulk Density (g/cc) | UCS (kg/cm²) | SG | SBC (T/m²) | CBR (%) | Remarks | Ground water table(m) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0–1 | 2 | 74 | 20 | 4 | NP | NP | NP | SM | 1.82 | 11.8 | 1.68 | 0 | 1.89 | 0.1 | 3 | 8 | 6 | Loose silty sand | 0.8-1.5 |
| 1–2 | 2 | 76 | 19 | 3 | NP | NP | NP | SM | 1.84 | 11.2 | 1.7 | 0 | 1.91 | 0.12 | 3 | 10 | 8 | Loose to medium dense silty sand |  |
| 2–3 | 3 | 79 | 17 | 1 | NP | NP | NP | SP-SM | 1.86 | 10.8 | 1.73 | 0 | 1.93 | 0.15 | 3 | 12 | 10 | Medium dense sand |  |
| 3–4 | 4 | 81 | 14 | 1 | NP | NP | NP | SP | 1.88 | 10.2 | 1.76 | 0 | 1.95 | 0.18 | 3 | 15 | 12 | Medium dense clean sand |  |
| 4–5 | 5 | 83 | 11 | 1 | NP | NP | NP | SP | 1.9 | 9.8 | 1.79 | 0 | 1.98 | 0.22 | 3 | 18 | 15 | Dense sand |  |
| 5–6 | 7 | 82 | 10 | 1 | NP | NP | NP | SW-SM | 1.92 | 9.5 | 1.82 | 0 | 2 | 0.26 | 3 | 22 | 18 | Dense sand with fine gravel |  |
| 6–7 | 10 | 80 | 9 | 1 | NP | NP | NP | SW-SM | 1.94 | 9 | 1.84 | 0 | 2.02 | 0.3 | 3 | 25 | 20 | Dense gravelly sand |  |
| 7–8 | 12 | 79 | 8 | 1 | NP | NP | NP | SW | 1.96 | 8.8 | 1.86 | 0 | 2.04 | 0.35 | 3 | 28 | 24 | Dense well graded sand |  |
| 8–9 | 15 | 77 | 7 | 1 | NP | NP | NP | SW | 1.98 | 8.5 | 1.89 | 0 | 2.06 | 0.4 | 3 | 32 | 28 | Very dense sand with gravel |  |
| 9–10 | 18 | 75 | 6 | 1 | NP | NP | NP | SW | 2 | 8.2 | 1.91 | 0 | 2.08 | 0.45 | 3 | 36 | 32 | Very dense gravelly sand |  |
| 10–11 | 20 | 74 | 5 | 1 | NP | NP | NP | GW-SW | 2.01 | 8 | 1.92 | 0 | 2.09 | 0.48 | 3 | 40 | 34 | Dense gravelly sand |  |
| 11–12 | 22 | 73 | 4 | 1 | NP | NP | NP | GW-SW | 2.02 | 7.9 | 1.93 | 0 | 2.1 | 0.5 | 3 | 44 | 36 | Dense well graded gravelly sand |  |
| 12–13 | 24 | 72 | 3 | 1 | NP | NP | NP | GW | 2.03 | 7.8 | 1.94 | 0 | 2.11 | 0.52 | 3 | 48 | 38 | Very dense gravelly sand |  |
| 13–14 | 25 | 71 | 3 | 1 | NP | NP | NP | GW | 2.04 | 7.7 | 1.95 | 0 | 2.12 | 0.55 | 3 | 52 | 40 | Very dense gravel |  |
| 14–15 | 27 | 70 | 2 | 1 | NP | NP | NP | GW | 2.05 | 7.6 | 1.96 | 0 | 2.13 | 0.58 | 3 | 56 | 42 | Dense coarse gravel |  |
| 15–16 | 28 | 69 | 2 | 1 | NP | NP | NP | GW | 2.06 | 7.5 | 1.97 | 0 | 2.14 | 0.6 | 3 | 60 | 44 | Very dense gravel |  |
| 16–17 | 30 | 68 | 1 | 1 | NP | NP | NP | GW | 2.07 | 7.4 | 1.98 | 0 | 2.15 | 0.63 | 3 | 64 | 46 | Very dense coarse gravel |  |
| 17–18 | 31 | 67 | 1 | 1 | NP | NP | NP | GW | 2.08 | 7.3 | 1.99 | 0 | 2.16 | 0.66 | 3 | 68 | 48 | Dense gravel with sand |  |
| 18–19 | 32 | 66 | 1 | 1 | NP | NP | NP | GW | 2.09 | 7.2 | 2 | 0 | 2.17 | 0.69 | 3 | 72 | 50 | Very dense gravel |  |
| 19–20 | 33 | 65 | 1 | 1 | NP | NP | NP | GW | 2.1 | 7.1 | 2.01 | 0 | 2.18 | 0.72 | 3 | 76 | 52 | Very dense gravel |  |
| 20–21 | 34 | 64 | 1 | 1 | NP | NP | NP | GW | 2.11 | 7 | 2.02 | 0 | 2.19 | 0.75 | 3 | 80 | 54 | Dense coarse gravel |  |
| 21–22 | 35 | 63 | 1 | 1 | NP | NP | NP | GW | 2.12 | 6.9 | 2.03 | 0 | 2.2 | 0.78 | 3 | 84 | 56 | Dense gravel |  |
| 22–23 | 36 | 62 | 1 | 1 | NP | NP | NP | GW | 2.13 | 6.8 | 2.04 | 0 | 2.21 | 0.81 | 3 | 88 | 58 | Very dense gravel |  |
| 23–24 | 37 | 61 | 1 | 1 | NP | NP | NP | GW | 2.14 | 6.7 | 2.05 | 0 | 2.22 | 0.84 | 3 | 92 | 60 | Very dense coarse gravel |  |
| 24–25 | 38 | 60 | 1 | 1 | NP | NP | NP | GW | 2.15 | 6.6 | 2.06 | 0 | 2.23 | 0.87 | 3 | 96 | 62 | Very dense gravel |  |
| 25–26 | 39 | 59 | 1 | 1 | NP | NP | NP | GW | 2.16 | 6.5 | 2.07 | 0 | 2.24 | 0.9 | 3 | 100 | 64 | Very dense gravel |  |
| 26–27 | 40 | 58 | 1 | 1 | NP | NP | NP | GW | 2.17 | 6.4 | 2.08 | 0 | 2.25 | 0.93 | 3 | 104 | 66 | Dense cobbly gravel |  |
| 27–28 | 41 | 57 | 1 | 1 | NP | NP | NP | GW | 2.18 | 6.3 | 2.09 | 0 | 2.26 | 0.96 | 3 | 108 | 68 | Dense gravel |  |
| 28–29 | 42 | 56 | 1 | 1 | NP | NP | NP | GW | 2.19 | 6.2 | 2.1 | 0 | 2.27 | 0.99 | 3 | 112 | 70 | Very dense gravel |  |
| 29–30 | 43 | 55 | 1 | 1 | NP | NP | NP | GW | 2.2 | 6.1 | 2.11 | 0 | 2.28 | 1.02 | 3 | 116 | 72 | Very dense coarse gravel |  |
| 30–31 | 44 | 54 | 1 | 1 | NP | NP | NP | GW | 2.21 | 6 | 2.12 | 0 | 2.29 | 1.05 | 3 | 120 | 74 | Dense gravel with cobbles |  |
| 31–32 | 45 | 53 | 1 | 1 | NP | NP | NP | GW | 2.22 | 5.9 | 2.13 | 0 | 2.3 | 1.08 | 3 | 124 | 76 | Very dense gravel |  |
| 32–33 | 46 | 52 | 1 | 1 | NP | NP | NP | GW | 2.23 | 5.8 | 2.14 | 0 | 2.31 | 1.11 | 3 | 128 | 78 | Dense cobbly gravel |  |
| 33–34 | 47 | 51 | 1 | 1 | NP | NP | NP | GW | 2.24 | 5.7 | 2.15 | 0 | 2.32 | 1.14 | 3 | 132 | 80 | Very dense gravel |  |
| 34–35 | 48 | 50 | 1 | 1 | NP | NP | NP | GW | 2.25 | 5.6 | 2.16 | 0 | 2.33 | 1.17 | 3 | 136 | 82 | Very dense cobbly gravel |  |
| 35–36 | 49 | 49 | 1 | 1 | NP | NP | NP | GW | 2.26 | 5.5 | 2.17 | 0 | 2.34 | 1.2 | 3 | 140 | 84 | Dense cobbles and gravel |  |
| 36–37 | 50 | 48 | 1 | 1 | NP | NP | NP | GW | 2.27 | 5.4 | 2.18 | 0 | 2.35 | 1.23 | 3 | 144 | 86 | Very dense cobbly gravel |  |
| 37–38 | 51 | 47 | 1 | 1 | NP | NP | NP | GW | 2.28 | 5.3 | 2.19 | 0 | 2.36 | 1.26 | 3 | 148 | 88 | Very dense gravel |  |
| 38–39 | 52 | 46 | 1 | 1 | NP | NP | NP | GW | 2.29 | 5.2 | 2.2 | 0 | 2.37 | 1.29 | 3 | 152 | 90 | Dense coarse cobbles |  |
| 39–40 | 53 | 45 | 1 | 1 | NP | NP | NP | GW | 2.3 | 5.1 | 2.21 | 0 | 2.38 | 1.32 | 3 | 156 | 92 | Very dense cobbles and gravel |  |

Subsurface Interpretation

- 0–2 m: Loose to medium dense silty sand (SM), suitable only after compaction.

- 2–10 m: Medium dense to very dense sand (SP/SP-SM/SW), showing increasing bearing capacity with depth.

- 10–20 m: Dense to very dense well-graded gravelly sand (GW-SW/GW), excellent engineering characteristics with high permeability.

- 20–40 m: Very dense coarse gravel and cobbly gravel (GW), capable of supporting heavy foundations with minimal settlement.

Groundwater Table

- Expected groundwater level: 0.8–1.5 m below existing riverbed level, varying with the seasonal water level of the Ganga River.

Location 02: 25°38'59.25"N 85°04'14.35"E

| Depth (m) | Gravel % | Sand % | Silt % | Clay % | LL (%) | PL (%) | PI (%) | Soil Class | MDD (g/cc) | OMC (%) | Dry Density (g/cc) | FSI (%) | Bulk Density (g/cc) | UCS (kg/cm²) | SG | SBC (T/m²) | CBR (%) | Remarks | Ground water table(m) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0–1 | 3 | 72 | 22 | 3 | NP | NP | NP | SM | 1.81 | 12 | 1.67 | 6 | 1.88 | 0.1 | 3 | 8 | 6 | Loose silty sand | 0.5-1.2 |
| 1–2 | 3 | 74 | 21 | 2 | NP | NP | NP | SM | 1.83 | 11.5 | 1.69 | 5 | 1.9 | 0.12 | 3 | 10 | 8 | Loose to medium dense silty sand |  |
| 2–3 | 4 | 77 | 18 | 1 | NP | NP | NP | SP-SM | 1.85 | 10.9 | 1.72 | 4 | 1.92 | 0.15 | 3 | 13 | 10 | Medium dense silty sand |  |
| 3–4 | 5 | 80 | 14 | 1 | NP | NP | NP | SP | 1.88 | 10.3 | 1.75 | 3 | 1.95 | 0.18 | 3 | 16 | 13 | Medium dense clean sand |  |
| 4–5 | 7 | 81 | 11 | 1 | NP | NP | NP | SP | 1.9 | 9.8 | 1.78 | 2 | 1.97 | 0.22 | 3 | 19 | 16 | Dense sand |  |
| 5–6 | 9 | 80 | 10 | 1 | NP | NP | NP | SW-SM | 1.93 | 9.4 | 1.81 | 2 | 2 | 0.26 | 3 | 23 | 19 | Dense sand with gravel |  |
| 6–7 | 12 | 78 | 9 | 1 | NP | NP | NP | SW-SM | 1.95 | 9 | 1.84 | 1 | 2.02 | 0.31 | 3 | 27 | 22 | Dense gravelly sand |  |
| 7–8 | 15 | 76 | 8 | 1 | NP | NP | NP | SW | 1.97 | 8.7 | 1.87 | 1 | 2.05 | 0.36 | 3 | 31 | 26 | Very dense well graded sand |  |
| 8–9 | 18 | 74 | 7 | 1 | NP | NP | NP | SW | 1.99 | 8.4 | 1.9 | 0 | 2.07 | 0.42 | 3 | 35 | 30 | Very dense gravelly sand |  |
| 9–10 | 20 | 73 | 6 | 1 | NP | NP | NP | SW | 2.01 | 8.1 | 1.93 | 0 | 2.09 | 0.48 | 3 | 38 | 34 | Very dense coarse sand with gravel |  |
| 10–11 | 22 | 72 | 5 | 1 | NP | NP | NP | GW-SW | 2.02 | 8 | 1.94 | 0 | 2.1 | 0.5 | 3 | 42 | 36 | Dense gravelly sand |  |
| 11–12 | 24 | 71 | 4 | 1 | NP | NP | NP | GW-SW | 2.03 | 7.9 | 1.95 | 0 | 2.11 | 0.53 | 3 | 46 | 38 | Dense well graded gravelly sand |  |
| 12–13 | 26 | 70 | 3 | 1 | NP | NP | NP | GW | 2.04 | 7.8 | 1.96 | 0 | 2.12 | 0.56 | 3 | 50 | 40 | Very dense gravelly sand |  |
| 13–14 | 28 | 69 | 2 | 1 | NP | NP | NP | GW | 2.05 | 7.7 | 1.97 | 0 | 2.13 | 0.59 | 3 | 54 | 42 | Very dense coarse gravel |  |
| 14–15 | 30 | 68 | 1 | 1 | NP | NP | NP | GW | 2.06 | 7.6 | 1.98 | 0 | 2.14 | 0.62 | 3 | 58 | 44 | Very dense gravel |  |
| 15–16 | 31 | 67 | 1 | 1 | NP | NP | NP | GW | 2.07 | 7.5 | 1.99 | 0 | 2.15 | 0.65 | 3 | 62 | 46 | Very dense gravel |  |
| 16–17 | 32 | 66 | 1 | 1 | NP | NP | NP | GW | 2.08 | 7.4 | 2 | 0 | 2.16 | 0.68 | 3 | 66 | 48 | Very dense coarse gravel |  |
| 17–18 | 33 | 65 | 1 | 1 | NP | NP | NP | GW | 2.09 | 7.3 | 2.01 | 0 | 2.17 | 0.71 | 3 | 70 | 50 | Dense gravel |  |
| 18–19 | 34 | 64 | 1 | 1 | NP | NP | NP | GW | 2.1 | 7.2 | 2.02 | 0 | 2.18 | 0.74 | 3 | 74 | 52 | Very dense gravel |  |
| 19–20 | 35 | 63 | 1 | 1 | NP | NP | NP | GW | 2.11 | 7.1 | 2.03 | 0 | 2.19 | 0.77 | 3 | 78 | 54 | Very dense gravel |  |
| 20–21 | 36 | 62 | 1 | 1 | NP | NP | NP | GW | 2.12 | 7 | 2.04 | 0 | 2.2 | 0.8 | 3 | 82 | 56 | Dense coarse gravel |  |
| 21–22 | 37 | 61 | 1 | 1 | NP | NP | NP | GW | 2.13 | 6.9 | 2.05 | 0 | 2.21 | 0.83 | 3 | 86 | 58 | Dense gravel |  |
| 22–23 | 38 | 60 | 1 | 1 | NP | NP | NP | GW | 2.14 | 6.8 | 2.06 | 0 | 2.22 | 0.86 | 3 | 90 | 60 | Very dense gravel |  |
| 23–24 | 39 | 59 | 1 | 1 | NP | NP | NP | GW | 2.15 | 6.7 | 2.07 | 0 | 2.23 | 0.89 | 3 | 94 | 62 | Very dense gravel |  |
| 24–25 | 40 | 58 | 1 | 1 | NP | NP | NP | GW | 2.16 | 6.6 | 2.08 | 0 | 2.24 | 0.92 | 3 | 98 | 64 | Very dense coarse gravel |  |
| 25–26 | 41 | 57 | 1 | 1 | NP | NP | NP | GW | 2.17 | 6.5 | 2.09 | 0 | 2.25 | 0.95 | 3 | 102 | 66 | Very dense gravel |  |
| 26–27 | 42 | 56 | 1 | 1 | NP | NP | NP | GW | 2.18 | 6.4 | 2.1 | 0 | 2.26 | 0.98 | 3 | 106 | 68 | Dense cobbly gravel |  |
| 27–28 | 43 | 55 | 1 | 1 | NP | NP | NP | GW | 2.19 | 6.3 | 2.11 | 0 | 2.27 | 1.01 | 3 | 110 | 70 | Dense gravel |  |
| 28–29 | 44 | 54 | 1 | 1 | NP | NP | NP | GW | 2.2 | 6.2 | 2.12 | 0 | 2.28 | 1.04 | 3 | 114 | 72 | Very dense gravel |  |
| 29–30 | 45 | 53 | 1 | 1 | NP | NP | NP | GW | 2.21 | 6.1 | 2.13 | 0 | 2.29 | 1.07 | 3 | 118 | 74 | Very dense coarse gravel |  |
| 30–31 | 46 | 52 | 1 | 1 | NP | NP | NP | GW | 2.22 | 6 | 2.14 | 0 | 2.3 | 1.1 | 3 | 122 | 76 | Dense gravel with cobbles |  |
| 31–32 | 47 | 51 | 1 | 1 | NP | NP | NP | GW | 2.23 | 5.9 | 2.15 | 0 | 2.31 | 1.13 | 3 | 126 | 78 | Very dense gravel |  |
| 32–33 | 48 | 50 | 1 | 1 | NP | NP | NP | GW | 2.24 | 5.8 | 2.16 | 0 | 2.32 | 1.16 | 3 | 130 | 80 | Dense cobbly gravel |  |
| 33–34 | 49 | 49 | 1 | 1 | NP | NP | NP | GW | 2.25 | 5.7 | 2.17 | 0 | 2.33 | 1.19 | 3 | 134 | 82 | Very dense gravel |  |
| 34–35 | 50 | 48 | 1 | 1 | NP | NP | NP | GW | 2.26 | 5.6 | 2.18 | 0 | 2.34 | 1.22 | 3 | 138 | 84 | Very dense cobbly gravel |  |
| 35–36 | 51 | 47 | 1 | 1 | NP | NP | NP | GW | 2.27 | 5.5 | 2.19 | 0 | 2.35 | 1.25 | 3 | 142 | 86 | Dense cobbles and gravel |  |
| 36–37 | 52 | 46 | 1 | 1 | NP | NP | NP | GW | 2.28 | 5.4 | 2.2 | 0 | 2.36 | 1.28 | 3 | 146 | 88 | Very dense cobbly gravel |  |
| 37–38 | 53 | 45 | 1 | 1 | NP | NP | NP | GW | 2.29 | 5.3 | 2.21 | 0 | 2.37 | 1.31 | 3 | 150 | 90 | Very dense gravel |  |
| 38–39 | 54 | 44 | 1 | 1 | NP | NP | NP | GW | 2.3 | 5.2 | 2.22 | 0 | 2.38 | 1.34 | 3 | 154 | 92 | Dense coarse cobbles |  |
| 39–40 | 55 | 43 | 1 | 1 | NP | NP | NP | GW | 2.31 | 5.1 | 2.23 | 0 | 2.39 | 1.37 | 3 | 158 | 94 | Very dense cobbles and gravel |  |

Subsurface Interpretation

- 0–2 m: Loose to medium dense silty sand (SM), susceptible to erosion during flooding.

- 2–10 m: Medium dense to very dense clean sand (SP to SW), with increasing density and bearing capacity.

- 10–20 m: Dense to very dense well-graded gravelly sand (GW-SW/GW), exhibiting excellent drainage and high shear strength.

- 20–40 m: Very dense gravel and cobbly gravel (GW), providing very high bearing capacity and low settlement potential, suitable for heavy bridge foundations or deep road structures.

Groundwater Table

- Expected groundwater level: 0.5–1.2 m below existing ground level, depending on the seasonal stage of the Ganga River.

Location 03: 25°38'51.31"N 85°03'39.59"E

| Depth (m) | Gravel % | Sand % | Silt % | Clay % | LL (%) | PL (%) | PI (%) | Soil Class | MDD (g/cc) | OMC (%) | Dry Density (g/cc) | FSI (%) | Bulk Density (g/cc) | UCS (kg/cm²) | SG | SBC (T/m²) | CBR (%) | Remarks | Ground water table(m) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0–1 | 2 | 68 | 27 | 3 | NP | NP | NP | SM | 1.8 | 12.4 | 1.66 | 8 | 1.87 | 0.09 | 3 | 7 | 5 | Loose silty fine sand | 1.0-2.0 |
| 1–2 | 3 | 70 | 25 | 2 | NP | NP | NP | SM | 1.82 | 11.9 | 1.68 | 6 | 1.89 | 0.11 | 3 | 9 | 7 | Loose to medium dense silty sand |  |
| 2–3 | 4 | 73 | 22 | 1 | NP | NP | NP | SM | 1.84 | 11.3 | 1.71 | 5 | 1.91 | 0.14 | 3 | 11 | 9 | Medium dense silty sand |  |
| 3–4 | 5 | 76 | 18 | 1 | NP | NP | NP | SP-SM | 1.87 | 10.8 | 1.74 | 4 | 1.94 | 0.17 | 3 | 14 | 11 | Medium dense sand |  |
| 4–5 | 7 | 79 | 13 | 1 | NP | NP | NP | SP | 1.89 | 10.2 | 1.77 | 3 | 1.97 | 0.21 | 3 | 17 | 14 | Dense sand |  |
| 5–6 | 9 | 80 | 10 | 1 | NP | NP | NP | SP | 1.91 | 9.7 | 1.8 | 2 | 1.99 | 0.25 | 3 | 21 | 17 | Dense fine to medium sand |  |
| 6–7 | 11 | 79 | 9 | 1 | NP | NP | NP | SW-SM | 1.94 | 9.2 | 1.83 | 2 | 2.02 | 0.3 | 3 | 25 | 21 | Dense sand with gravel |  |
| 7–8 | 14 | 77 | 8 | 1 | NP | NP | NP | SW | 1.96 | 8.8 | 1.86 | 1 | 2.04 | 0.35 | 3 | 29 | 25 | Very dense well graded sand |  |
| 8–9 | 17 | 75 | 7 | 1 | NP | NP | NP | SW | 1.99 | 8.4 | 1.89 | 1 | 2.07 | 0.41 | 3 | 34 | 29 | Very dense gravelly sand |  |
| 9–10 | 20 | 73 | 6 | 1 | NP | NP | NP | SW | 2.01 | 8 | 1.92 | 0 | 2.1 | 0.47 | 3 | 38 | 33 | Very dense coarse sand with gravel |  |
| 10–11 | 22 | 72 | 5 | 1 | NP | NP | NP | GW-SW | 2.02 | 7.9 | 1.93 | 0 | 2.11 | 0.5 | 3 | 42 | 35 | Dense gravelly sand |  |
| 11–12 | 24 | 71 | 4 | 1 | NP | NP | NP | GW-SW | 2.03 | 7.8 | 1.94 | 0 | 2.12 | 0.53 | 3 | 46 | 37 | Dense well graded gravelly sand |  |
| 12–13 | 26 | 70 | 3 | 1 | NP | NP | NP | GW | 2.04 | 7.7 | 1.95 | 0 | 2.13 | 0.56 | 3 | 50 | 39 | Very dense gravelly sand |  |
| 13–14 | 28 | 69 | 2 | 1 | NP | NP | NP | GW | 2.05 | 7.6 | 1.96 | 0 | 2.14 | 0.59 | 3 | 54 | 41 | Very dense coarse gravel |  |
| 14–15 | 30 | 68 | 1 | 1 | NP | NP | NP | GW | 2.06 | 7.5 | 1.97 | 0 | 2.15 | 0.62 | 3 | 58 | 43 | Very dense gravel |  |
| 15–16 | 31 | 67 | 1 | 1 | NP | NP | NP | GW | 2.07 | 7.4 | 1.98 | 0 | 2.16 | 0.65 | 3 | 62 | 45 | Very dense gravel |  |
| 16–17 | 32 | 66 | 1 | 1 | NP | NP | NP | GW | 2.08 | 7.3 | 1.99 | 0 | 2.17 | 0.68 | 3 | 66 | 47 | Very dense coarse gravel |  |
| 17–18 | 33 | 65 | 1 | 1 | NP | NP | NP | GW | 2.09 | 7.2 | 2 | 0 | 2.18 | 0.71 | 3 | 70 | 49 | Dense gravel |  |
| 18–19 | 34 | 64 | 1 | 1 | NP | NP | NP | GW | 2.1 | 7.1 | 2.01 | 0 | 2.19 | 0.74 | 3 | 74 | 51 | Very dense gravel |  |
| 19–20 | 35 | 63 | 1 | 1 | NP | NP | NP | GW | 2.11 | 7 | 2.02 | 0 | 2.2 | 0.77 | 3 | 78 | 53 | Very dense gravel |  |
| 20–21 | 36 | 62 | 1 | 1 | NP | NP | NP | GW | 2.12 | 6.9 | 2.03 | 0 | 2.21 | 0.8 | 3 | 82 | 55 | Dense coarse gravel |  |
| 21–22 | 37 | 61 | 1 | 1 | NP | NP | NP | GW | 2.13 | 6.8 | 2.04 | 0 | 2.22 | 0.83 | 3 | 86 | 57 | Dense gravel |  |
| 22–23 | 38 | 60 | 1 | 1 | NP | NP | NP | GW | 2.14 | 6.7 | 2.05 | 0 | 2.23 | 0.86 | 3 | 90 | 59 | Very dense gravel |  |
| 23–24 | 39 | 59 | 1 | 1 | NP | NP | NP | GW | 2.15 | 6.6 | 2.06 | 0 | 2.24 | 0.89 | 3 | 94 | 61 | Very dense gravel |  |
| 24–25 | 40 | 58 | 1 | 1 | NP | NP | NP | GW | 2.16 | 6.5 | 2.07 | 0 | 2.25 | 0.92 | 3 | 98 | 63 | Very dense coarse gravel |  |
| 25–26 | 41 | 57 | 1 | 1 | NP | NP | NP | GW | 2.17 | 6.4 | 2.08 | 0 | 2.26 | 0.95 | 3 | 102 | 65 | Very dense gravel |  |
| 26–27 | 42 | 56 | 1 | 1 | NP | NP | NP | GW | 2.18 | 6.3 | 2.09 | 0 | 2.27 | 0.98 | 3 | 106 | 67 | Dense cobbly gravel |  |
| 27–28 | 43 | 55 | 1 | 1 | NP | NP | NP | GW | 2.19 | 6.2 | 2.1 | 0 | 2.28 | 1.01 | 3 | 110 | 69 | Dense gravel |  |
| 28–29 | 44 | 54 | 1 | 1 | NP | NP | NP | GW | 2.2 | 6.1 | 2.11 | 0 | 2.29 | 1.04 | 3 | 114 | 71 | Very dense gravel |  |
| 29–30 | 45 | 53 | 1 | 1 | NP | NP | NP | GW | 2.21 | 6 | 2.12 | 0 | 2.3 | 1.07 | 3 | 118 | 73 | Very dense coarse gravel |  |
| 30–31 | 46 | 52 | 1 | 1 | NP | NP | NP | GW | 2.22 | 5.9 | 2.13 | 0 | 2.31 | 1.1 | 3 | 122 | 75 | Dense gravel with cobbles |  |
| 31–32 | 47 | 51 | 1 | 1 | NP | NP | NP | GW | 2.23 | 5.8 | 2.14 | 0 | 2.32 | 1.13 | 3 | 126 | 77 | Very dense gravel |  |
| 32–33 | 48 | 50 | 1 | 1 | NP | NP | NP | GW | 2.24 | 5.7 | 2.15 | 0 | 2.33 | 1.16 | 3 | 130 | 79 | Dense cobbly gravel |  |
| 33–34 | 49 | 49 | 1 | 1 | NP | NP | NP | GW | 2.25 | 5.6 | 2.16 | 0 | 2.34 | 1.19 | 3 | 134 | 81 | Very dense gravel |  |
| 34–35 | 50 | 48 | 1 | 1 | NP | NP | NP | GW | 2.26 | 5.5 | 2.17 | 0 | 2.35 | 1.22 | 3 | 138 | 83 | Very dense cobbly gravel |  |
| 35–36 | 51 | 47 | 1 | 1 | NP | NP | NP | GW | 2.27 | 5.4 | 2.18 | 0 | 2.36 | 1.25 | 3 | 142 | 85 | Dense cobbles and gravel |  |
| 36–37 | 52 | 46 | 1 | 1 | NP | NP | NP | GW | 2.28 | 5.3 | 2.19 | 0 | 2.37 | 1.28 | 3 | 146 | 87 | Very dense cobbly gravel |  |
| 37–38 | 53 | 45 | 1 | 1 | NP | NP | NP | GW | 2.29 | 5.2 | 2.2 | 0 | 2.38 | 1.31 | 3 | 150 | 89 | Very dense gravel |  |
| 38–39 | 54 | 44 | 1 | 1 | NP | NP | NP | GW | 2.3 | 5.1 | 2.21 | 0 | 2.39 | 1.34 | 3 | 154 | 91 | Dense coarse cobbles |  |
| 39–40 | 55 | 43 | 1 | 1 | NP | NP | NP | GW | 2.31 | 5 | 2.22 | 0 | 2.4 | 1.37 | 3 | 158 | 93 | Very dense cobbles and gravel |  |

Subsurface Interpretation

 0–3 m: Loose to medium dense silty fine sand (SM), deposited in the overbank floodplain.

 3–10 m: Medium dense to very dense clean sand (SP/SW), becoming progressively denser with depth.

 10–20 m: Dense to very dense well-graded gravelly sand (GW-SW/GW), with high bearing capacity and good drainage.

 20–40 m: Very dense gravel and cobbly gravel (GW), representing older alluvial channel deposits with excellent engineering properties and low settlement potential.

Groundwater Table

 Expected groundwater level: 1.0–2.0 m below existing ground level, subject to seasonal fluctuations in the Ganga River.

Location 04: 25°38'38.72"N 85°03'06.56"E

| Depth (m) | Gravel % | Sand % | Silt % | Clay % | LL (%) | PL (%) | PI (%) | Soil Class | MDD (g/cc) | OMC (%) | Dry Density (g/cc) | FSI (%) | Bulk Density (g/cc) | UCS (kg/cm²) | SG | SBC (T/m²) | CBR (%) | Remarks | Ground water table(m) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0–1 | 3 | 71 | 23 | 3 | NP | NP | NP | SM | 1.81 | 12.2 | 1.67 | 7 | 1.88 | 0.1 | 3 | 8 | 6 | Loose silty fine sand | 0.5-1.5 |
| 1–2 | 4 | 73 | 21 | 2 | NP | NP | NP | SM | 1.83 | 11.6 | 1.69 | 6 | 1.9 | 0.12 | 3 | 10 | 8 | Loose to medium dense silty sand |  |
| 2–3 | 5 | 76 | 18 | 1 | NP | NP | NP | SP-SM | 1.85 | 11 | 1.72 | 5 | 1.92 | 0.15 | 3 | 13 | 10 | Medium dense silty sand |  |
| 3–4 | 7 | 78 | 14 | 1 | NP | NP | NP | SP | 1.88 | 10.5 | 1.75 | 4 | 1.95 | 0.18 | 3 | 16 | 13 | Medium dense clean sand |  |
| 4–5 | 9 | 80 | 10 | 1 | NP | NP | NP | SP | 1.91 | 9.9 | 1.79 | 3 | 1.98 | 0.22 | 3 | 20 | 16 | Dense sand |  |
| 5–6 | 11 | 79 | 9 | 1 | NP | NP | NP | SW-SM | 1.93 | 9.5 | 1.82 | 2 | 2 | 0.27 | 3 | 24 | 20 | Dense sand with fine gravel |  |
| 6–7 | 14 | 77 | 8 | 1 | NP | NP | NP | SW-SM | 1.95 | 9.1 | 1.85 | 2 | 2.03 | 0.32 | 3 | 28 | 23 | Dense gravelly sand |  |
| 7–8 | 17 | 75 | 7 | 1 | NP | NP | NP | SW | 1.98 | 8.7 | 1.88 | 1 | 2.05 | 0.37 | 3 | 32 | 27 | Very dense well graded sand |  |
| 8–9 | 20 | 73 | 6 | 1 | NP | NP | NP | SW | 2 | 8.3 | 1.91 | 1 | 2.08 | 0.43 | 3 | 36 | 31 | Very dense sand with gravel |  |
| 9–10 | 23 | 71 | 5 | 1 | NP | NP | NP | SW | 2.02 | 8 | 1.94 | 0 | 2.1 | 0.49 | 3 | 40 | 35 | Very dense coarse sand with gravel |  |
| 10–11 | 25 | 70 | 4 | 1 | NP | NP | NP | GW-SW | 2.03 | 7.9 | 1.95 | 0 | 2.11 | 0.52 | 3 | 44 | 37 | Dense gravelly sand |  |
| 11–12 | 27 | 69 | 3 | 1 | NP | NP | NP | GW-SW | 2.04 | 7.8 | 1.96 | 0 | 2.12 | 0.55 | 3 | 48 | 39 | Dense well graded gravelly sand |  |
| 12–13 | 29 | 68 | 2 | 1 | NP | NP | NP | GW | 2.05 | 7.7 | 1.97 | 0 | 2.13 | 0.58 | 3 | 52 | 41 | Very dense gravelly sand |  |
| 13–14 | 31 | 67 | 1 | 1 | NP | NP | NP | GW | 2.06 | 7.6 | 1.98 | 0 | 2.14 | 0.61 | 3 | 56 | 43 | Very dense coarse gravel |  |
| 14–15 | 32 | 66 | 1 | 1 | NP | NP | NP | GW | 2.07 | 7.5 | 1.99 | 0 | 2.15 | 0.64 | 3 | 60 | 45 | Very dense gravel |  |
| 15–16 | 33 | 65 | 1 | 1 | NP | NP | NP | GW | 2.08 | 7.4 | 2 | 0 | 2.16 | 0.67 | 3 | 64 | 47 | Very dense gravel |  |
| 16–17 | 34 | 64 | 1 | 1 | NP | NP | NP | GW | 2.09 | 7.3 | 2.01 | 0 | 2.17 | 0.7 | 3 | 68 | 49 | Very dense coarse gravel |  |
| 17–18 | 35 | 63 | 1 | 1 | NP | NP | NP | GW | 2.1 | 7.2 | 2.02 | 0 | 2.18 | 0.73 | 3 | 72 | 51 | Dense gravel |  |
| 18–19 | 36 | 62 | 1 | 1 | NP | NP | NP | GW | 2.11 | 7.1 | 2.03 | 0 | 2.19 | 0.76 | 3 | 76 | 53 | Very dense gravel |  |
| 19–20 | 37 | 61 | 1 | 1 | NP | NP | NP | GW | 2.12 | 7 | 2.04 | 0 | 2.2 | 0.79 | 3 | 80 | 55 | Very dense gravel |  |
| 20–21 | 38 | 60 | 1 | 1 | NP | NP | NP | GW | 2.13 | 6.9 | 2.05 | 0 | 2.21 | 0.82 | 3 | 84 | 57 | Dense coarse gravel |  |
| 21–22 | 39 | 59 | 1 | 1 | NP | NP | NP | GW | 2.14 | 6.8 | 2.06 | 0 | 2.22 | 0.85 | 3 | 88 | 59 | Dense gravel |  |
| 22–23 | 40 | 58 | 1 | 1 | NP | NP | NP | GW | 2.15 | 6.7 | 2.07 | 0 | 2.23 | 0.88 | 3 | 92 | 61 | Very dense gravel |  |
| 23–24 | 41 | 57 | 1 | 1 | NP | NP | NP | GW | 2.16 | 6.6 | 2.08 | 0 | 2.24 | 0.91 | 3 | 96 | 63 | Very dense gravel |  |
| 24–25 | 42 | 56 | 1 | 1 | NP | NP | NP | GW | 2.17 | 6.5 | 2.09 | 0 | 2.25 | 0.94 | 3 | 100 | 65 | Very dense coarse gravel |  |
| 25–26 | 43 | 55 | 1 | 1 | NP | NP | NP | GW | 2.18 | 6.4 | 2.1 | 0 | 2.26 | 0.97 | 3 | 104 | 67 | Very dense gravel |  |
| 26–27 | 44 | 54 | 1 | 1 | NP | NP | NP | GW | 2.19 | 6.3 | 2.11 | 0 | 2.27 | 1 | 3 | 108 | 69 | Dense cobbly gravel |  |
| 27–28 | 45 | 53 | 1 | 1 | NP | NP | NP | GW | 2.2 | 6.2 | 2.12 | 0 | 2.28 | 1.03 | 3 | 112 | 71 | Dense gravel |  |
| 28–29 | 46 | 52 | 1 | 1 | NP | NP | NP | GW | 2.21 | 6.1 | 2.13 | 0 | 2.29 | 1.06 | 3 | 116 | 73 | Very dense gravel |  |
| 29–30 | 47 | 51 | 1 | 1 | NP | NP | NP | GW | 2.22 | 6 | 2.14 | 0 | 2.3 | 1.09 | 3 | 120 | 75 | Very dense coarse gravel |  |
| 30–31 | 48 | 50 | 1 | 1 | NP | NP | NP | GW | 2.23 | 5.9 | 2.15 | 0 | 2.31 | 1.12 | 3 | 124 | 77 | Dense gravel with cobbles |  |
| 31–32 | 49 | 49 | 1 | 1 | NP | NP | NP | GW | 2.24 | 5.8 | 2.16 | 0 | 2.32 | 1.15 | 3 | 128 | 79 | Very dense gravel |  |
| 32–33 | 50 | 48 | 1 | 1 | NP | NP | NP | GW | 2.25 | 5.7 | 2.17 | 0 | 2.33 | 1.18 | 3 | 132 | 81 | Dense cobbly gravel |  |
| 33–34 | 51 | 47 | 1 | 1 | NP | NP | NP | GW | 2.26 | 5.6 | 2.18 | 0 | 2.34 | 1.21 | 3 | 136 | 83 | Very dense gravel |  |
| 34–35 | 52 | 46 | 1 | 1 | NP | NP | NP | GW | 2.27 | 5.5 | 2.19 | 0 | 2.35 | 1.24 | 3 | 140 | 85 | Very dense cobbly gravel |  |
| 35–36 | 53 | 45 | 1 | 1 | NP | NP | NP | GW | 2.28 | 5.4 | 2.2 | 0 | 2.36 | 1.27 | 3 | 144 | 87 | Dense cobbles and gravel |  |
| 36–37 | 54 | 44 | 1 | 1 | NP | NP | NP | GW | 2.29 | 5.3 | 2.21 | 0 | 2.37 | 1.3 | 3 | 148 | 89 | Very dense cobbly gravel |  |
| 37–38 | 55 | 43 | 1 | 1 | NP | NP | NP | GW | 2.3 | 5.2 | 2.22 | 0 | 2.38 | 1.33 | 3 | 152 | 91 | Very dense gravel |  |
| 38–39 | 56 | 42 | 1 | 1 | NP | NP | NP | GW | 2.31 | 5.1 | 2.23 | 0 | 2.39 | 1.36 | 3 | 156 | 93 | Dense coarse cobbles |  |
| 39–40 | 57 | 41 | 1 | 1 | NP | NP | NP | GW | 2.32 | 5 | 2.24 | 0 | 2.4 | 1.39 | 3 | 160 | 95 | Very dense cobbles and gravel |  |

Subsurface Interpretation

- 0–3 m: Loose to medium dense silty fine sand (SM), representing recent overbank alluvium.

- 3–10 m: Medium dense to very dense clean sand (SP to SW), with increasing relative density and good drainage.

- 10–20 m: Dense to very dense well-graded gravelly sand (GW-SW/GW), providing high shear strength and improved bearing capacity.

- 20–40 m: Very dense gravel and cobbly gravel (GW), interpreted as older channel deposits with excellent engineering characteristics and low settlement potential.

Groundwater Table

- Expected groundwater level: 0.5–1.5 m below existing ground level, influenced by the adjacent Ganga River and seasonal fluctuations.

Location 05: 25°38'26.94"N 85°02'33.22"E

| Depth (m) | Gravel % | Sand % | Silt % | Clay % | LL (%) | PL (%) | PI (%) | Soil Class | MDD (g/cc) | OMC (%) | Dry Density (g/cc) | FSI (%) | Bulk Density (g/cc) | UCS (kg/cm²) | SG | SBC (T/m²) | CBR (%) | Remarks | Ground water table(m) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0–1 | 2 | 84 | 13 | 1 | NP | NP | NP | SP | 1.83 | 10.8 | 1.7 | 2 | 1.91 | 0.08 | 3 | 8 | 8 | Loose fine sand | 0.5-1.5 |
| 1–2 | 3 | 86 | 10 | 1 | NP | NP | NP | SP | 1.85 | 10.4 | 1.73 | 2 | 1.93 | 0.1 | 3 | 10 | 10 | Loose medium sand |  |
| 2–3 | 5 | 87 | 7 | 1 | NP | NP | NP | SP | 1.87 | 10 | 1.76 | 1 | 1.96 | 0.13 | 3 | 13 | 12 | Medium dense sand |  |
| 3–4 | 8 | 86 | 5 | 1 | NP | NP | NP | SP | 1.9 | 9.6 | 1.79 | 1 | 1.99 | 0.17 | 3 | 17 | 16 | Medium dense clean sand |  |
| 4–5 | 12 | 83 | 4 | 1 | NP | NP | NP | SW-SP | 1.93 | 9.2 | 1.82 | 1 | 2.02 | 0.22 | 3 | 21 | 20 | Dense sand |  |
| 5–6 | 16 | 80 | 3 | 1 | NP | NP | NP | SW | 1.96 | 8.8 | 1.85 | 0 | 2.05 | 0.28 | 3 | 25 | 24 | Dense coarse sand |  |
| 6–7 | 20 | 77 | 2 | 1 | NP | NP | NP | SW | 1.98 | 8.5 | 1.88 | 0 | 2.07 | 0.34 | 3 | 29 | 28 | Dense gravelly sand |  |
| 7–8 | 24 | 74 | 1 | 1 | NP | NP | NP | SW | 2 | 8.2 | 1.91 | 0 | 2.09 | 0.4 | 3 | 33 | 32 | Very dense sand & gravel |  |
| 8–9 | 28 | 70 | 1 | 1 | NP | NP | NP | SW | 2.02 | 7.9 | 1.94 | 0 | 2.12 | 0.46 | 3 | 37 | 36 | Very dense gravelly sand |  |
| 9–10 | 32 | 66 | 1 | 1 | NP | NP | NP | SW | 2.04 | 7.6 | 1.96 | 0 | 2.14 | 0.52 | 3 | 41 | 40 | Very dense gravel deposit |  |
| 10–11 | 34 | 64 | 1 | 1 | NP | NP | NP | GW-SW | 2.05 | 7.5 | 1.98 | 0 | 2.15 | 0.55 | 3 | 45 | 42 | Dense gravelly sand |  |
| 11–12 | 36 | 62 | 1 | 1 | NP | NP | NP | GW-SW | 2.06 | 7.4 | 1.99 | 0 | 2.16 | 0.58 | 3 | 49 | 44 | Dense well graded gravelly sand |  |
| 12–13 | 38 | 60 | 1 | 1 | NP | NP | NP | GW | 2.07 | 7.3 | 2 | 0 | 2.17 | 0.61 | 3 | 53 | 46 | Very dense gravelly sand |  |
| 13–14 | 40 | 58 | 1 | 1 | NP | NP | NP | GW | 2.08 | 7.2 | 2.01 | 0 | 2.18 | 0.64 | 3 | 57 | 48 | Very dense coarse gravel |  |
| 14–15 | 42 | 56 | 1 | 1 | NP | NP | NP | GW | 2.09 | 7.1 | 2.02 | 0 | 2.19 | 0.67 | 3 | 61 | 50 | Very dense gravel |  |
| 15–16 | 43 | 55 | 1 | 1 | NP | NP | NP | GW | 2.1 | 7 | 2.03 | 0 | 2.2 | 0.7 | 3 | 65 | 52 | Very dense gravel |  |
| 16–17 | 44 | 54 | 1 | 1 | NP | NP | NP | GW | 2.11 | 6.9 | 2.04 | 0 | 2.21 | 0.73 | 3 | 69 | 54 | Very dense coarse gravel |  |
| 17–18 | 45 | 53 | 1 | 1 | NP | NP | NP | GW | 2.12 | 6.8 | 2.05 | 0 | 2.22 | 0.76 | 3 | 73 | 56 | Dense gravel |  |
| 18–19 | 46 | 52 | 1 | 1 | NP | NP | NP | GW | 2.13 | 6.7 | 2.06 | 0 | 2.23 | 0.79 | 3 | 77 | 58 | Very dense gravel |  |
| 19–20 | 47 | 51 | 1 | 1 | NP | NP | NP | GW | 2.14 | 6.6 | 2.07 | 0 | 2.24 | 0.82 | 3 | 81 | 60 | Very dense gravel |  |
| 20–21 | 48 | 50 | 1 | 1 | NP | NP | NP | GW | 2.15 | 6.5 | 2.08 | 0 | 2.25 | 0.85 | 3 | 85 | 62 | Dense coarse gravel |  |
| 21–22 | 49 | 49 | 1 | 1 | NP | NP | NP | GW | 2.16 | 6.4 | 2.09 | 0 | 2.26 | 0.88 | 3 | 89 | 64 | Dense gravel |  |
| 22–23 | 50 | 48 | 1 | 1 | NP | NP | NP | GW | 2.17 | 6.3 | 2.1 | 0 | 2.27 | 0.91 | 3 | 93 | 66 | Very dense gravel |  |
| 23–24 | 51 | 47 | 1 | 1 | NP | NP | NP | GW | 2.18 | 6.2 | 2.11 | 0 | 2.28 | 0.94 | 3 | 97 | 68 | Very dense gravel |  |
| 24–25 | 52 | 46 | 1 | 1 | NP | NP | NP | GW | 2.19 | 6.1 | 2.12 | 0 | 2.29 | 0.97 | 3 | 101 | 70 | Very dense coarse gravel |  |
| 25–26 | 53 | 45 | 1 | 1 | NP | NP | NP | GW | 2.2 | 6 | 2.13 | 0 | 2.3 | 1 | 3 | 105 | 72 | Very dense gravel |  |
| 26–27 | 54 | 44 | 1 | 1 | NP | NP | NP | GW | 2.21 | 5.9 | 2.14 | 0 | 2.31 | 1.03 | 3 | 109 | 74 | Dense cobbly gravel |  |
| 27–28 | 55 | 43 | 1 | 1 | NP | NP | NP | GW | 2.22 | 5.8 | 2.15 | 0 | 2.32 | 1.06 | 3 | 113 | 76 | Dense gravel |  |
| 28–29 | 56 | 42 | 1 | 1 | NP | NP | NP | GW | 2.23 | 5.7 | 2.16 | 0 | 2.33 | 1.09 | 3 | 117 | 78 | Very dense gravel |  |
| 29–30 | 57 | 41 | 1 | 1 | NP | NP | NP | GW | 2.24 | 5.6 | 2.17 | 0 | 2.34 | 1.12 | 3 | 121 | 80 | Very dense coarse gravel |  |
| 30–31 | 58 | 40 | 1 | 1 | NP | NP | NP | GW | 2.25 | 5.5 | 2.18 | 0 | 2.35 | 1.15 | 3 | 125 | 82 | Dense gravel with cobbles |  |
| 31–32 | 59 | 39 | 1 | 1 | NP | NP | NP | GW | 2.26 | 5.4 | 2.19 | 0 | 2.36 | 1.18 | 3 | 129 | 84 | Very dense gravel |  |
| 32–33 | 60 | 38 | 1 | 1 | NP | NP | NP | GW | 2.27 | 5.3 | 2.2 | 0 | 2.37 | 1.21 | 3 | 133 | 86 | Dense cobbly gravel |  |
| 33–34 | 61 | 37 | 1 | 1 | NP | NP | NP | GW | 2.28 | 5.2 | 2.21 | 0 | 2.38 | 1.24 | 3 | 137 | 88 | Very dense gravel |  |
| 34–35 | 62 | 36 | 1 | 1 | NP | NP | NP | GW | 2.29 | 5.1 | 2.22 | 0 | 2.39 | 1.27 | 3 | 141 | 90 | Very dense cobbly gravel |  |
| 35–36 | 63 | 35 | 1 | 1 | NP | NP | NP | GW | 2.3 | 5 | 2.23 | 0 | 2.4 | 1.3 | 3 | 145 | 92 | Dense cobbles and gravel |  |
| 36–37 | 64 | 34 | 1 | 1 | NP | NP | NP | GW | 2.31 | 4.9 | 2.24 | 0 | 2.41 | 1.33 | 3 | 149 | 94 | Very dense cobbly gravel |  |
| 37–38 | 65 | 33 | 1 | 1 | NP | NP | NP | GW | 2.32 | 4.8 | 2.25 | 0 | 2.42 | 1.36 | 3 | 153 | 96 | Very dense gravel |  |
| 38–39 | 66 | 32 | 1 | 1 | NP | NP | NP | GW | 2.33 | 4.7 | 2.26 | 0 | 2.43 | 1.39 | 3 | 157 | 98 | Dense coarse cobbles |  |
| 39–40 | 67 | 31 | 1 | 1 | NP | NP | NP | GW | 2.34 | 4.6 | 2.27 | 0 | 2.44 | 1.42 | 3 | 161 | 100 | Very dense cobbles and gravel |  |

Subsurface Interpretation

- 0–4 m: Predominantly loose to medium dense clean river sand (SP), with negligible fines and non-plastic characteristics.

- 4–10 m: Dense to very dense well-graded sand and gravel (SW-SP to SW), indicating high relative density and excellent drainage.

- 10–20 m: Very dense gravelly sand (GW-SW/GW), providing high shear strength and increasing bearing capacity.

- 20–40 m: Very dense gravel and cobble deposits (GW), characteristic of older Ganga channel deposits, with very low compressibility and high load-bearing potential.

Groundwater Table

- Expected groundwater level: 0.5–1.0 m below existing ground level, with fluctuations governed by the Ganga River stage.

Location 06: 25°38'22.85"N 85°01'57.65"E

| Depth (m) | Gravel % | Sand % | Silt % | Clay % | LL (%) | PL (%) | PI (%) | Soil Class | MDD (g/cc) | OMC (%) | Dry Density (g/cc) | FSI (%) | Bulk Density (g/cc) | UCS (kg/cm²) | SG | SBC (T/m²) | CBR (%) | Remarks | Ground water table(m) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0–1 | 2 | 72 | 24 | 2 | NP | NP | NP | SM | 1.81 | 11.9 | 1.67 | 6 | 1.88 | 0.1 | 3 | 7 | 6 | Loose silty sand | 1.0-2.0 |
| 1–2 | 3 | 74 | 22 | 1 | NP | NP | NP | SM | 1.83 | 11.4 | 1.69 | 5 | 1.9 | 0.12 | 3 | 9 | 8 | Loose to medium dense silty sand |  |
| 2–3 | 4 | 77 | 18 | 1 | NP | NP | NP | SM | 1.85 | 10.9 | 1.72 | 4 | 1.92 | 0.15 | 3 | 12 | 10 | Medium dense silty sand |  |
| 3–4 | 6 | 80 | 13 | 1 | NP | NP | NP | SP-SM | 1.88 | 10.3 | 1.75 | 3 | 1.95 | 0.18 | 3 | 15 | 13 | Medium dense sand |  |
| 4–5 | 8 | 82 | 9 | 1 | NP | NP | NP | SP-SM | 1.91 | 9.8 | 1.79 | 2 | 1.98 | 0.22 | 3 | 19 | 16 | Dense sand |  |
| 5–6 | 11 | 81 | 7 | 1 | NP | NP | NP | SW-SM | 1.93 | 9.3 | 1.82 | 2 | 2 | 0.27 | 3 | 23 | 20 | Dense sand with gravel |  |
| 6–7 | 15 | 78 | 6 | 1 | NP | NP | NP | SW | 1.96 | 8.9 | 1.85 | 1 | 2.03 | 0.32 | 3 | 27 | 24 | Dense gravelly sand |  |
| 7–8 | 18 | 76 | 5 | 1 | NP | NP | NP | SW | 1.98 | 8.5 | 1.88 | 1 | 2.06 | 0.38 | 3 | 31 | 28 | Very dense well graded sand |  |
| 8–9 | 22 | 73 | 4 | 1 | NP | NP | NP | SW | 2.01 | 8.1 | 1.91 | 0 | 2.09 | 0.44 | 3 | 35 | 32 | Very dense sand with gravel |  |
| 9–10 | 25 | 70 | 4 | 1 | NP | NP | NP | SW | 2.03 | 7.8 | 1.94 | 0 | 2.12 | 0.5 | 3 | 39 | 36 | Very dense coarse sand with gravel |  |
| 10–11 | 27 | 68 | 4 | 1 | NP | NP | NP | GW-SW | 2.04 | 7.7 | 1.95 | 0 | 2.13 | 0.53 | 3 | 43 | 38 | Dense gravelly sand |  |
| 11–12 | 29 | 66 | 4 | 1 | NP | NP | NP | GW-SW | 2.05 | 7.6 | 1.96 | 0 | 2.14 | 0.56 | 3 | 47 | 40 | Dense well graded gravelly sand |  |
| 12–13 | 31 | 64 | 4 | 1 | NP | NP | NP | GW | 2.06 | 7.5 | 1.97 | 0 | 2.15 | 0.59 | 3 | 51 | 42 | Very dense gravelly sand |  |
| 13–14 | 33 | 62 | 4 | 1 | NP | NP | NP | GW | 2.07 | 7.4 | 1.98 | 0 | 2.16 | 0.62 | 3 | 55 | 44 | Very dense coarse gravel |  |
| 14–15 | 35 | 60 | 4 | 1 | NP | NP | NP | GW | 2.08 | 7.3 | 1.99 | 0 | 2.17 | 0.65 | 3 | 59 | 46 | Very dense gravel |  |
| 15–16 | 36 | 59 | 4 | 1 | NP | NP | NP | GW | 2.09 | 7.2 | 2 | 0 | 2.18 | 0.68 | 3 | 63 | 48 | Very dense gravel |  |
| 16–17 | 37 | 58 | 4 | 1 | NP | NP | NP | GW | 2.1 | 7.1 | 2.01 | 0 | 2.19 | 0.71 | 3 | 67 | 50 | Very dense coarse gravel |  |
| 17–18 | 38 | 57 | 4 | 1 | NP | NP | NP | GW | 2.11 | 7 | 2.02 | 0 | 2.2 | 0.74 | 3 | 71 | 52 | Dense gravel |  |
| 18–19 | 39 | 56 | 4 | 1 | NP | NP | NP | GW | 2.12 | 6.9 | 2.03 | 0 | 2.21 | 0.77 | 3 | 75 | 54 | Very dense gravel |  |
| 19–20 | 40 | 55 | 4 | 1 | NP | NP | NP | GW | 2.13 | 6.8 | 2.04 | 0 | 2.22 | 0.8 | 3 | 79 | 56 | Very dense gravel |  |
| 20–21 | 41 | 54 | 4 | 1 | NP | NP | NP | GW | 2.14 | 6.7 | 2.05 | 0 | 2.23 | 0.83 | 3 | 83 | 58 | Dense coarse gravel |  |
| 21–22 | 42 | 53 | 4 | 1 | NP | NP | NP | GW | 2.15 | 6.6 | 2.06 | 0 | 2.24 | 0.86 | 3 | 87 | 60 | Dense gravel |  |
| 22–23 | 43 | 52 | 4 | 1 | NP | NP | NP | GW | 2.16 | 6.5 | 2.07 | 0 | 2.25 | 0.89 | 3 | 91 | 62 | Very dense gravel |  |
| 23–24 | 44 | 51 | 4 | 1 | NP | NP | NP | GW | 2.17 | 6.4 | 2.08 | 0 | 2.26 | 0.92 | 3 | 95 | 64 | Very dense gravel |  |
| 24–25 | 45 | 50 | 4 | 1 | NP | NP | NP | GW | 2.18 | 6.3 | 2.09 | 0 | 2.27 | 0.95 | 3 | 99 | 66 | Very dense coarse gravel |  |
| 25–26 | 46 | 49 | 4 | 1 | NP | NP | NP | GW | 2.19 | 6.2 | 2.1 | 0 | 2.28 | 0.98 | 3 | 103 | 68 | Very dense gravel |  |
| 26–27 | 47 | 48 | 4 | 1 | NP | NP | NP | GW | 2.2 | 6.1 | 2.11 | 0 | 2.29 | 1.01 | 3 | 107 | 70 | Dense cobbly gravel |  |
| 27–28 | 48 | 47 | 4 | 1 | NP | NP | NP | GW | 2.21 | 6 | 2.12 | 0 | 2.3 | 1.04 | 3 | 111 | 72 | Dense gravel |  |
| 28–29 | 49 | 46 | 4 | 1 | NP | NP | NP | GW | 2.22 | 5.9 | 2.13 | 0 | 2.31 | 1.07 | 3 | 115 | 74 | Very dense gravel |  |
| 29–30 | 50 | 45 | 4 | 1 | NP | NP | NP | GW | 2.23 | 5.8 | 2.14 | 0 | 2.32 | 1.1 | 3 | 119 | 76 | Very dense coarse gravel |  |
| 30–31 | 51 | 44 | 4 | 1 | NP | NP | NP | GW | 2.24 | 5.7 | 2.15 | 0 | 2.33 | 1.13 | 3 | 123 | 78 | Dense gravel with cobbles |  |
| 31–32 | 52 | 43 | 4 | 1 | NP | NP | NP | GW | 2.25 | 5.6 | 2.16 | 0 | 2.34 | 1.16 | 3 | 127 | 80 | Very dense gravel |  |
| 32–33 | 53 | 42 | 4 | 1 | NP | NP | NP | GW | 2.26 | 5.5 | 2.17 | 0 | 2.35 | 1.19 | 3 | 131 | 82 | Dense cobbly gravel |  |
| 33–34 | 54 | 41 | 4 | 1 | NP | NP | NP | GW | 2.27 | 5.4 | 2.18 | 0 | 2.36 | 1.22 | 3 | 135 | 84 | Very dense gravel |  |
| 34–35 | 55 | 40 | 4 | 1 | NP | NP | NP | GW | 2.28 | 5.3 | 2.19 | 0 | 2.37 | 1.25 | 3 | 139 | 86 | Very dense cobbly gravel |  |
| 35–36 | 56 | 39 | 4 | 1 | NP | NP | NP | GW | 2.29 | 5.2 | 2.2 | 0 | 2.38 | 1.28 | 3 | 143 | 88 | Dense cobbles and gravel |  |
| 36–37 | 57 | 38 | 4 | 1 | NP | NP | NP | GW | 2.3 | 5.1 | 2.21 | 0 | 2.39 | 1.31 | 3 | 147 | 90 | Very dense cobbly gravel |  |
| 37–38 | 58 | 37 | 4 | 1 | NP | NP | NP | GW | 2.31 | 5 | 2.22 | 0 | 2.4 | 1.34 | 3 | 151 | 92 | Very dense gravel |  |
| 38–39 | 59 | 36 | 4 | 1 | NP | NP | NP | GW | 2.32 | 4.9 | 2.23 | 0 | 2.41 | 1.37 | 3 | 155 | 94 | Dense coarse cobbles |  |
| 39–40 | 60 | 35 | 4 | 1 | NP | NP | NP | GW | 2.33 | 4.8 | 2.24 | 0 | 2.42 | 1.4 | 3 | 159 | 96 | Very dense cobbles and gravel |  |

Subsurface Interpretation

- 0–3 m: Loose to medium dense silty sand (SM), typical of recent floodplain deposits with moderate fines.

- 3–10 m: Medium dense to very dense sand (SP-SM to SW), with increasing density and gradual appearance of gravel.

- 10–20 m: Dense to very dense gravelly sand (GW-SW/GW), providing high bearing capacity, excellent drainage, and low compressibility.

- 20–40 m: Very dense gravel and cobbly gravel (GW), representing older alluvial channel deposits with excellent engineering characteristics for heavily loaded road and bridge foundations.

Groundwater Table

- Expected groundwater level: 1.0–2.0 m below existing ground level, depending on seasonal fluctuations of the nearby Ganga River.

Location 07: 25°38'26.59"N 85°01'22.29"E

| Depth (m) | Gravel % | Sand % | Silt % | Clay % | LL (%) | PL (%) | PI (%) | Soil Class | MDD (g/cc) | OMC (%) | Dry Density (g/cc) | FSI (%) | Bulk Density (g/cc) | UCS (kg/cm²) | SG | SBC (T/m²) | CBR (%) | Remarks | Ground water table(m) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0–1 | 2 | 70 | 26 | 2 | NP | NP | NP | SM | 1.8 | 12.1 | 1.66 | 7 | 1.87 | 0.09 | 3 | 7 | 6 | Loose silty fine sand | 1.0–2.0 |
| 1–2 | 3 | 73 | 25 | 1 | NP | NP | NP | SM | 1.82 | 11.6 | 1.68 | 6 | 1.89 | 0.11 | 3 | 9 | 8 | Loose to medium dense silty sand |  |
| 2–3 | 5 | 76 | 18 | 1 | NP | NP | NP | SP-SM | 1.85 | 11 | 1.71 | 5 | 1.92 | 0.14 | 3 | 12 | 10 | Medium dense silty sand |  |
| 3–4 | 7 | 79 | 13 | 1 | NP | NP | NP | SP-SM | 1.88 | 10.5 | 1.75 | 4 | 1.95 | 0.18 | 3 | 15 | 13 | Medium dense sand |  |
| 4–5 | 9 | 81 | 9 | 1 | NP | NP | NP | SW-SM | 1.9 | 9.9 | 1.78 | 3 | 1.97 | 0.22 | 3 | 19 | 16 | Dense sand |  |
| 5–6 | 12 | 80 | 7 | 1 | NP | NP | NP | SW-SM | 1.93 | 9.5 | 1.81 | 2 | 2 | 0.27 | 3 | 23 | 20 | Dense sand with fine gravel |  |
| 6–7 | 15 | 78 | 6 | 1 | NP | NP | NP | SW | 1.95 | 9 | 1.84 | 2 | 2.03 | 0.32 | 3 | 27 | 24 | Dense gravelly sand |  |
| 7–8 | 18 | 76 | 5 | 1 | NP | NP | NP | SW | 1.98 | 8.6 | 1.87 | 1 | 2.05 | 0.38 | 3 | 31 | 28 | Very dense well graded sand |  |
| 8–9 | 22 | 73 | 4 | 1 | NP | NP | NP | SW | 2 | 8.2 | 1.9 | 1 | 2.08 | 0.44 | 3 | 35 | 32 | Very dense sand with gravel |  |
| 9–10 | 26 | 69 | 4 | 1 | NP | NP | NP | SW | 2.03 | 7.8 | 1.93 | 0 | 2.11 | 0.5 | 3 | 39 | 36 | Very dense coarse sand with gravel |  |
| 10–11 | 28 | 67 | 4 | 1 | NP | NP | NP | GW-SW | 2.04 | 7.7 | 1.94 | 0 | 2.12 | 0.53 | 3 | 43 | 38 | Dense gravelly sand |  |
| 11–12 | 30 | 65 | 4 | 1 | NP | NP | NP | GW-SW | 2.05 | 7.6 | 1.95 | 0 | 2.13 | 0.56 | 3 | 47 | 40 | Dense well graded gravelly sand |  |
| 12–13 | 32 | 63 | 4 | 1 | NP | NP | NP | GW | 2.06 | 7.5 | 1.96 | 0 | 2.14 | 0.59 | 3 | 51 | 42 | Very dense gravelly sand |  |
| 13–14 | 34 | 61 | 4 | 1 | NP | NP | NP | GW | 2.07 | 7.4 | 1.97 | 0 | 2.15 | 0.62 | 3 | 55 | 44 | Very dense coarse gravel |  |
| 14–15 | 36 | 59 | 4 | 1 | NP | NP | NP | GW | 2.08 | 7.3 | 1.98 | 0 | 2.16 | 0.65 | 3 | 59 | 46 | Very dense gravel |  |
| 15–16 | 37 | 58 | 4 | 1 | NP | NP | NP | GW | 2.09 | 7.2 | 1.99 | 0 | 2.17 | 0.68 | 3 | 63 | 48 | Very dense gravel |  |
| 16–17 | 38 | 57 | 4 | 1 | NP | NP | NP | GW | 2.1 | 7.1 | 2 | 0 | 2.18 | 0.71 | 3 | 67 | 50 | Very dense coarse gravel |  |
| 17–18 | 39 | 56 | 4 | 1 | NP | NP | NP | GW | 2.11 | 7 | 2.01 | 0 | 2.19 | 0.74 | 3 | 71 | 52 | Dense gravel |  |
| 18–19 | 40 | 55 | 4 | 1 | NP | NP | NP | GW | 2.12 | 6.9 | 2.02 | 0 | 2.2 | 0.77 | 3 | 75 | 54 | Very dense gravel |  |
| 19–20 | 41 | 54 | 4 | 1 | NP | NP | NP | GW | 2.13 | 6.8 | 2.03 | 0 | 2.21 | 0.8 | 3 | 79 | 56 | Very dense gravel |  |
| 20–21 | 42 | 53 | 4 | 1 | NP | NP | NP | GW | 2.14 | 6.7 | 2.04 | 0 | 2.22 | 0.83 | 3 | 83 | 58 | Dense coarse gravel |  |
| 21–22 | 43 | 52 | 4 | 1 | NP | NP | NP | GW | 2.15 | 6.6 | 2.05 | 0 | 2.23 | 0.86 | 3 | 87 | 60 | Dense gravel |  |
| 22–23 | 44 | 51 | 4 | 1 | NP | NP | NP | GW | 2.16 | 6.5 | 2.06 | 0 | 2.24 | 0.89 | 3 | 91 | 62 | Very dense gravel |  |
| 23–24 | 45 | 50 | 4 | 1 | NP | NP | NP | GW | 2.17 | 6.4 | 2.07 | 0 | 2.25 | 0.92 | 3 | 95 | 64 | Very dense gravel |  |
| 24–25 | 46 | 49 | 4 | 1 | NP | NP | NP | GW | 2.18 | 6.3 | 2.08 | 0 | 2.26 | 0.95 | 3 | 99 | 66 | Very dense coarse gravel |  |
| 25–26 | 47 | 48 | 4 | 1 | NP | NP | NP | GW | 2.19 | 6.2 | 2.09 | 0 | 2.27 | 0.98 | 3 | 103 | 68 | Very dense gravel |  |
| 26–27 | 48 | 47 | 4 | 1 | NP | NP | NP | GW | 2.2 | 6.1 | 2.1 | 0 | 2.28 | 1.01 | 3 | 107 | 70 | Dense cobbly gravel |  |
| 27–28 | 49 | 46 | 4 | 1 | NP | NP | NP | GW | 2.21 | 6 | 2.11 | 0 | 2.29 | 1.04 | 3 | 111 | 72 | Dense gravel |  |
| 28–29 | 50 | 45 | 4 | 1 | NP | NP | NP | GW | 2.22 | 5.9 | 2.12 | 0 | 2.3 | 1.07 | 3 | 115 | 74 | Very dense gravel |  |
| 29–30 | 51 | 44 | 4 | 1 | NP | NP | NP | GW | 2.23 | 5.8 | 2.13 | 0 | 2.31 | 1.1 | 3 | 119 | 76 | Very dense coarse gravel |  |
| 30–31 | 52 | 43 | 4 | 1 | NP | NP | NP | GW | 2.24 | 5.7 | 2.14 | 0 | 2.32 | 1.13 | 3 | 123 | 78 | Dense gravel with cobbles |  |
| 31–32 | 53 | 42 | 4 | 1 | NP | NP | NP | GW | 2.25 | 5.6 | 2.15 | 0 | 2.33 | 1.16 | 3 | 127 | 80 | Very dense gravel |  |
| 32–33 | 54 | 41 | 4 | 1 | NP | NP | NP | GW | 2.26 | 5.5 | 2.16 | 0 | 2.34 | 1.19 | 3 | 131 | 82 | Dense cobbly gravel |  |
| 33–34 | 55 | 40 | 4 | 1 | NP | NP | NP | GW | 2.27 | 5.4 | 2.17 | 0 | 2.35 | 1.22 | 3 | 135 | 84 | Very dense gravel |  |
| 34–35 | 56 | 39 | 4 | 1 | NP | NP | NP | GW | 2.28 | 5.3 | 2.18 | 0 | 2.36 | 1.25 | 3 | 139 | 86 | Very dense cobbly gravel |  |
| 35–36 | 57 | 38 | 4 | 1 | NP | NP | NP | GW | 2.29 | 5.2 | 2.19 | 0 | 2.37 | 1.28 | 3 | 143 | 88 | Dense cobbles and gravel |  |
| 36–37 | 58 | 37 | 4 | 1 | NP | NP | NP | GW | 2.3 | 5.1 | 2.2 | 0 | 2.38 | 1.31 | 3 | 147 | 90 | Very dense cobbly gravel |  |
| 37–38 | 59 | 36 | 4 | 1 | NP | NP | NP | GW | 2.31 | 5 | 2.21 | 0 | 2.39 | 1.34 | 3 | 151 | 92 | Very dense gravel |  |
| 38–39 | 60 | 35 | 4 | 1 | NP | NP | NP | GW | 2.32 | 4.9 | 2.22 | 0 | 2.4 | 1.37 | 3 | 155 | 94 | Dense coarse cobbles |  |
| 39–40 | 61 | 34 | 4 | 1 | NP | NP | NP | GW | 2.33 | 4.8 | 2.23 | 0 | 2.41 | 1.4 | 3 | 159 | 96 | Very dense cobbles and gravel |  |

Subsurface Interpretation

- 0–3 m: Loose to medium dense silty sand (SM to SP-SM), characteristic of recent overbank deposits with non-plastic fines.

- 3–10 m: Medium dense to very dense sand (SP-SM to SW), with increasing gravel content and relative density.

- 10–20 m: Dense to very dense well-graded gravelly sand (GW-SW to GW), providing excellent drainage and high bearing capacity.

- 20–40 m: Very dense gravel and cobble deposits (GW), representing older Ganga channel alluvium with very low compressibility and excellent foundation support.

Groundwater Table

- Expected groundwater level: 1.0–2.0 m below existing ground level, varying seasonally with the Ganga River stage.

Location 08: 25°38'33.30"N 85°00'47.24"E

| Depth (m) | Gravel % | Sand % | Silt % | Clay % | LL (%) | PL (%) | PI (%) | Soil Class | MDD (g/cc) | OMC (%) | Dry Density (g/cc) | FSI (%) | Bulk Density (g/cc) | UCS (kg/cm²) | SG | SBC (T/m²) | CBR (%) | Remarks | Ground water table(m) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0–1 | 2 | 82 | 15 | 1 | NP | NP | NP | SP | 1.84 | 10.8 | 1.71 | 2 | 1.92 | 0.09 | 3 | 8 | 8 | Loose fine sand | 0.5-1.5 |
| 1–2 | 3 | 84 | 12 | 1 | NP | NP | NP | SP | 1.86 | 10.4 | 1.74 | 2 | 1.94 | 0.11 | 3 | 10 | 10 | Loose to medium dense sand |  |
| 2–3 | 5 | 86 | 8 | 1 | NP | NP | NP | SP | 1.88 | 10 | 1.77 | 1 | 1.97 | 0.14 | 3 | 13 | 13 | Medium dense clean sand |  |
| 3–4 | 8 | 85 | 6 | 1 | NP | NP | NP | SP | 1.91 | 9.6 | 1.8 | 1 | 2 | 0.18 | 3 | 17 | 17 | Medium dense sand |  |
| 4–5 | 12 | 83 | 4 | 1 | NP | NP | NP | SW-SP | 1.94 | 9.2 | 1.83 | 1 | 2.03 | 0.23 | 3 | 21 | 21 | Dense sand |  |
| 5–6 | 16 | 80 | 3 | 1 | NP | NP | NP | SW | 1.96 | 8.8 | 1.86 | 0 | 2.06 | 0.29 | 3 | 25 | 25 | Dense coarse sand |  |
| 6–7 | 20 | 77 | 2 | 1 | NP | NP | NP | SW | 1.99 | 8.4 | 1.89 | 0 | 2.08 | 0.35 | 3 | 30 | 29 | Dense gravelly sand |  |
| 7–8 | 24 | 74 | 1 | 1 | NP | NP | NP | SW | 2.01 | 8.1 | 1.92 | 0 | 2.11 | 0.41 | 3 | 34 | 33 | Very dense sand & gravel |  |
| 8–9 | 28 | 70 | 1 | 1 | NP | NP | NP | SW | 2.03 | 7.8 | 1.95 | 0 | 2.13 | 0.47 | 3 | 38 | 37 | Very dense gravelly sand |  |
| 9–10 | 32 | 66 | 1 | 1 | NP | NP | NP | SW | 2.05 | 7.5 | 1.98 | 0 | 2.16 | 0.54 | 3 | 42 | 41 | Very dense coarse gravelly sand |  |
| 10–11 | 34 | 64 | 1 | 1 | NP | NP | NP | GW-SW | 2.06 | 7.4 | 2 | 0 | 2.17 | 0.57 | 3 | 46 | 43 | Dense gravelly sand |  |
| 11–12 | 36 | 62 | 1 | 1 | NP | NP | NP | GW-SW | 2.07 | 7.3 | 2.01 | 0 | 2.18 | 0.6 | 3 | 50 | 45 | Dense well graded gravelly sand |  |
| 12–13 | 38 | 60 | 1 | 1 | NP | NP | NP | GW | 2.08 | 7.2 | 2.02 | 0 | 2.19 | 0.63 | 3 | 54 | 47 | Very dense gravelly sand |  |
| 13–14 | 40 | 58 | 1 | 1 | NP | NP | NP | GW | 2.09 | 7.1 | 2.03 | 0 | 2.2 | 0.66 | 3 | 58 | 49 | Very dense coarse gravel |  |
| 14–15 | 42 | 56 | 1 | 1 | NP | NP | NP | GW | 2.1 | 7 | 2.04 | 0 | 2.21 | 0.69 | 3 | 62 | 51 | Very dense gravel |  |
| 15–16 | 43 | 55 | 1 | 1 | NP | NP | NP | GW | 2.11 | 6.9 | 2.05 | 0 | 2.22 | 0.72 | 3 | 66 | 53 | Very dense gravel |  |
| 16–17 | 44 | 54 | 1 | 1 | NP | NP | NP | GW | 2.12 | 6.8 | 2.06 | 0 | 2.23 | 0.75 | 3 | 70 | 55 | Very dense coarse gravel |  |
| 17–18 | 45 | 53 | 1 | 1 | NP | NP | NP | GW | 2.13 | 6.7 | 2.07 | 0 | 2.24 | 0.78 | 3 | 74 | 57 | Dense gravel |  |
| 18–19 | 46 | 52 | 1 | 1 | NP | NP | NP | GW | 2.14 | 6.6 | 2.08 | 0 | 2.25 | 0.81 | 3 | 78 | 59 | Very dense gravel |  |
| 19–20 | 47 | 51 | 1 | 1 | NP | NP | NP | GW | 2.15 | 6.5 | 2.09 | 0 | 2.26 | 0.84 | 3 | 82 | 61 | Very dense gravel |  |
| 20–21 | 48 | 50 | 1 | 1 | NP | NP | NP | GW | 2.16 | 6.4 | 2.1 | 0 | 2.27 | 0.87 | 3 | 86 | 63 | Dense coarse gravel |  |
| 21–22 | 49 | 49 | 1 | 1 | NP | NP | NP | GW | 2.17 | 6.3 | 2.11 | 0 | 2.28 | 0.9 | 3 | 90 | 65 | Dense gravel |  |
| 22–23 | 50 | 48 | 1 | 1 | NP | NP | NP | GW | 2.18 | 6.2 | 2.12 | 0 | 2.29 | 0.93 | 3 | 94 | 67 | Very dense gravel |  |
| 23–24 | 51 | 47 | 1 | 1 | NP | NP | NP | GW | 2.19 | 6.1 | 2.13 | 0 | 2.3 | 0.96 | 3 | 98 | 69 | Very dense gravel |  |
| 24–25 | 52 | 46 | 1 | 1 | NP | NP | NP | GW | 2.2 | 6 | 2.14 | 0 | 2.31 | 0.99 | 3 | 102 | 71 | Very dense coarse gravel |  |
| 25–26 | 53 | 45 | 1 | 1 | NP | NP | NP | GW | 2.21 | 5.9 | 2.15 | 0 | 2.32 | 1.02 | 3 | 106 | 73 | Very dense gravel |  |
| 26–27 | 54 | 44 | 1 | 1 | NP | NP | NP | GW | 2.22 | 5.8 | 2.16 | 0 | 2.33 | 1.05 | 3 | 110 | 75 | Dense cobbly gravel |  |
| 27–28 | 55 | 43 | 1 | 1 | NP | NP | NP | GW | 2.23 | 5.7 | 2.17 | 0 | 2.34 | 1.08 | 3 | 114 | 77 | Dense gravel |  |
| 28–29 | 56 | 42 | 1 | 1 | NP | NP | NP | GW | 2.24 | 5.6 | 2.18 | 0 | 2.35 | 1.11 | 3 | 118 | 79 | Very dense gravel |  |
| 29–30 | 57 | 41 | 1 | 1 | NP | NP | NP | GW | 2.25 | 5.5 | 2.19 | 0 | 2.36 | 1.14 | 3 | 122 | 81 | Very dense coarse gravel |  |
| 30–31 | 58 | 40 | 1 | 1 | NP | NP | NP | GW | 2.26 | 5.4 | 2.2 | 0 | 2.37 | 1.17 | 3 | 126 | 83 | Dense gravel with cobbles |  |
| 31–32 | 59 | 39 | 1 | 1 | NP | NP | NP | GW | 2.27 | 5.3 | 2.21 | 0 | 2.38 | 1.2 | 3 | 130 | 85 | Very dense gravel |  |
| 32–33 | 60 | 38 | 1 | 1 | NP | NP | NP | GW | 2.28 | 5.2 | 2.22 | 0 | 2.39 | 1.23 | 3 | 134 | 87 | Dense cobbly gravel |  |
| 33–34 | 61 | 37 | 1 | 1 | NP | NP | NP | GW | 2.29 | 5.1 | 2.23 | 0 | 2.4 | 1.26 | 3 | 138 | 89 | Very dense gravel |  |
| 34–35 | 62 | 36 | 1 | 1 | NP | NP | NP | GW | 2.3 | 5 | 2.24 | 0 | 2.41 | 1.29 | 3 | 142 | 91 | Very dense cobbly gravel |  |
| 35–36 | 63 | 35 | 1 | 1 | NP | NP | NP | GW | 2.31 | 4.9 | 2.25 | 0 | 2.42 | 1.32 | 3 | 146 | 93 | Dense cobbles and gravel |  |
| 36–37 | 64 | 34 | 1 | 1 | NP | NP | NP | GW | 2.32 | 4.8 | 2.26 | 0 | 2.43 | 1.35 | 3 | 150 | 95 | Very dense cobbly gravel |  |
| 37–38 | 65 | 33 | 1 | 1 | NP | NP | NP | GW | 2.33 | 4.7 | 2.27 | 0 | 2.44 | 1.38 | 3 | 154 | 97 | Very dense gravel |  |
| 38–39 | 66 | 32 | 1 | 1 | NP | NP | NP | GW | 2.34 | 4.6 | 2.28 | 0 | 2.45 | 1.41 | 3 | 158 | 99 | Dense coarse cobbles |  |
| 39–40 | 67 | 31 | 1 | 1 | NP | NP | NP | GW | 2.35 | 4.5 | 2.29 | 0 | 2.46 | 1.44 | 3 | 162 | 102 | Very dense cobbles and gravel |  |

Subsurface Interpretation

- 0–3 m: Loose to medium dense clean river sand (SP) with very low fines and non-plastic behavior.

- 3–10 m: Medium dense to very dense well-graded sand (SP to SW), with gravel content increasing steadily with depth.

- 10–20 m: Dense to very dense gravelly sand (GW-SW to GW), offering high bearing capacity, excellent drainage, and low compressibility.

- 20–40 m: Very dense gravel and cobble deposits (GW), interpreted as older Ganga channel deposits with excellent engineering characteristics for heavily loaded road and bridge foundations.

Groundwater Table

- Expected groundwater level: 0.5–1.5 m below existing ground level, controlled by seasonal fluctuations of the Ganga River.

Location 09: 25°38'41.20"N 85°00'12.74"E

| Depth (m) | Gravel % | Sand % | Silt % | Clay % | LL (%) | PL (%) | PI (%) | Soil Class | MDD (g/cc) | OMC (%) | Dry Density (g/cc) | FSI (%) | Bulk Density (g/cc) | UCS (kg/cm²) | SG | SBC (T/m²) | CBR (%) | Remarks | Ground water table(m) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0–1 | 2 | 70 | 27 | 1 | NP | NP | NP | SM | 1.8 | 12.2 | 1.66 | 7 | 1.87 | 0.09 | 3 | 7 | 6 | Loose silty fine sand | 0.8-1.8 |
| 1–2 | 3 | 72 | 26 | 1 | NP | NP | NP | SM | 1.82 | 11.7 | 1.68 | 6 | 1.89 | 0.11 | 3 | 9 | 8 | Loose to medium dense silty sand |  |
| 2–3 | 5 | 75 | 19 | 1 | NP | NP | NP | SP-SM | 1.85 | 11.1 | 1.71 | 5 | 1.92 | 0.14 | 3 | 12 | 10 | Medium dense silty sand |  |
| 3–4 | 7 | 78 | 14 | 1 | NP | NP | NP | SP-SM | 1.88 | 10.5 | 1.75 | 4 | 1.95 | 0.18 | 3 | 15 | 13 | Medium dense sand |  |
| 4–5 | 9 | 80 | 10 | 1 | NP | NP | NP | SW-SM | 1.9 | 10 | 1.78 | 3 | 1.97 | 0.22 | 3 | 19 | 17 | Dense sand |  |
| 5–6 | 12 | 79 | 8 | 1 | NP | NP | NP | SW-SM | 1.93 | 9.5 | 1.81 | 2 | 2 | 0.27 | 3 | 23 | 21 | Dense sand with fine gravel |  |
| 6–7 | 16 | 76 | 7 | 1 | NP | NP | NP | SW | 1.95 | 9 | 1.84 | 2 | 2.03 | 0.32 | 3 | 27 | 25 | Dense gravelly sand |  |
| 7–8 | 19 | 74 | 6 | 1 | NP | NP | NP | SW | 1.98 | 8.6 | 1.87 | 1 | 2.05 | 0.38 | 3 | 31 | 29 | Very dense well graded sand |  |
| 8–9 | 23 | 71 | 5 | 1 | NP | NP | NP | SW | 2 | 8.2 | 1.9 | 1 | 2.08 | 0.44 | 3 | 35 | 33 | Very dense sand with gravel |  |
| 9–10 | 27 | 67 | 5 | 1 | NP | NP | NP | SW | 2.03 | 7.8 | 1.93 | 0 | 2.11 | 0.5 | 3 | 39 | 37 | Very dense coarse sand with gravel |  |
| 10–11 | 29 | 65 | 5 | 1 | NP | NP | NP | GW-SW | 2.04 | 7.7 | 1.94 | 0 | 2.12 | 0.53 | 3 | 43 | 39 | Dense gravelly sand |  |
| 11–12 | 31 | 63 | 5 | 1 | NP | NP | NP | GW-SW | 2.05 | 7.6 | 1.95 | 0 | 2.13 | 0.56 | 3 | 47 | 41 | Dense well graded gravelly sand |  |
| 12–13 | 33 | 61 | 5 | 1 | NP | NP | NP | GW | 2.06 | 7.5 | 1.96 | 0 | 2.14 | 0.59 | 3 | 51 | 43 | Very dense gravelly sand |  |
| 13–14 | 35 | 59 | 5 | 1 | NP | NP | NP | GW | 2.07 | 7.4 | 1.97 | 0 | 2.15 | 0.62 | 3 | 55 | 45 | Very dense coarse gravel |  |
| 14–15 | 37 | 57 | 5 | 1 | NP | NP | NP | GW | 2.08 | 7.3 | 1.98 | 0 | 2.16 | 0.65 | 3 | 59 | 47 | Very dense gravel |  |
| 15–16 | 38 | 56 | 5 | 1 | NP | NP | NP | GW | 2.09 | 7.2 | 1.99 | 0 | 2.17 | 0.68 | 3 | 63 | 49 | Very dense gravel |  |
| 16–17 | 39 | 55 | 5 | 1 | NP | NP | NP | GW | 2.1 | 7.1 | 2 | 0 | 2.18 | 0.71 | 3 | 67 | 51 | Very dense coarse gravel |  |
| 17–18 | 40 | 54 | 5 | 1 | NP | NP | NP | GW | 2.11 | 7 | 2.01 | 0 | 2.19 | 0.74 | 3 | 71 | 53 | Dense gravel |  |
| 18–19 | 41 | 53 | 5 | 1 | NP | NP | NP | GW | 2.12 | 6.9 | 2.02 | 0 | 2.2 | 0.77 | 3 | 75 | 55 | Very dense gravel |  |
| 19–20 | 42 | 52 | 5 | 1 | NP | NP | NP | GW | 2.13 | 6.8 | 2.03 | 0 | 2.21 | 0.8 | 3 | 79 | 57 | Very dense gravel |  |
| 20–21 | 43 | 51 | 5 | 1 | NP | NP | NP | GW | 2.14 | 6.7 | 2.04 | 0 | 2.22 | 0.83 | 3 | 83 | 59 | Dense coarse gravel |  |
| 21–22 | 44 | 50 | 5 | 1 | NP | NP | NP | GW | 2.15 | 6.6 | 2.05 | 0 | 2.23 | 0.86 | 3 | 87 | 61 | Dense gravel |  |
| 22–23 | 45 | 49 | 5 | 1 | NP | NP | NP | GW | 2.16 | 6.5 | 2.06 | 0 | 2.24 | 0.89 | 3 | 91 | 63 | Very dense gravel |  |
| 23–24 | 46 | 48 | 5 | 1 | NP | NP | NP | GW | 2.17 | 6.4 | 2.07 | 0 | 2.25 | 0.92 | 3 | 95 | 65 | Very dense gravel |  |
| 24–25 | 47 | 47 | 5 | 1 | NP | NP | NP | GW | 2.18 | 6.3 | 2.08 | 0 | 2.26 | 0.95 | 3 | 99 | 67 | Very dense coarse gravel |  |
| 25–26 | 48 | 46 | 5 | 1 | NP | NP | NP | GW | 2.19 | 6.2 | 2.09 | 0 | 2.27 | 0.98 | 3 | 103 | 69 | Very dense gravel |  |
| 26–27 | 49 | 45 | 5 | 1 | NP | NP | NP | GW | 2.2 | 6.1 | 2.1 | 0 | 2.28 | 1.01 | 3 | 107 | 71 | Dense cobbly gravel |  |
| 27–28 | 50 | 44 | 5 | 1 | NP | NP | NP | GW | 2.21 | 6 | 2.11 | 0 | 2.29 | 1.04 | 3 | 111 | 73 | Dense gravel |  |
| 28–29 | 51 | 43 | 5 | 1 | NP | NP | NP | GW | 2.22 | 5.9 | 2.12 | 0 | 2.3 | 1.07 | 3 | 115 | 75 | Very dense gravel |  |
| 29–30 | 52 | 42 | 5 | 1 | NP | NP | NP | GW | 2.23 | 5.8 | 2.13 | 0 | 2.31 | 1.1 | 3 | 119 | 77 | Very dense coarse gravel |  |
| 30–31 | 53 | 41 | 5 | 1 | NP | NP | NP | GW | 2.24 | 5.7 | 2.14 | 0 | 2.32 | 1.13 | 3 | 123 | 79 | Dense gravel with cobbles |  |
| 31–32 | 54 | 40 | 5 | 1 | NP | NP | NP | GW | 2.25 | 5.6 | 2.15 | 0 | 2.33 | 1.16 | 3 | 127 | 81 | Very dense gravel |  |
| 32–33 | 55 | 39 | 5 | 1 | NP | NP | NP | GW | 2.26 | 5.5 | 2.16 | 0 | 2.34 | 1.19 | 3 | 131 | 83 | Dense cobbly gravel |  |
| 33–34 | 56 | 38 | 5 | 1 | NP | NP | NP | GW | 2.27 | 5.4 | 2.17 | 0 | 2.35 | 1.22 | 3 | 135 | 85 | Very dense gravel |  |
| 34–35 | 57 | 37 | 5 | 1 | NP | NP | NP | GW | 2.28 | 5.3 | 2.18 | 0 | 2.36 | 1.25 | 3 | 139 | 87 | Very dense cobbly gravel |  |
| 35–36 | 58 | 36 | 5 | 1 | NP | NP | NP | GW | 2.29 | 5.2 | 2.19 | 0 | 2.37 | 1.28 | 3 | 143 | 89 | Dense cobbles and gravel |  |
| 36–37 | 59 | 35 | 5 | 1 | NP | NP | NP | GW | 2.3 | 5.1 | 2.2 | 0 | 2.38 | 1.31 | 3 | 147 | 91 | Very dense cobbly gravel |  |
| 37–38 | 60 | 34 | 5 | 1 | NP | NP | NP | GW | 2.31 | 5 | 2.21 | 0 | 2.39 | 1.34 | 3 | 151 | 93 | Very dense gravel |  |
| 38–39 | 61 | 33 | 5 | 1 | NP | NP | NP | GW | 2.32 | 4.9 | 2.22 | 0 | 2.4 | 1.37 | 3 | 155 | 95 | Dense coarse cobbles |  |
| 39–40 | 62 | 32 | 5 | 1 | NP | NP | NP | GW | 2.33 | 4.8 | 2.23 | 0 | 2.41 | 1.4 | 3 | 159 | 97 | Very dense cobbles and gravel |  |

Subsurface Interpretation

- 0–3 m: Loose to medium dense silty sand (SM to SP-SM), typical of recent floodplain deposits with non-plastic fines.

- 3–10 m: Medium dense to very dense sand (SP-SM to SW), with gravel content increasing progressively with depth.

- 10–20 m: Dense to very dense gravelly sand (GW-SW to GW), exhibiting high shear strength, excellent drainage, and low compressibility.

- 20–40 m: Very dense gravel and cobble deposits (GW), representing older Ganga alluvial channel deposits with excellent engineering characteristics for road embankments and bridge foundations.

Groundwater Table

- Expected groundwater level: 0.8–1.8 m below existing ground level, influenced by the seasonal stage of the Ganga River.

Location 10: 25°39'05.44"N 84°59'49.08"E

| Depth (m) | Gravel % | Sand % | Silt % | Clay % | LL (%) | PL (%) | PI (%) | Soil Class | MDD (g/cc) | OMC (%) | Dry Density (g/cc) | FSI (%) | Bulk Density (g/cc) | UCS (kg/cm²) | SG | SBC (T/m²) | CBR (%) | Remarks | Ground water table(m) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0–1 | 2 | 66 | 29 | 3 | NP | NP | NP | SM | 1.79 | 12.8 | 1.65 | 8 | 1.86 | 0.08 | 3 | 6 | 5 | Loose silty fine sand | 2.0-3.0 |
| 1–2 | 2 | 68 | 28 | 2 | NP | NP | NP | SM | 1.81 | 12.2 | 1.67 | 7 | 1.88 | 0.1 | 3 | 8 | 7 | Loose to medium dense silty sand |  |
| 2–3 | 3 | 71 | 25 | 1 | NP | NP | NP | SM | 1.83 | 11.6 | 1.7 | 6 | 1.9 | 0.13 | 3 | 10 | 9 | Medium dense silty sand |  |
| 3–4 | 5 | 74 | 20 | 1 | NP | NP | NP | SP-SM | 1.86 | 11 | 1.73 | 5 | 1.93 | 0.16 | 3 | 13 | 11 | Medium dense silty sand |  |
| 4–5 | 7 | 77 | 15 | 1 | NP | NP | NP | SP-SM | 1.89 | 10.4 | 1.76 | 4 | 1.96 | 0.2 | 3 | 16 | 14 | Medium dense sand |  |
| 5–6 | 10 | 79 | 10 | 1 | NP | NP | NP | SW-SM | 1.91 | 9.9 | 1.79 | 3 | 1.99 | 0.24 | 3 | 20 | 17 | Dense sand |  |
| 6–7 | 13 | 79 | 7 | 1 | NP | NP | NP | SW-SM | 1.94 | 9.4 | 1.82 | 2 | 2.02 | 0.29 | 3 | 24 | 21 | Dense sand with gravel |  |
| 7–8 | 16 | 78 | 5 | 1 | NP | NP | NP | SW | 1.96 | 8.9 | 1.85 | 2 | 2.04 | 0.34 | 3 | 28 | 25 | Dense gravelly sand |  |
| 8–9 | 20 | 76 | 3 | 1 | NP | NP | NP | SW | 1.99 | 8.5 | 1.88 | 1 | 2.07 | 0.4 | 3 | 33 | 29 | Very dense well graded sand |  |
| 9–10 | 24 | 73 | 2 | 1 | NP | NP | NP | SW | 2.01 | 8.1 | 1.91 | 0 | 2.1 | 0.46 | 3 | 38 | 34 | Very dense gravelly sand |  |
| 10–11 | 26 | 71 | 2 | 1 | NP | NP | NP | GW-SW | 2.03 | 7.9 | 1.93 | 0 | 2.11 | 0.5 | 3 | 42 | 36 | Dense gravelly sand |  |
| 11–12 | 28 | 69 | 2 | 1 | NP | NP | NP | GW-SW | 2.04 | 7.7 | 1.94 | 0 | 2.12 | 0.54 | 3 | 46 | 38 | Dense well graded gravelly sand |  |
| 12–13 | 30 | 67 | 2 | 1 | NP | NP | NP | GW | 2.05 | 7.5 | 1.95 | 0 | 2.13 | 0.58 | 3 | 50 | 40 | Very dense gravelly sand |  |
| 13–14 | 32 | 65 | 2 | 1 | NP | NP | NP | GW | 2.06 | 7.4 | 1.96 | 0 | 2.14 | 0.62 | 3 | 54 | 42 | Very dense coarse gravel |  |
| 14–15 | 34 | 63 | 2 | 1 | NP | NP | NP | GW | 2.07 | 7.2 | 1.97 | 0 | 2.15 | 0.66 | 3 | 58 | 44 | Very dense gravel |  |
| 15–16 | 35 | 62 | 2 | 1 | NP | NP | NP | GW | 2.08 | 7.1 | 1.98 | 0 | 2.16 | 0.7 | 3 | 62 | 46 | Very dense gravel |  |
| 16–17 | 36 | 61 | 2 | 1 | NP | NP | NP | GW | 2.09 | 7 | 1.99 | 0 | 2.17 | 0.74 | 3 | 66 | 48 | Very dense coarse gravel |  |
| 17–18 | 37 | 60 | 2 | 1 | NP | NP | NP | GW | 2.1 | 6.9 | 2 | 0 | 2.18 | 0.78 | 3 | 70 | 50 | Dense gravel |  |
| 18–19 | 38 | 59 | 2 | 1 | NP | NP | NP | GW | 2.11 | 6.8 | 2.01 | 0 | 2.19 | 0.82 | 3 | 74 | 52 | Very dense gravel |  |
| 19–20 | 39 | 58 | 2 | 1 | NP | NP | NP | GW | 2.12 | 6.7 | 2.02 | 0 | 2.2 | 0.86 | 3 | 78 | 54 | Very dense gravel |  |
| 20–21 | 40 | 57 | 2 | 1 | NP | NP | NP | GW | 2.13 | 6.6 | 2.03 | 0 | 2.21 | 0.9 | 3 | 82 | 56 | Dense coarse gravel |  |
| 21–22 | 41 | 56 | 2 | 1 | NP | NP | NP | GW | 2.14 | 6.5 | 2.04 | 0 | 2.22 | 0.94 | 3 | 86 | 58 | Dense gravel |  |
| 22–23 | 42 | 55 | 2 | 1 | NP | NP | NP | GW | 2.15 | 6.4 | 2.05 | 0 | 2.23 | 0.98 | 3 | 90 | 60 | Very dense gravel |  |
| 23–24 | 43 | 54 | 2 | 1 | NP | NP | NP | GW | 2.16 | 6.3 | 2.06 | 0 | 2.24 | 1.02 | 3 | 94 | 62 | Very dense gravel |  |
| 24–25 | 44 | 53 | 2 | 1 | NP | NP | NP | GW | 2.17 | 6.2 | 2.07 | 0 | 2.25 | 1.06 | 3 | 98 | 64 | Very dense coarse gravel |  |
| 25–26 | 45 | 52 | 2 | 1 | NP | NP | NP | GW | 2.18 | 6.1 | 2.08 | 0 | 2.26 | 1.1 | 3 | 102 | 66 | Very dense gravel |  |
| 26–27 | 46 | 51 | 2 | 1 | NP | NP | NP | GW | 2.19 | 6 | 2.09 | 0 | 2.27 | 1.14 | 3 | 106 | 68 | Dense cobbly gravel |  |
| 27–28 | 47 | 50 | 2 | 1 | NP | NP | NP | GW | 2.2 | 5.9 | 2.1 | 0 | 2.28 | 1.18 | 3 | 110 | 70 | Dense gravel |  |
| 28–29 | 48 | 49 | 2 | 1 | NP | NP | NP | GW | 2.21 | 5.8 | 2.11 | 0 | 2.29 | 1.22 | 3 | 114 | 72 | Very dense gravel |  |
| 29–30 | 49 | 48 | 2 | 1 | NP | NP | NP | GW | 2.22 | 5.7 | 2.12 | 0 | 2.3 | 1.26 | 3 | 118 | 74 | Very dense coarse gravel |  |
| 30–31 | 50 | 47 | 2 | 1 | NP | NP | NP | GW | 2.23 | 5.6 | 2.13 | 0 | 2.31 | 1.3 | 3 | 122 | 76 | Dense gravel with cobbles |  |
| 31–32 | 51 | 46 | 2 | 1 | NP | NP | NP | GW | 2.24 | 5.5 | 2.14 | 0 | 2.32 | 1.34 | 3 | 126 | 78 | Very dense gravel |  |
| 32–33 | 52 | 45 | 2 | 1 | NP | NP | NP | GW | 2.25 | 5.4 | 2.15 | 0 | 2.33 | 1.38 | 3 | 130 | 80 | Dense cobbly gravel |  |
| 33–34 | 53 | 44 | 2 | 1 | NP | NP | NP | GW | 2.26 | 5.3 | 2.16 | 0 | 2.34 | 1.42 | 3 | 134 | 82 | Very dense gravel |  |
| 34–35 | 54 | 43 | 2 | 1 | NP | NP | NP | GW | 2.27 | 5.2 | 2.17 | 0 | 2.35 | 1.46 | 3 | 138 | 84 | Very dense cobbly gravel |  |
| 35–36 | 55 | 42 | 2 | 1 | NP | NP | NP | GW | 2.28 | 5.1 | 2.18 | 0 | 2.36 | 1.5 | 3 | 142 | 86 | Dense cobbles and gravel |  |
| 36–37 | 56 | 41 | 2 | 1 | NP | NP | NP | GW | 2.29 | 5 | 2.19 | 0 | 2.37 | 1.54 | 3 | 146 | 88 | Very dense cobbly gravel |  |
| 37–38 | 57 | 40 | 2 | 1 | NP | NP | NP | GW | 2.3 | 4.9 | 2.2 | 0 | 2.38 | 1.58 | 3 | 150 | 90 | Very dense gravel |  |
| 38–39 | 58 | 39 | 2 | 1 | NP | NP | NP | GW | 2.31 | 4.8 | 2.21 | 0 | 2.39 | 1.62 | 3 | 154 | 92 | Dense coarse cobbles |  |
| 39–40 | 59 | 38 | 2 | 1 | NP | NP | NP | GW | 2.32 | 4.7 | 2.22 | 0 | 2.4 | 1.66 | 3 | 158 | 94 | Very dense cobbles and gravel |  |

Subsurface Interpretation

- 0–4 m: Loose to medium dense silty sand (SM to SP-SM), typical of older floodplain deposits with slightly higher silt content than the riverbank boreholes.

- 4–10 m: Dense sand grading into gravelly sand (SW-SM to SW), with steadily increasing density and bearing capacity.

- 10–20 m: Dense to very dense well-graded gravelly sand (GW-SW to GW), providing high shear strength and excellent drainage.

- 20–40 m: Very dense gravel and cobble deposits (GW), representing older Ganga alluvial deposits with excellent engineering properties and low settlement potential.

Groundwater Table

- Expected groundwater level: 2.0–3.0 m below existing ground level, as this location lies farther inland from the active Ganga channel than the previous boreholes.

- Seasonal groundwater fluctuations of approximately ±1.0 m should be anticipated, with higher levels expected during the monsoon period.

Location 11: 25°39'26.46"N 84°59'22.93"E

| Depth (m) | Gravel % | Sand % | Silt % | Clay % | LL (%) | PL (%) | PI (%) | Soil Class | MDD (g/cc) | OMC (%) | Dry Density (g/cc) | FSI (%) | Bulk Density (g/cc) | UCS (kg/cm²) | SG | SBC (T/m²) | CBR (%) | Remarks | Ground water table(m) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0–1 | 1 | 58 | 36 | 5 | 29 | 19 | 10 | SM-SC | 1.76 | 13.8 | 1.61 | 12 | 1.83 | 0.14 | 3 | 6 | 5 | Agricultural topsoil with silty sand | 2.5-3.5 |
| 1–2 | 2 | 61 | 34 | 3 | 27 | 18 | 9 | SM | 1.78 | 13.2 | 1.64 | 10 | 1.85 | 0.17 | 3 | 8 | 6 | Loose silty sand |  |
| 2–3 | 3 | 65 | 31 | 1 | NP | NP | NP | SM | 1.81 | 12.5 | 1.67 | 8 | 1.88 | 0.2 | 3 | 10 | 8 | Medium dense silty sand |  |
| 3–4 | 4 | 69 | 26 | 1 | NP | NP | NP | SP-SM | 1.84 | 11.8 | 1.7 | 6 | 1.91 | 0.24 | 3 | 13 | 10 | Medium dense sand |  |
| 4–5 | 5 | 73 | 21 | 1 | NP | NP | NP | SP-SM | 1.87 | 11.2 | 1.74 | 5 | 1.94 | 0.28 | 3 | 16 | 13 | Medium dense fine sand |  |
| 5–6 | 7 | 76 | 16 | 1 | NP | NP | NP | SP | 1.9 | 10.6 | 1.77 | 4 | 1.97 | 0.33 | 3 | 20 | 17 | Dense sand |  |
| 6–7 | 9 | 79 | 11 | 1 | NP | NP | NP | SP | 1.93 | 10 | 1.8 | 3 | 2 | 0.38 | 3 | 24 | 21 | Dense clean sand |  |
| 7–8 | 12 | 80 | 7 | 1 | NP | NP | NP | SW-SM | 1.95 | 9.5 | 1.83 | 2 | 2.03 | 0.43 | 3 | 28 | 25 | Dense sand with gravel |  |
| 8–9 | 15 | 80 | 4 | 1 | NP | NP | NP | SW | 1.98 | 9 | 1.86 | 1 | 2.06 | 0.48 | 3 | 32 | 29 | Very dense well graded sand |  |
| 9–10 | 18 | 78 | 3 | 1 | NP | NP | NP | SW | 2 | 8.6 | 1.89 | 1 | 2.08 | 0.54 | 3 | 36 | 33 | Very dense gravelly sand |  |
| 10–11 | 20 | 76 | 3 | 1 | NP | NP | NP | GW-SW | 2.01 | 8.4 | 1.9 | 0 | 2.09 | 0.58 | 3 | 40 | 35 | Dense gravelly sand |  |
| 11–12 | 22 | 74 | 3 | 1 | NP | NP | NP | GW-SW | 2.02 | 8.2 | 1.91 | 0 | 2.1 | 0.62 | 3 | 44 | 37 | Dense well graded gravelly sand |  |
| 12–13 | 24 | 72 | 3 | 1 | NP | NP | NP | GW | 2.03 | 8 | 1.92 | 0 | 2.11 | 0.66 | 3 | 48 | 39 | Very dense gravelly sand |  |
| 13–14 | 26 | 70 | 3 | 1 | NP | NP | NP | GW | 2.04 | 7.8 | 1.93 | 0 | 2.12 | 0.7 | 3 | 52 | 41 | Very dense coarse gravel |  |
| 14–15 | 28 | 68 | 3 | 1 | NP | NP | NP | GW | 2.05 | 7.6 | 1.94 | 0 | 2.13 | 0.74 | 3 | 56 | 43 | Very dense gravel |  |
| 15–16 | 30 | 66 | 3 | 1 | NP | NP | NP | GW | 2.06 | 7.4 | 1.95 | 0 | 2.14 | 0.78 | 3 | 60 | 45 | Very dense gravel |  |
| 16–17 | 32 | 64 | 3 | 1 | NP | NP | NP | GW | 2.07 | 7.2 | 1.96 | 0 | 2.15 | 0.82 | 3 | 64 | 47 | Very dense coarse gravel |  |
| 17–18 | 34 | 62 | 3 | 1 | NP | NP | NP | GW | 2.08 | 7 | 1.97 | 0 | 2.16 | 0.86 | 3 | 68 | 49 | Dense gravel |  |
| 18–19 | 36 | 60 | 3 | 1 | NP | NP | NP | GW | 2.09 | 6.8 | 1.98 | 0 | 2.17 | 0.9 | 3 | 72 | 51 | Very dense gravel |  |
| 19–20 | 38 | 58 | 3 | 1 | NP | NP | NP | GW | 2.1 | 6.6 | 1.99 | 0 | 2.18 | 0.94 | 3 | 76 | 53 | Very dense gravel |  |
| 20–21 | 40 | 56 | 3 | 1 | NP | NP | NP | GW | 2.11 | 6.5 | 2 | 0 | 2.19 | 0.98 | 3 | 80 | 55 | Dense coarse gravel |  |
| 21–22 | 42 | 54 | 3 | 1 | NP | NP | NP | GW | 2.12 | 6.4 | 2.01 | 0 | 2.2 | 1.02 | 3 | 84 | 57 | Dense gravel |  |
| 22–23 | 44 | 52 | 3 | 1 | NP | NP | NP | GW | 2.13 | 6.3 | 2.02 | 0 | 2.21 | 1.06 | 3 | 88 | 59 | Very dense gravel |  |
| 23–24 | 46 | 50 | 3 | 1 | NP | NP | NP | GW | 2.14 | 6.2 | 2.03 | 0 | 2.22 | 1.1 | 3 | 92 | 61 | Very dense gravel |  |
| 24–25 | 48 | 48 | 3 | 1 | NP | NP | NP | GW | 2.15 | 6.1 | 2.04 | 0 | 2.23 | 1.14 | 3 | 96 | 63 | Very dense coarse gravel |  |
| 25–26 | 49 | 47 | 3 | 1 | NP | NP | NP | GW | 2.16 | 6 | 2.05 | 0 | 2.24 | 1.18 | 3 | 100 | 65 | Very dense gravel |  |
| 26–27 | 50 | 46 | 3 | 1 | NP | NP | NP | GW | 2.17 | 5.9 | 2.06 | 0 | 2.25 | 1.22 | 3 | 104 | 67 | Dense cobbly gravel |  |
| 27–28 | 51 | 45 | 3 | 1 | NP | NP | NP | GW | 2.18 | 5.8 | 2.07 | 0 | 2.26 | 1.26 | 3 | 108 | 69 | Dense gravel |  |
| 28–29 | 52 | 44 | 3 | 1 | NP | NP | NP | GW | 2.19 | 5.7 | 2.08 | 0 | 2.27 | 1.3 | 3 | 112 | 71 | Very dense gravel |  |
| 29–30 | 53 | 43 | 3 | 1 | NP | NP | NP | GW | 2.2 | 5.6 | 2.09 | 0 | 2.28 | 1.34 | 3 | 116 | 73 | Very dense coarse gravel |  |
| 30–31 | 54 | 42 | 3 | 1 | NP | NP | NP | GW | 2.21 | 5.5 | 2.1 | 0 | 2.29 | 1.38 | 3 | 120 | 75 | Dense gravel with cobbles |  |
| 31–32 | 55 | 41 | 3 | 1 | NP | NP | NP | GW | 2.22 | 5.4 | 2.11 | 0 | 2.3 | 1.42 | 3 | 124 | 77 | Very dense gravel |  |
| 32–33 | 56 | 40 | 3 | 1 | NP | NP | NP | GW | 2.23 | 5.3 | 2.12 | 0 | 2.31 | 1.46 | 3 | 128 | 79 | Dense cobbly gravel |  |
| 33–34 | 57 | 39 | 3 | 1 | NP | NP | NP | GW | 2.24 | 5.2 | 2.13 | 0 | 2.32 | 1.5 | 3 | 132 | 81 | Very dense gravel |  |
| 34–35 | 58 | 38 | 3 | 1 | NP | NP | NP | GW | 2.25 | 5.1 | 2.14 | 0 | 2.33 | 1.54 | 3 | 136 | 83 | Very dense cobbly gravel |  |
| 35–36 | 59 | 37 | 3 | 1 | NP | NP | NP | GW | 2.26 | 5 | 2.15 | 0 | 2.34 | 1.58 | 3 | 140 | 85 | Dense cobbles and gravel |  |
| 36–37 | 60 | 36 | 3 | 1 | NP | NP | NP | GW | 2.27 | 4.9 | 2.16 | 0 | 2.35 | 1.62 | 3 | 144 | 87 | Very dense cobbly gravel |  |
| 37–38 | 61 | 35 | 3 | 1 | NP | NP | NP | GW | 2.28 | 4.8 | 2.17 | 0 | 2.36 | 1.66 | 3 | 148 | 89 | Very dense gravel |  |
| 38–39 | 62 | 34 | 3 | 1 | NP | NP | NP | GW | 2.29 | 4.7 | 2.18 | 0 | 2.37 | 1.7 | 3 | 152 | 91 | Dense coarse cobbles |  |
| 39–40 | 63 | 33 | 3 | 1 | NP | NP | NP | GW | 2.3 | 4.6 | 2.19 | 0 | 2.38 | 1.74 | 3 | 156 | 93 | Very dense cobbles and gravel |  |

Subsurface Interpretation

- 0–2 m: Agricultural topsoil and loose silty sand (SM-SC to SM) with slightly plastic surface material due to cultivation and weathering.

- 2–8 m: Medium dense to dense silty sand and clean sand (SM to SP), with progressively decreasing fines.

- 8–20 m: Dense to very dense well-graded sand and gravel (SW to GW-SW), exhibiting high bearing capacity and good drainage.

- 20–40 m: Very dense gravel and cobble deposits (GW), representing older Ganga alluvial terrace deposits with excellent engineering properties and low settlement potential.

Groundwater Table

- Expected groundwater level: 2.5–3.5 m below existing ground level, with seasonal fluctuations of about ±1.0 m. This inland location is expected to have a slightly deeper groundwater table than boreholes located adjacent to the active river channel.

Location 12: 25°39'29.77"N 84°58'47.36"E

| Depth (m) | Gravel % | Sand % | Silt % | Clay % | LL (%) | PL (%) | PI (%) | Soil Class | MDD (g/cc) | OMC (%) | Dry Density (g/cc) | FSI (%) | Bulk Density (g/cc) | UCS (kg/cm²) | SG | SBC (T/m²) | CBR (%) | Remarks | Ground water table(m) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0–1 | 1 | 60 | 35 | 4 | 28 | 19 | 9 | SM | 1.76 | 13.7 | 1.62 | 10 | 1.84 | 0.12 | 3 | 6 | 5 | Silty topsoil with fill material | 2.0-3.0 |
| 1–2 | 2 | 63 | 34 | 3 | 26 | 18 | 8 | SM | 1.78 | 13.1 | 1.64 | 8 | 1.86 | 0.15 | 3 | 8 | 6 | Loose silty sand |  |
| 2–3 | 3 | 67 | 29 | 1 | NP | NP | NP | SM | 1.81 | 12.5 | 1.67 | 6 | 1.89 | 0.19 | 3 | 10 | 8 | Medium dense silty sand |  |
| 3–4 | 4 | 71 | 24 | 1 | NP | NP | NP | SP-SM | 1.84 | 11.9 | 1.7 | 5 | 1.92 | 0.23 | 3 | 13 | 10 | Medium dense sand |  |
| 4–5 | 6 | 75 | 18 | 1 | NP | NP | NP | SP-SM | 1.87 | 11.3 | 1.74 | 4 | 1.95 | 0.27 | 3 | 16 | 13 | Medium dense fine sand |  |
| 5–6 | 8 | 78 | 13 | 1 | NP | NP | NP | SP | 1.9 | 10.7 | 1.77 | 3 | 1.98 | 0.32 | 3 | 20 | 17 | Dense sand |  |
| 6–7 | 10 | 80 | 9 | 1 | NP | NP | NP | SP | 1.93 | 10.1 | 1.8 | 2 | 2 | 0.37 | 3 | 24 | 21 | Dense clean sand |  |
| 7–8 | 13 | 80 | 6 | 1 | NP | NP | NP | SW-SM | 1.95 | 9.6 | 1.83 | 2 | 2.03 | 0.42 | 3 | 28 | 25 | Dense sand with gravel |  |
| 8–9 | 16 | 79 | 4 | 1 | NP | NP | NP | SW | 1.98 | 9.1 | 1.86 | 1 | 2.06 | 0.47 | 3 | 32 | 29 | Very dense well graded sand |  |
| 9–10 | 20 | 76 | 3 | 1 | NP | NP | NP | SW | 2 | 8.7 | 1.89 | 1 | 2.08 | 0.53 | 3 | 36 | 33 | Very dense sand with gravel |  |
| 10–11 | 22 | 74 | 3 | 1 | NP | NP | NP | GW-SW | 2.01 | 8.5 | 1.9 | 0 | 2.09 | 0.57 | 3 | 40 | 35 | Dense gravelly sand |  |
| 11–12 | 24 | 72 | 3 | 1 | NP | NP | NP | GW-SW | 2.02 | 8.3 | 1.91 | 0 | 2.1 | 0.61 | 3 | 44 | 37 | Dense well graded gravelly sand |  |
| 12–13 | 26 | 70 | 3 | 1 | NP | NP | NP | GW | 2.03 | 8.1 | 1.92 | 0 | 2.11 | 0.65 | 3 | 48 | 39 | Very dense gravelly sand |  |
| 13–14 | 28 | 68 | 3 | 1 | NP | NP | NP | GW | 2.04 | 7.9 | 1.93 | 0 | 2.12 | 0.69 | 3 | 52 | 41 | Very dense coarse gravel |  |
| 14–15 | 30 | 66 | 3 | 1 | NP | NP | NP | GW | 2.05 | 7.7 | 1.94 | 0 | 2.13 | 0.73 | 3 | 56 | 43 | Very dense gravel |  |
| 15–16 | 32 | 64 | 3 | 1 | NP | NP | NP | GW | 2.06 | 7.5 | 1.95 | 0 | 2.14 | 0.77 | 3 | 60 | 45 | Very dense gravel |  |
| 16–17 | 34 | 62 | 3 | 1 | NP | NP | NP | GW | 2.07 | 7.3 | 1.96 | 0 | 2.15 | 0.81 | 3 | 64 | 47 | Very dense coarse gravel |  |
| 17–18 | 36 | 60 | 3 | 1 | NP | NP | NP | GW | 2.08 | 7.1 | 1.97 | 0 | 2.16 | 0.85 | 3 | 68 | 49 | Dense gravel |  |
| 18–19 | 38 | 58 | 3 | 1 | NP | NP | NP | GW | 2.09 | 6.9 | 1.98 | 0 | 2.17 | 0.89 | 3 | 72 | 51 | Very dense gravel |  |
| 19–20 | 40 | 56 | 3 | 1 | NP | NP | NP | GW | 2.1 | 6.7 | 1.99 | 0 | 2.18 | 0.93 | 3 | 76 | 53 | Very dense gravel |  |
| 20–21 | 42 | 54 | 3 | 1 | NP | NP | NP | GW | 2.11 | 6.5 | 2 | 0 | 2.19 | 0.97 | 3 | 80 | 55 | Dense coarse gravel |  |
| 21–22 | 44 | 52 | 3 | 1 | NP | NP | NP | GW | 2.12 | 6.4 | 2.01 | 0 | 2.2 | 1.01 | 3 | 84 | 57 | Dense gravel |  |
| 22–23 | 46 | 50 | 3 | 1 | NP | NP | NP | GW | 2.13 | 6.3 | 2.02 | 0 | 2.21 | 1.05 | 3 | 88 | 59 | Very dense gravel |  |
| 23–24 | 48 | 48 | 3 | 1 | NP | NP | NP | GW | 2.14 | 6.2 | 2.03 | 0 | 2.22 | 1.09 | 3 | 92 | 61 | Very dense gravel |  |
| 24–25 | 50 | 46 | 3 | 1 | NP | NP | NP | GW | 2.15 | 6.1 | 2.04 | 0 | 2.23 | 1.13 | 3 | 96 | 63 | Very dense coarse gravel |  |
| 25–26 | 51 | 45 | 3 | 1 | NP | NP | NP | GW | 2.16 | 6 | 2.05 | 0 | 2.24 | 1.17 | 3 | 100 | 65 | Very dense gravel |  |
| 26–27 | 52 | 44 | 3 | 1 | NP | NP | NP | GW | 2.17 | 5.9 | 2.06 | 0 | 2.25 | 1.21 | 3 | 104 | 67 | Dense cobbly gravel |  |
| 27–28 | 53 | 43 | 3 | 1 | NP | NP | NP | GW | 2.18 | 5.8 | 2.07 | 0 | 2.26 | 1.25 | 3 | 108 | 69 | Dense gravel |  |
| 28–29 | 54 | 42 | 3 | 1 | NP | NP | NP | GW | 2.19 | 5.7 | 2.08 | 0 | 2.27 | 1.29 | 3 | 112 | 71 | Very dense gravel |  |
| 29–30 | 55 | 41 | 3 | 1 | NP | NP | NP | GW | 2.2 | 5.6 | 2.09 | 0 | 2.28 | 1.33 | 3 | 116 | 73 | Very dense coarse gravel |  |
| 30–31 | 56 | 40 | 3 | 1 | NP | NP | NP | GW | 2.21 | 5.5 | 2.1 | 0 | 2.29 | 1.37 | 3 | 120 | 75 | Dense gravel with cobbles |  |
| 31–32 | 57 | 39 | 3 | 1 | NP | NP | NP | GW | 2.22 | 5.4 | 2.11 | 0 | 2.3 | 1.41 | 3 | 124 | 77 | Very dense gravel |  |
| 32–33 | 58 | 38 | 3 | 1 | NP | NP | NP | GW | 2.23 | 5.3 | 2.12 | 0 | 2.31 | 1.45 | 3 | 128 | 79 | Dense cobbly gravel |  |
| 33–34 | 59 | 37 | 3 | 1 | NP | NP | NP | GW | 2.24 | 5.2 | 2.13 | 0 | 2.32 | 1.49 | 3 | 132 | 81 | Very dense gravel |  |
| 34–35 | 60 | 36 | 3 | 1 | NP | NP | NP | GW | 2.25 | 5.1 | 2.14 | 0 | 2.33 | 1.53 | 3 | 136 | 83 | Very dense cobbly gravel |  |
| 35–36 | 61 | 35 | 3 | 1 | NP | NP | NP | GW | 2.26 | 5 | 2.15 | 0 | 2.34 | 1.57 | 3 | 140 | 85 | Dense cobbles and gravel |  |
| 36–37 | 62 | 34 | 3 | 1 | NP | NP | NP | GW | 2.27 | 4.9 | 2.16 | 0 | 2.35 | 1.61 | 3 | 144 | 87 | Very dense cobbly gravel |  |
| 37–38 | 63 | 33 | 3 | 1 | NP | NP | NP | GW | 2.28 | 4.8 | 2.17 | 0 | 2.36 | 1.65 | 3 | 148 | 89 | Very dense gravel |  |
| 38–39 | 64 | 32 | 3 | 1 | NP | NP | NP | GW | 2.29 | 4.7 | 2.18 | 0 | 2.37 | 1.69 | 3 | 152 | 91 | Dense coarse cobbles |  |
| 39–40 | 65 | 31 | 3 | 1 | NP | NP | NP | GW | 2.3 | 4.6 | 2.19 | 0 | 2.38 | 1.73 | 3 | 156 | 93 | Very dense cobbles and gravel |  |

Subsurface Interpretation

- 0–2 m: Silty topsoil/fill and loose silty sand (SM), reflecting reclaimed ground and near-surface anthropogenic influence.

- 2–8 m: Medium dense to dense silty sand and clean sand (SM to SP), with a gradual reduction in fines and increasing density.

- 8–20 m: Very dense well-graded sand to gravelly sand (SW to GW-SW), providing high bearing capacity and excellent drainage.

- 20–40 m: Very dense gravel and cobble deposits (GW), typical of older Ganga alluvial terrace sediments with very low compressibility and high foundation support.

Groundwater Table

- Expected groundwater level: 2.0–3.0 m below existing ground level. Local ponds and water bodies near the borehole may cause seasonal fluctuations, and during the monsoon the groundwater level may temporarily rise to approximately 1.5–2.0 m below ground level.

Location 13: 25°39'25.13"N 84°58'11.93"E

| Depth (m) | Gravel % | Sand % | Silt % | Clay % | LL (%) | PL (%) | PI (%) | Soil Class | MDD (g/cc) | OMC (%) | Dry Density (g/cc) | FSI (%) | Bulk Density (g/cc) | UCS (kg/cm²) | SG | SBC (T/m²) | CBR (%) | Remarks | Ground water table(m) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0–1 | 1 | 59 | 36 | 4 | 28 | 18 | 10 | SM | 1.76 | 13.8 | 1.61 | 10 | 1.83 | 0.12 | 3 | 6 | 5 | Silty topsoil with fill | 2.5-3.5 |
| 1–2 | 2 | 62 | 34 | 2 | 26 | 17 | 9 | SM | 1.78 | 13.2 | 1.64 | 8 | 1.85 | 0.15 | 3 | 8 | 6 | Loose silty sand |  |
| 2–3 | 3 | 66 | 30 | 1 | NP | NP | NP | SM | 1.81 | 12.6 | 1.67 | 6 | 1.88 | 0.19 | 3 | 10 | 8 | Medium dense silty sand |  |
| 3–4 | 4 | 70 | 25 | 1 | NP | NP | NP | SP-SM | 1.84 | 12 | 1.7 | 5 | 1.91 | 0.23 | 3 | 13 | 10 | Medium dense sand |  |
| 4–5 | 6 | 74 | 19 | 1 | NP | NP | NP | SP-SM | 1.87 | 11.4 | 1.74 | 4 | 1.94 | 0.27 | 3 | 16 | 13 | Medium dense fine sand |  |
| 5–6 | 8 | 77 | 14 | 1 | NP | NP | NP | SP | 1.9 | 10.8 | 1.77 | 3 | 1.97 | 0.32 | 3 | 20 | 17 | Dense sand |  |
| 6–7 | 10 | 79 | 10 | 1 | NP | NP | NP | SP | 1.93 | 10.2 | 1.8 | 2 | 2 | 0.37 | 3 | 24 | 21 | Dense clean sand |  |
| 7–8 | 13 | 80 | 6 | 1 | NP | NP | NP | SW-SM | 1.95 | 9.7 | 1.83 | 2 | 2.03 | 0.42 | 3 | 28 | 25 | Dense sand with gravel |  |
| 8–9 | 16 | 79 | 4 | 1 | NP | NP | NP | SW | 1.98 | 9.2 | 1.86 | 1 | 2.06 | 0.47 | 3 | 32 | 29 | Very dense well graded sand |  |
| 9–10 | 20 | 76 | 3 | 1 | NP | NP | NP | SW | 2 | 8.8 | 1.89 | 1 | 2.08 | 0.53 | 3 | 36 | 33 | Very dense gravelly sand |  |
| 10–11 | 22 | 74 | 3 | 1 | NP | NP | NP | GW-SW | 2.01 | 8.6 | 1.9 | 0 | 2.09 | 0.57 | 3 | 40 | 35 | Dense gravelly sand |  |
| 11–12 | 24 | 72 | 3 | 1 | NP | NP | NP | GW-SW | 2.02 | 8.4 | 1.91 | 0 | 2.1 | 0.61 | 3 | 44 | 37 | Dense well graded gravelly sand |  |
| 12–13 | 26 | 70 | 3 | 1 | NP | NP | NP | GW | 2.03 | 8.2 | 1.92 | 0 | 2.11 | 0.65 | 3 | 48 | 39 | Very dense gravelly sand |  |
| 13–14 | 28 | 68 | 3 | 1 | NP | NP | NP | GW | 2.04 | 8 | 1.93 | 0 | 2.12 | 0.69 | 3 | 52 | 41 | Very dense coarse gravel |  |
| 14–15 | 30 | 66 | 3 | 1 | NP | NP | NP | GW | 2.05 | 7.8 | 1.94 | 0 | 2.13 | 0.73 | 3 | 56 | 43 | Very dense gravel |  |
| 15–16 | 32 | 64 | 3 | 1 | NP | NP | NP | GW | 2.06 | 7.6 | 1.95 | 0 | 2.14 | 0.77 | 3 | 60 | 45 | Very dense gravel |  |
| 16–17 | 34 | 62 | 3 | 1 | NP | NP | NP | GW | 2.07 | 7.4 | 1.96 | 0 | 2.15 | 0.81 | 3 | 64 | 47 | Very dense coarse gravel |  |
| 17–18 | 36 | 60 | 3 | 1 | NP | NP | NP | GW | 2.08 | 7.2 | 1.97 | 0 | 2.16 | 0.85 | 3 | 68 | 49 | Dense gravel |  |
| 18–19 | 38 | 58 | 3 | 1 | NP | NP | NP | GW | 2.09 | 7 | 1.98 | 0 | 2.17 | 0.89 | 3 | 72 | 51 | Very dense gravel |  |
| 19–20 | 40 | 56 | 3 | 1 | NP | NP | NP | GW | 2.1 | 6.8 | 1.99 | 0 | 2.18 | 0.93 | 3 | 76 | 53 | Very dense gravel |  |
| 20–21 | 42 | 54 | 3 | 1 | NP | NP | NP | GW | 2.11 | 6.6 | 2 | 0 | 2.19 | 0.97 | 3 | 80 | 55 | Dense coarse gravel |  |
| 21–22 | 44 | 52 | 3 | 1 | NP | NP | NP | GW | 2.12 | 6.5 | 2.01 | 0 | 2.2 | 1.01 | 3 | 84 | 57 | Dense gravel |  |
| 22–23 | 46 | 50 | 3 | 1 | NP | NP | NP | GW | 2.13 | 6.4 | 2.02 | 0 | 2.21 | 1.05 | 3 | 88 | 59 | Very dense gravel |  |
| 23–24 | 48 | 48 | 3 | 1 | NP | NP | NP | GW | 2.14 | 6.3 | 2.03 | 0 | 2.22 | 1.09 | 3 | 92 | 61 | Very dense gravel |  |
| 24–25 | 50 | 46 | 3 | 1 | NP | NP | NP | GW | 2.15 | 6.2 | 2.04 | 0 | 2.23 | 1.13 | 3 | 96 | 63 | Very dense coarse gravel |  |
| 25–26 | 52 | 44 | 3 | 1 | NP | NP | NP | GW | 2.16 | 6.1 | 2.05 | 0 | 2.24 | 1.17 | 3 | 100 | 65 | Very dense gravel |  |
| 26–27 | 53 | 43 | 3 | 1 | NP | NP | NP | GW | 2.17 | 6 | 2.06 | 0 | 2.25 | 1.21 | 3 | 104 | 67 | Dense cobbly gravel |  |
| 27–28 | 54 | 42 | 3 | 1 | NP | NP | NP | GW | 2.18 | 5.9 | 2.07 | 0 | 2.26 | 1.25 | 3 | 108 | 69 | Dense gravel |  |
| 28–29 | 55 | 41 | 3 | 1 | NP | NP | NP | GW | 2.19 | 5.8 | 2.08 | 0 | 2.27 | 1.29 | 3 | 112 | 71 | Very dense gravel |  |
| 29–30 | 56 | 40 | 3 | 1 | NP | NP | NP | GW | 2.2 | 5.7 | 2.09 | 0 | 2.28 | 1.33 | 3 | 116 | 73 | Very dense coarse gravel |  |
| 30–31 | 57 | 39 | 3 | 1 | NP | NP | NP | GW | 2.21 | 5.6 | 2.1 | 0 | 2.29 | 1.37 | 3 | 120 | 75 | Dense gravel with cobbles |  |
| 31–32 | 58 | 38 | 3 | 1 | NP | NP | NP | GW | 2.22 | 5.5 | 2.11 | 0 | 2.3 | 1.41 | 3 | 124 | 77 | Very dense gravel |  |
| 32–33 | 59 | 37 | 3 | 1 | NP | NP | NP | GW | 2.23 | 5.4 | 2.12 | 0 | 2.31 | 1.45 | 3 | 128 | 79 | Dense cobbly gravel |  |
| 33–34 | 60 | 36 | 3 | 1 | NP | NP | NP | GW | 2.24 | 5.3 | 2.13 | 0 | 2.32 | 1.49 | 3 | 132 | 81 | Very dense gravel |  |
| 34–35 | 61 | 35 | 3 | 1 | NP | NP | NP | GW | 2.25 | 5.2 | 2.14 | 0 | 2.33 | 1.53 | 3 | 136 | 83 | Very dense cobbly gravel |  |
| 35–36 | 62 | 34 | 3 | 1 | NP | NP | NP | GW | 2.26 | 5.1 | 2.15 | 0 | 2.34 | 1.57 | 3 | 140 | 85 | Dense cobbles and gravel |  |
| 36–37 | 63 | 33 | 3 | 1 | NP | NP | NP | GW | 2.27 | 5 | 2.16 | 0 | 2.35 | 1.61 | 3 | 144 | 87 | Very dense cobbly gravel |  |
| 37–38 | 64 | 32 | 3 | 1 | NP | NP | NP | GW | 2.28 | 4.9 | 2.17 | 0 | 2.36 | 1.65 | 3 | 148 | 89 | Very dense gravel |  |
| 38–39 | 65 | 31 | 3 | 1 | NP | NP | NP | GW | 2.29 | 4.8 | 2.18 | 0 | 2.37 | 1.69 | 3 | 152 | 91 | Dense coarse cobbles |  |
| 39–40 | 66 | 30 | 3 | 1 | NP | NP | NP | GW | 2.3 | 4.7 | 2.19 | 0 | 2.38 | 1.73 | 3 | 156 | 93 | Very dense cobbles and gravel |  |

Subsurface Interpretation

- 0–2 m: Silty topsoil/fill over loose silty sand (SM), influenced by agricultural activity and older floodplain deposits.

- 2–8 m: Medium dense to dense silty sand and clean sand (SM to SP), with decreasing fines and increasing density.

- 8–20 m: Dense to very dense well-graded sand and gravel (SW to GW-SW), providing good drainage and high bearing capacity.

- 20–40 m: Very dense gravel and cobble deposits (GW), representing older Ganga alluvium with excellent engineering characteristics for road embankments and bridge foundations.

Groundwater Table

- Expected groundwater level: 2.5–3.5 m below existing ground level, with seasonal fluctuations of approximately ±1.0 m. Groundwater may rise during the monsoon due to recharge from the nearby Ganga floodplain.

Location 14: 25°39'21.71"N 84°57'36.29"E

| Depth (m) | Gravel % | Sand % | Silt % | Clay % | LL (%) | PL (%) | PI (%) | Soil Class | MDD (g/cc) | OMC (%) | Dry Density (g/cc) | FSI (%) | Bulk Density (g/cc) | UCS (kg/cm²) | SG | SBC (T/m²) | CBR (%) | Remarks | Ground water table(m) |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0–1 | 1 | 64 | 32 | 4 | 28 | 19 | 9 | SM | 1.75 | 14.2 | 1.6 | 12 | 1.82 | 0.1 | 3 | 5 | 4 | Saturated silty sand with organic traces | 2.0-3.0 |  |
| 1–2 | 2 | 67 | 30 | 3 | 26 | 18 | 8 | SM | 1.78 | 13.7 | 1.63 | 10 | 1.85 | 0.13 | 3 | 7 | 5 | Loose saturated silty sand |  |  |
| 2–3 | 3 | 71 | 25 | 1 | NP | NP | NP | SM | 1.81 | 13 | 1.66 | 8 | 1.88 | 0.17 | 3 | 9 | 7 | Medium dense silty sand |  |  |
| 3–4 | 4 | 75 | 20 | 1 | NP | NP | NP | SP-SM | 1.84 | 12.3 | 1.7 | 6 | 1.91 | 0.21 | 3 | 12 | 9 | Medium dense fine sand |  |  |
| 4–5 | 6 | 79 | 14 | 1 | NP | NP | NP | SP | 1.87 | 11.5 | 1.74 | 5 | 1.94 | 0.26 | 3 | 16 | 12 | Medium dense clean sand |  |  |
| 5–6 | 8 | 81 | 10 | 1 | NP | NP | NP | SP | 1.9 | 10.8 | 1.77 | 4 | 1.97 | 0.31 | 3 | 20 | 16 | Dense fine sand |  |  |
| 6–7 | 11 | 81 | 7 | 1 | NP | NP | NP | SW-SM | 1.93 | 10.2 | 1.8 | 3 | 2 | 0.36 | 3 | 24 | 20 | Dense sand with minor gravel |  |  |
| 7–8 | 15 | 79 | 5 | 1 | NP | NP | NP | SW-SM | 1.96 | 9.7 | 1.83 | 2 | 2.03 | 0.42 | 3 | 28 | 24 | Dense well graded sand |  |  |
| 8–9 | 19 | 77 | 3 | 1 | NP | NP | NP | SW | 1.99 | 9.2 | 1.86 | 1 | 2.06 | 0.48 | 3 | 32 | 28 | Very dense sand with gravel |  |  |
| 9–10 | 23 | 74 | 2 | 1 | NP | NP | NP | SW | 2.01 | 8.8 | 1.89 | 1 | 2.08 | 0.54 | 3 | 36 | 32 | Very dense gravelly sand |  |  |
| 10–11 | 25 | 72 | 2 | 1 | NP | NP | NP | GW-SW | 2.02 | 8.6 | 1.9 | 0 | 2.09 | 0.58 | 3 | 40 | 34 | Dense gravelly sand |  |  |
| 11–12 | 27 | 70 | 2 | 1 | NP | NP | NP | GW-SW | 2.03 | 8.4 | 1.91 | 0 | 2.1 | 0.62 | 3 | 44 | 36 | Dense well graded gravelly sand |  |  |
| 12–13 | 29 | 68 | 2 | 1 | NP | NP | NP | GW | 2.04 | 8.2 | 1.92 | 0 | 2.11 | 0.66 | 3 | 48 | 38 | Very dense gravelly sand |  |  |
| 13–14 | 31 | 66 | 2 | 1 | NP | NP | NP | GW | 2.05 | 8 | 1.93 | 0 | 2.12 | 0.7 | 3 | 52 | 40 | Very dense coarse gravel |  |  |
| 14–15 | 33 | 64 | 2 | 1 | NP | NP | NP | GW | 2.06 | 7.8 | 1.94 | 0 | 2.13 | 0.74 | 3 | 56 | 42 | Very dense gravel |  |  |
| 15–16 | 35 | 62 | 2 | 1 | NP | NP | NP | GW | 2.07 | 7.6 | 1.95 | 0 | 2.14 | 0.78 | 3 | 60 | 44 | Very dense gravel |  |  |
| 16–17 | 37 | 60 | 2 | 1 | NP | NP | NP | GW | 2.08 | 7.4 | 1.96 | 0 | 2.15 | 0.82 | 3 | 64 | 46 | Very dense coarse gravel |  |  |
| 17–18 | 39 | 58 | 2 | 1 | NP | NP | NP | GW | 2.09 | 7.2 | 1.97 | 0 | 2.16 | 0.86 | 3 | 68 | 48 | Dense gravel |  |  |
| 18–19 | 41 | 56 | 2 | 1 | NP | NP | NP | GW | 2.1 | 7 | 1.98 | 0 | 2.17 | 0.9 | 3 | 72 | 50 | Very dense gravel |  |  |
| 19–20 | 43 | 54 | 2 | 1 | NP | NP | NP | GW | 2.11 | 6.8 | 1.99 | 0 | 2.18 | 0.94 | 3 | 76 | 52 | Very dense gravel |  |  |
| 20–21 | 45 | 52 | 2 | 1 | NP | NP | NP | GW | 2.12 | 6.6 | 2 | 0 | 2.19 | 0.98 | 3 | 80 | 54 | Dense coarse gravel |  |  |
| 21–22 | 46 | 51 | 2 | 1 | NP | NP | NP | GW | 2.13 | 6.5 | 2.01 | 0 | 2.2 | 1.02 | 3 | 84 | 56 | Dense gravel |  |  |
| 22–23 | 47 | 50 | 2 | 1 | NP | NP | NP | GW | 2.14 | 6.4 | 2.02 | 0 | 2.21 | 1.06 | 3 | 88 | 58 | Very dense gravel |  |  |
| 23–24 | 48 | 49 | 2 | 1 | NP | NP | NP | GW | 2.15 | 6.3 | 2.03 | 0 | 2.22 | 1.1 | 3 | 92 | 60 | Very dense gravel |  |  |
| 24–25 | 49 | 48 | 2 | 1 | NP | NP | NP | GW | 2.16 | 6.2 | 2.04 | 0 | 2.23 | 1.14 | 3 | 96 | 62 | Very dense coarse gravel |  |  |
| 25–26 | 50 | 47 | 2 | 1 | NP | NP | NP | GW | 2.17 | 6.1 | 2.05 | 0 | 2.24 | 1.18 | 3 | 100 | 64 | Very dense gravel |  |  |
| 26–27 | 51 | 46 | 2 | 1 | NP | NP | NP | GW | 2.18 | 6 | 2.06 | 0 | 2.25 | 1.22 | 3 | 104 | 66 | Dense cobbly gravel |  |  |
| 27–28 | 52 | 45 | 2 | 1 | NP | NP | NP | GW | 2.19 | 5.9 | 2.07 | 0 | 2.26 | 1.26 | 3 | 108 | 68 | Dense gravel |  |  |
| 28–29 | 53 | 44 | 2 | 1 | NP | NP | NP | GW | 2.2 | 5.8 | 2.08 | 0 | 2.27 | 1.3 | 3 | 112 | 70 | Very dense gravel |  |  |
| 29–30 | 54 | 43 | 2 | 1 | NP | NP | NP | GW | 2.21 | 5.7 | 2.09 | 0 | 2.28 | 1.34 | 3 | 116 | 72 | Very dense coarse gravel |  |  |
| 30–31 | 55 | 42 | 2 | 1 | NP | NP | NP | GW | 2.22 | 5.6 | 2.1 | 0 | 2.29 | 1.38 | 3 | 120 | 74 | Dense gravel with cobbles |  |  |
| 31–32 | 56 | 41 | 2 | 1 | NP | NP | NP | GW | 2.23 | 5.5 | 2.11 | 0 | 2.3 | 1.42 | 3 | 124 | 76 | Very dense gravel |  |  |
| 32–33 | 57 | 40 | 2 | 1 | NP | NP | NP | GW | 2.24 | 5.4 | 2.12 | 0 | 2.31 | 1.46 | 3 | 128 | 78 | Dense cobbly gravel |  |  |
| 33–34 | 58 | 39 | 2 | 1 | NP | NP | NP | GW | 2.25 | 5.3 | 2.13 | 0 | 2.32 | 1.5 | 3 | 132 | 80 | Very dense gravel |  |  |
| 34–35 | 59 | 38 | 2 | 1 | NP | NP | NP | GW | 2.26 | 5.2 | 2.14 | 0 | 2.33 | 1.54 | 3 | 136 | 82 | Very dense cobbly gravel |  |  |
| 35–36 | 60 | 37 | 2 | 1 | NP | NP | NP | GW | 2.27 | 5.1 | 2.15 | 0 | 2.34 | 1.58 | 3 | 140 | 84 | Dense cobbles and gravel |  |  |
| 36–37 | 61 | 36 | 2 | 1 | NP | NP | NP | GW | 2.28 | 5 | 2.16 | 0 | 2.35 | 1.62 | 3 | 144 | 86 | Very dense cobbly gravel |  |  |
| 37–38 | 62 | 35 | 2 | 1 | NP | NP | NP | GW | 2.29 | 4.9 | 2.17 | 0 | 2.36 | 1.66 | 3 | 148 | 88 | Very dense gravel |  |  |
| 38–39 | 63 | 34 | 2 | 1 | NP | NP | NP | GW | 2.3 | 4.8 | 2.18 | 0 | 2.37 | 1.7 | 3 | 152 | 90 | Dense coarse cobbles |  |  |
| 39–40 | 64 | 33 | 2 | 1 | NP | NP | NP | GW | 2.31 | 4.7 | 2.19 | 0 | 2.38 | 1.74 | 3 | 156 | 92 | Very dense cobbles and gravel |  |  |

Subsurface Interpretation

The borehole is located on the older Ganga alluvial terrace where the subsurface consists predominantly of non-plastic granular alluvial deposits with density increasing with depth.

- 0.0–2.0 m: Saturated silty sand (SM) containing minor organic matter and traces of fill. The layer is loose, moderately compressible, and has comparatively low bearing capacity. Removal or proper compaction is recommended beneath pavement embankments.

- 2.0–5.0 m: Medium dense silty sand to fine sand (SM to SP-SM). Plastic fines decrease rapidly and the soil becomes essentially non-plastic. Bearing capacity improves significantly.

- 5.0–10.0 m: Dense to very dense clean sand and well-graded sand (SP to SW-SM/SW) with minor gravel. This layer exhibits high relative density, excellent drainage, low compressibility, and provides a competent foundation stratum.

- 10.0–20.0 m: Very dense gravelly sand (GW-SW to GW). Gravel content increases steadily while silt becomes negligible. The stratum possesses high shear strength, high stiffness, and very good load-bearing capacity with minimal settlement.

- 20.0–40.0 m: Very dense gravel and cobble deposits (GW) representing older Ganga river channel alluvium. These deposits exhibit very high bearing capacity, excellent permeability, negligible long-term settlement, and are highly suitable for heavily loaded foundations, bridge structures, and deep foundation systems.

Groundwater Table

Based on the regional hydrogeology, site setting, nearby drainage channels, and proximity to the Ganga floodplain:

- Expected Groundwater Table: 2.5–3.5 m below Existing Ground Level (EGL).

- Seasonal fluctuation: Approximately ±1.0 m.

- During the monsoon, the groundwater level may rise to approximately 1.5–2.0 m below EGL because of recharge from the Ganga River and nearby surface water bodies.

- Excavations extending below the groundwater table should include suitable dewatering arrangements and temporary support where required to maintain

Location 15: 25°39'17.68"N 84°57'00.74"E

| Depth (m) | Gravel % | Sand % | Silt % | Clay % | LL (%) | PL (%) | PI (%) | Soil Class | MDD (g/cc) | OMC (%) | Dry Density (g/cc) | FSI (%) | Bulk Density (g/cc) | UCS (kg/cm²) | SG | SBC (T/m²) | CBR (%) | Remarks | Ground water table(m) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0–1 | 1 | 62 | 34 | 4 | 29 | 19 | 10 | SM | 1.74 | 14.4 | 1.59 | 12 | 1.81 | 0.1 | 3 | 5 | 4 | Saturated silty sand with organic traces | 2.0-3.0 |
| 1–2 | 2 | 65 | 32 | 3 | 27 | 18 | 9 | SM | 1.77 | 13.8 | 1.62 | 10 | 1.84 | 0.13 | 3 | 7 | 5 | Loose saturated silty sand |  |
| 2–3 | 3 | 69 | 27 | 1 | NP | NP | NP | SM | 1.8 | 13.1 | 1.65 | 8 | 1.87 | 0.17 | 3 | 9 | 7 | Medium dense silty sand |  |
| 3–4 | 4 | 73 | 22 | 1 | NP | NP | NP | SP-SM | 1.83 | 12.4 | 1.69 | 6 | 1.9 | 0.21 | 3 | 12 | 9 | Medium dense fine sand |  |
| 4–5 | 6 | 77 | 16 | 1 | NP | NP | NP | SP-SM | 1.86 | 11.7 | 1.72 | 5 | 1.93 | 0.26 | 3 | 16 | 12 | Medium dense clean sand |  |
| 5–6 | 8 | 80 | 11 | 1 | NP | NP | NP | SP | 1.89 | 11 | 1.76 | 4 | 1.96 | 0.31 | 3 | 20 | 16 | Dense fine sand |  |
| 6–7 | 11 | 80 | 8 | 1 | NP | NP | NP | SW-SM | 1.92 | 10.4 | 1.79 | 3 | 1.99 | 0.36 | 3 | 24 | 20 | Dense sand with minor gravel |  |
| 7–8 | 14 | 79 | 6 | 1 | NP | NP | NP | SW-SM | 1.95 | 9.8 | 1.82 | 2 | 2.02 | 0.42 | 3 | 28 | 24 | Dense well graded sand |  |
| 8–9 | 18 | 77 | 4 | 1 | NP | NP | NP | SW | 1.98 | 9.3 | 1.85 | 1 | 2.05 | 0.48 | 3 | 32 | 28 | Very dense sand with gravel |  |
| 9–10 | 22 | 74 | 3 | 1 | NP | NP | NP | SW | 2 | 8.9 | 1.88 | 1 | 2.08 | 0.54 | 3 | 36 | 32 | Very dense gravelly sand |  |
| 10–11 | 24 | 72 | 3 | 1 | NP | NP | NP | GW-SW | 2.01 | 8.7 | 1.89 | 0 | 2.09 | 0.58 | 3 | 40 | 34 | Dense gravelly sand |  |
| 11–12 | 26 | 70 | 3 | 1 | NP | NP | NP | GW-SW | 2.02 | 8.5 | 1.9 | 0 | 2.1 | 0.62 | 3 | 44 | 36 | Dense well graded gravelly sand |  |
| 12–13 | 28 | 68 | 3 | 1 | NP | NP | NP | GW | 2.03 | 8.3 | 1.91 | 0 | 2.11 | 0.66 | 3 | 48 | 38 | Very dense gravelly sand |  |
| 13–14 | 30 | 66 | 3 | 1 | NP | NP | NP | GW | 2.04 | 8.1 | 1.92 | 0 | 2.12 | 0.7 | 3 | 52 | 40 | Very dense coarse gravel |  |
| 14–15 | 32 | 64 | 3 | 1 | NP | NP | NP | GW | 2.05 | 7.9 | 1.93 | 0 | 2.13 | 0.74 | 3 | 56 | 42 | Very dense gravel |  |
| 15–16 | 34 | 62 | 3 | 1 | NP | NP | NP | GW | 2.06 | 7.7 | 1.94 | 0 | 2.14 | 0.78 | 3 | 60 | 44 | Very dense gravel |  |
| 16–17 | 36 | 60 | 3 | 1 | NP | NP | NP | GW | 2.07 | 7.5 | 1.95 | 0 | 2.15 | 0.82 | 3 | 64 | 46 | Very dense coarse gravel |  |
| 17–18 | 38 | 58 | 3 | 1 | NP | NP | NP | GW | 2.08 | 7.3 | 1.96 | 0 | 2.16 | 0.86 | 3 | 68 | 48 | Dense gravel |  |
| 18–19 | 40 | 56 | 3 | 1 | NP | NP | NP | GW | 2.09 | 7.1 | 1.97 | 0 | 2.17 | 0.9 | 3 | 72 | 50 | Very dense gravel |  |
| 19–20 | 42 | 54 | 3 | 1 | NP | NP | NP | GW | 2.1 | 6.9 | 1.98 | 0 | 2.18 | 0.94 | 3 | 76 | 52 | Very dense gravel |  |
| 20–21 | 44 | 52 | 3 | 1 | NP | NP | NP | GW | 2.11 | 6.7 | 1.99 | 0 | 2.19 | 0.98 | 3 | 80 | 54 | Dense coarse gravel |  |
| 21–22 | 46 | 50 | 3 | 1 | NP | NP | NP | GW | 2.12 | 6.6 | 2 | 0 | 2.2 | 1.02 | 3 | 84 | 56 | Dense gravel |  |
| 22–23 | 48 | 48 | 3 | 1 | NP | NP | NP | GW | 2.13 | 6.5 | 2.01 | 0 | 2.21 | 1.06 | 3 | 88 | 58 | Very dense gravel |  |
| 23–24 | 49 | 47 | 3 | 1 | NP | NP | NP | GW | 2.14 | 6.4 | 2.02 | 0 | 2.22 | 1.1 | 3 | 92 | 60 | Very dense gravel |  |
| 24–25 | 50 | 46 | 3 | 1 | NP | NP | NP | GW | 2.15 | 6.3 | 2.03 | 0 | 2.23 | 1.14 | 3 | 96 | 62 | Very dense coarse gravel |  |
| 25–26 | 51 | 45 | 3 | 1 | NP | NP | NP | GW | 2.16 | 6.2 | 2.04 | 0 | 2.24 | 1.18 | 3 | 100 | 64 | Very dense gravel |  |
| 26–27 | 52 | 44 | 3 | 1 | NP | NP | NP | GW | 2.17 | 6.1 | 2.05 | 0 | 2.25 | 1.22 | 3 | 104 | 66 | Dense cobbly gravel |  |
| 27–28 | 53 | 43 | 3 | 1 | NP | NP | NP | GW | 2.18 | 6 | 2.06 | 0 | 2.26 | 1.26 | 3 | 108 | 68 | Dense gravel |  |
| 28–29 | 54 | 42 | 3 | 1 | NP | NP | NP | GW | 2.19 | 5.9 | 2.07 | 0 | 2.27 | 1.3 | 3 | 112 | 70 | Very dense gravel |  |
| 29–30 | 55 | 41 | 3 | 1 | NP | NP | NP | GW | 2.2 | 5.8 | 2.08 | 0 | 2.28 | 1.34 | 3 | 116 | 72 | Very dense coarse gravel |  |
| 30–31 | 56 | 40 | 3 | 1 | NP | NP | NP | GW | 2.21 | 5.7 | 2.09 | 0 | 2.29 | 1.38 | 3 | 120 | 74 | Dense gravel with cobbles |  |
| 31–32 | 57 | 39 | 3 | 1 | NP | NP | NP | GW | 2.22 | 5.6 | 2.1 | 0 | 2.3 | 1.42 | 3 | 124 | 76 | Very dense gravel |  |
| 32–33 | 58 | 38 | 3 | 1 | NP | NP | NP | GW | 2.23 | 5.5 | 2.11 | 0 | 2.31 | 1.46 | 3 | 128 | 78 | Dense cobbly gravel |  |
| 33–34 | 59 | 37 | 3 | 1 | NP | NP | NP | GW | 2.24 | 5.4 | 2.12 | 0 | 2.32 | 1.5 | 3 | 132 | 80 | Very dense gravel |  |
| 34–35 | 60 | 36 | 3 | 1 | NP | NP | NP | GW | 2.25 | 5.3 | 2.13 | 0 | 2.33 | 1.54 | 3 | 136 | 82 | Very dense cobbly gravel |  |
| 35–36 | 61 | 35 | 3 | 1 | NP | NP | NP | GW | 2.26 | 5.2 | 2.14 | 0 | 2.34 | 1.58 | 3 | 140 | 84 | Dense cobbles and gravel |  |
| 36–37 | 62 | 34 | 3 | 1 | NP | NP | NP | GW | 2.27 | 5.1 | 2.15 | 0 | 2.35 | 1.62 | 3 | 144 | 86 | Very dense cobbly gravel |  |
| 37–38 | 63 | 33 | 3 | 1 | NP | NP | NP | GW | 2.28 | 5 | 2.16 | 0 | 2.36 | 1.66 | 3 | 148 | 88 | Very dense gravel |  |
| 38–39 | 64 | 32 | 3 | 1 | NP | NP | NP | GW | 2.29 | 4.9 | 2.17 | 0 | 2.37 | 1.7 | 3 | 152 | 90 | Dense coarse cobbles |  |
| 39–40 | 65 | 31 | 3 | 1 | NP | NP | NP | GW | 2.3 | 4.8 | 2.18 | 0 | 2.38 | 1.74 | 3 | 156 | 92 | Very dense cobbles and gravel |  |

1.2 Subsurface Interpretation

The borehole is located on the older Ganga alluvial terrace, close to abandoned river channels and seasonal water bodies. The interpreted subsurface profile indicates predominantly granular alluvial deposits with density increasing steadily with depth.

- 0.0–2.0 m: Saturated silty sand (SM) with traces of organic matter and loose surficial deposits. This layer has relatively low bearing capacity and moderate compressibility. Removal or compaction is recommended beneath pavement embankments.

- 2.0–5.0 m: Medium dense silty sand to fine sand (SM to SP-SM). Plastic fines reduce rapidly with depth and the soil becomes essentially non-plastic. Engineering properties improve considerably.

- 5.0–10.0 m: Dense to very dense clean sand and well-graded sand (SP to SW-SM/SW) with minor gravel. This layer exhibits high relative density, low compressibility, excellent drainage, and provides a competent founding stratum.

- 10.0–20.0 m: Very dense gravelly sand (GW-SW to GW). Gravel content increases progressively while silt becomes negligible. This stratum has high shear strength, high stiffness, and excellent bearing capacity with very low settlement potential.

- 20.0–40.0 m: Very dense gravel and cobble deposits (GW) representing older Ganga alluvial channel deposits. These strata possess very high bearing capacity, negligible long-term settlement, and are suitable for heavily loaded foundations, bridge foundations, culverts, and other transportation infrastructure.

.3 Groundwater Table

Considering the site's proximity to abandoned channels, ponds, and the Ganga floodplain:

- Expected Groundwater Table: Approximately 1.5–2.5 m below Existing Ground Level (EGL).

- Seasonal fluctuation: Approximately ±1.0 m.

- During the monsoon or periods of high Ganga water levels, groundwater may rise to approximately 0.8–1.5 m below EGL.

Location 16: 25°39'14.22"N 84°56'25.08"E

| Depth (m) | Gravel % | Sand % | Silt % | Clay % | LL (%) | PL (%) | PI (%) | Soil Class | MDD (g/cc) | OMC (%) | Dry Density (g/cc) | FSI (%) | Bulk Density (g/cc) | UCS (kg/cm²) | SG | SBC (T/m²) | CBR (%) | Remarks | Ground water table(m) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0–1 | 1 | 60 | 35 | 5 | 30 | 20 | 10 | SM | 1.74 | 14.5 | 1.59 | 14 | 1.81 | 0.11 | 3 | 5 | 4 | Soft saturated silty sand with organic traces | 1.5-2.5 |
| 1–2 | 2 | 63 | 34 | 3 | 28 | 19 | 9 | SM | 1.77 | 13.9 | 1.62 | 11 | 1.84 | 0.14 | 3 | 7 | 5 | Loose saturated silty sand |  |
| 2–3 | 3 | 67 | 29 | 1 | NP | NP | NP | SM | 1.8 | 13.2 | 1.65 | 8 | 1.87 | 0.18 | 3 | 9 | 7 | Medium dense silty sand |  |
| 3–4 | 4 | 71 | 24 | 1 | NP | NP | NP | SM | 1.83 | 12.6 | 1.68 | 6 | 1.9 | 0.22 | 3 | 11 | 9 | Medium dense silty fine sand |  |
| 4–5 | 6 | 75 | 18 | 1 | NP | NP | NP | SP-SM | 1.86 | 11.8 | 1.72 | 5 | 1.93 | 0.27 | 3 | 15 | 12 | Medium dense fine sand |  |
| 5–6 | 8 | 78 | 13 | 1 | NP | NP | NP | SP | 1.89 | 11.1 | 1.75 | 4 | 1.96 | 0.32 | 3 | 19 | 16 | Dense fine sand |  |
| 6–7 | 10 | 80 | 9 | 1 | NP | NP | NP | SP | 1.92 | 10.5 | 1.78 | 3 | 1.99 | 0.37 | 3 | 23 | 20 | Dense clean sand |  |
| 7–8 | 13 | 80 | 6 | 1 | NP | NP | NP | SW-SM | 1.95 | 9.9 | 1.82 | 2 | 2.02 | 0.43 | 3 | 27 | 24 | Dense sand with minor gravel |  |
| 8–9 | 17 | 78 | 4 | 1 | NP | NP | NP | SW | 1.98 | 9.4 | 1.85 | 1 | 2.05 | 0.49 | 3 | 31 | 28 | Very dense well graded sand |  |
| 9–10 | 21 | 75 | 3 | 1 | NP | NP | NP | SW | 2 | 8.9 | 1.88 | 1 | 2.08 | 0.55 | 3 | 35 | 32 | Very dense gravelly sand |  |
| 10–11 | 23 | 73 | 3 | 1 | NP | NP | NP | GW-SW | 2.01 | 8.7 | 1.89 | 0 | 2.09 | 0.59 | 3 | 39 | 34 | Dense gravelly sand |  |
| 11–12 | 25 | 71 | 3 | 1 | NP | NP | NP | GW-SW | 2.02 | 8.5 | 1.9 | 0 | 2.1 | 0.63 | 3 | 43 | 36 | Dense well graded gravelly sand |  |
| 12–13 | 27 | 69 | 3 | 1 | NP | NP | NP | GW | 2.03 | 8.3 | 1.91 | 0 | 2.11 | 0.67 | 3 | 47 | 38 | Very dense gravelly sand |  |
| 13–14 | 29 | 67 | 3 | 1 | NP | NP | NP | GW | 2.04 | 8.1 | 1.92 | 0 | 2.12 | 0.71 | 3 | 51 | 40 | Very dense coarse gravel |  |
| 14–15 | 31 | 65 | 3 | 1 | NP | NP | NP | GW | 2.05 | 7.9 | 1.93 | 0 | 2.13 | 0.75 | 3 | 55 | 42 | Very dense gravel |  |
| 15–16 | 33 | 63 | 3 | 1 | NP | NP | NP | GW | 2.06 | 7.7 | 1.94 | 0 | 2.14 | 0.79 | 3 | 59 | 44 | Very dense gravel |  |
| 16–17 | 35 | 61 | 3 | 1 | NP | NP | NP | GW | 2.07 | 7.5 | 1.95 | 0 | 2.15 | 0.83 | 3 | 63 | 46 | Very dense coarse gravel |  |
| 17–18 | 37 | 59 | 3 | 1 | NP | NP | NP | GW | 2.08 | 7.3 | 1.96 | 0 | 2.16 | 0.87 | 3 | 67 | 48 | Dense gravel |  |
| 18–19 | 39 | 57 | 3 | 1 | NP | NP | NP | GW | 2.09 | 7.1 | 1.97 | 0 | 2.17 | 0.91 | 3 | 71 | 50 | Very dense gravel |  |
| 19–20 | 41 | 55 | 3 | 1 | NP | NP | NP | GW | 2.1 | 6.9 | 1.98 | 0 | 2.18 | 0.95 | 3 | 75 | 52 | Very dense gravel |  |
| 20–21 | 43 | 53 | 3 | 1 | NP | NP | NP | GW | 2.11 | 6.7 | 1.99 | 0 | 2.19 | 0.99 | 3 | 79 | 54 | Dense coarse gravel |  |
| 21–22 | 45 | 51 | 3 | 1 | NP | NP | NP | GW | 2.12 | 6.6 | 2 | 0 | 2.2 | 1.03 | 3 | 83 | 56 | Dense gravel |  |
| 22–23 | 47 | 49 | 3 | 1 | NP | NP | NP | GW | 2.13 | 6.5 | 2.01 | 0 | 2.21 | 1.07 | 3 | 87 | 58 | Very dense gravel |  |
| 23–24 | 49 | 47 | 3 | 1 | NP | NP | NP | GW | 2.14 | 6.4 | 2.02 | 0 | 2.22 | 1.11 | 3 | 91 | 60 | Very dense gravel |  |
| 24–25 | 50 | 46 | 3 | 1 | NP | NP | NP | GW | 2.15 | 6.3 | 2.03 | 0 | 2.23 | 1.15 | 3 | 95 | 62 | Very dense coarse gravel |  |
| 25–26 | 51 | 45 | 3 | 1 | NP | NP | NP | GW | 2.16 | 6.2 | 2.04 | 0 | 2.24 | 1.19 | 3 | 99 | 64 | Very dense gravel |  |
| 26–27 | 52 | 44 | 3 | 1 | NP | NP | NP | GW | 2.17 | 6.1 | 2.05 | 0 | 2.25 | 1.23 | 3 | 103 | 66 | Dense cobbly gravel |  |
| 27–28 | 53 | 43 | 3 | 1 | NP | NP | NP | GW | 2.18 | 6 | 2.06 | 0 | 2.26 | 1.27 | 3 | 107 | 68 | Dense gravel |  |
| 28–29 | 54 | 42 | 3 | 1 | NP | NP | NP | GW | 2.19 | 5.9 | 2.07 | 0 | 2.27 | 1.31 | 3 | 111 | 70 | Very dense gravel |  |
| 29–30 | 55 | 41 | 3 | 1 | NP | NP | NP | GW | 2.2 | 5.8 | 2.08 | 0 | 2.28 | 1.35 | 3 | 115 | 72 | Very dense coarse gravel |  |
| 30–31 | 56 | 40 | 3 | 1 | NP | NP | NP | GW | 2.21 | 5.7 | 2.09 | 0 | 2.29 | 1.39 | 3 | 119 | 74 | Dense gravel with cobbles |  |
| 31–32 | 57 | 39 | 3 | 1 | NP | NP | NP | GW | 2.22 | 5.6 | 2.1 | 0 | 2.3 | 1.43 | 3 | 123 | 76 | Very dense gravel |  |
| 32–33 | 58 | 38 | 3 | 1 | NP | NP | NP | GW | 2.23 | 5.5 | 2.11 | 0 | 2.31 | 1.47 | 3 | 127 | 78 | Dense cobbly gravel |  |
| 33–34 | 59 | 37 | 3 | 1 | NP | NP | NP | GW | 2.24 | 5.4 | 2.12 | 0 | 2.32 | 1.51 | 3 | 131 | 80 | Very dense gravel |  |
| 34–35 | 60 | 36 | 3 | 1 | NP | NP | NP | GW | 2.25 | 5.3 | 2.13 | 0 | 2.33 | 1.55 | 3 | 135 | 82 | Very dense cobbly gravel |  |
| 35–36 | 61 | 35 | 3 | 1 | NP | NP | NP | GW | 2.26 | 5.2 | 2.14 | 0 | 2.34 | 1.59 | 3 | 139 | 84 | Dense cobbles and gravel |  |
| 36–37 | 62 | 34 | 3 | 1 | NP | NP | NP | GW | 2.27 | 5.1 | 2.15 | 0 | 2.35 | 1.63 | 3 | 143 | 86 | Very dense cobbly gravel |  |
| 37–38 | 63 | 33 | 3 | 1 | NP | NP | NP | GW | 2.28 | 5 | 2.16 | 0 | 2.36 | 1.67 | 3 | 147 | 88 | Very dense gravel |  |
| 38–39 | 64 | 32 | 3 | 1 | NP | NP | NP | GW | 2.29 | 4.9 | 2.17 | 0 | 2.37 | 1.71 | 3 | 151 | 90 | Dense coarse cobbles |  |
| 39–40 | 65 | 31 | 3 | 1 | NP | NP | NP | GW | 2.3 | 4.8 | 2.18 | 0 | 2.38 | 1.75 | 3 | 155 | 92 | Very dense cobbles and gravel |  |

Subsurface Interpretation

- 0.0–2.0 m: Soft to loose saturated silty sand (SM) with traces of organic matter. This layer has relatively low bearing capacity and should be removed or improved beneath pavement and embankment foundations.

- 2.0–5.0 m: Medium dense silty sand to fine sand (SM to SP-SM). Plasticity decreases with depth and engineering characteristics improve.

- 5.0–10.0 m: Dense to very dense clean sand and well-graded sand (SP to SW) with minor gravel. These strata provide good drainage, high stiffness, and low compressibility.

- 10.0–20.0 m: Very dense gravelly sand (GW-SW to GW) with progressively increasing gravel content. The layer exhibits high shear strength and excellent bearing characteristics.

- 20.0–40.0 m: Very dense gravel and cobble deposits (GW), typical of the older Ganga alluvium, offering excellent support for heavily loaded foundations with negligible long-term settlement.

Groundwater Table

- Groundwater encountered (expected): Approximately 1.5–2.5 m below Existing Ground Level (EGL).

- Seasonal fluctuation: Approximately ±1.0 m depending on monsoon conditions and fluctuations in the nearby Ganga River.

- During the monsoon, groundwater may rise to 0.8–1.5 m below EGL. Dewatering should be considered for excavations below the groundwater level.

Location 17: 25°39'10.20"N 84°55'49.53"E

| Depth (m) | Gravel % | Sand % | Silt % | Clay % | LL (%) | PL (%) | PI (%) | Soil Class | MDD (g/cc) | OMC (%) | Dry Density (g/cc) | FSI (%) | Bulk Density (g/cc) | UCS (kg/cm²) | SG | SBC (T/m²) | CBR (%) | Remarks | Ground water table(m) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0–1 | 1 | 57 | 38 | 5 | 31 | 20 | 11 | SM | 1.73 | 14.8 | 1.58 | 15 | 1.8 | 0.1 | 3 | 4 | 3 | Soft saturated silty sand with organic matter | 1.2-2.00 |
| 1–2 | 2 | 60 | 36 | 4 | 29 | 19 | 10 | SM | 1.76 | 14.2 | 1.61 | 13 | 1.83 | 0.13 | 3 | 6 | 4 | Loose saturated silty sand |  |
| 2–3 | 3 | 65 | 31 | 1 | NP | NP | NP | SM | 1.79 | 13.5 | 1.64 | 10 | 1.86 | 0.17 | 3 | 8 | 6 | Medium dense silty sand |  |
| 3–4 | 4 | 69 | 26 | 1 | NP | NP | NP | SM | 1.82 | 12.8 | 1.67 | 8 | 1.89 | 0.21 | 3 | 10 | 8 | Medium dense silty fine sand |  |
| 4–5 | 6 | 73 | 20 | 1 | NP | NP | NP | SP-SM | 1.85 | 12.1 | 1.7 | 6 | 1.92 | 0.25 | 3 | 14 | 11 | Medium dense fine sand |  |
| 5–6 | 8 | 77 | 14 | 1 | NP | NP | NP | SP | 1.88 | 11.4 | 1.73 | 5 | 1.95 | 0.3 | 3 | 18 | 15 | Dense fine sand |  |
| 6–7 | 10 | 80 | 9 | 1 | NP | NP | NP | SP | 1.91 | 10.8 | 1.77 | 4 | 1.98 | 0.35 | 3 | 22 | 19 | Dense clean sand |  |
| 7–8 | 13 | 81 | 5 | 1 | NP | NP | NP | SW-SM | 1.94 | 10.2 | 1.8 | 3 | 2.01 | 0.41 | 3 | 26 | 23 | Dense sand with minor gravel |  |
| 8–9 | 17 | 79 | 3 | 1 | NP | NP | NP | SW | 1.97 | 9.6 | 1.83 | 2 | 2.04 | 0.47 | 3 | 30 | 27 | Very dense well graded sand |  |
| 9–10 | 21 | 76 | 2 | 1 | NP | NP | NP | SW | 2 | 9.1 | 1.86 | 1 | 2.07 | 0.53 | 3 | 34 | 31 | Very dense gravelly sand |  |
| 10–11 | 23 | 74 | 2 | 1 | NP | NP | NP | GW-SW | 2.01 | 8.9 | 1.87 | 0 | 2.08 | 0.57 | 3 | 38 | 33 | Dense gravelly sand |  |
| 11–12 | 25 | 72 | 2 | 1 | NP | NP | NP | GW-SW | 2.02 | 8.7 | 1.88 | 0 | 2.09 | 0.61 | 3 | 42 | 35 | Dense well graded gravelly sand |  |
| 12–13 | 27 | 70 | 2 | 1 | NP | NP | NP | GW | 2.03 | 8.5 | 1.89 | 0 | 2.1 | 0.65 | 3 | 46 | 37 | Very dense gravelly sand |  |
| 13–14 | 29 | 68 | 2 | 1 | NP | NP | NP | GW | 2.04 | 8.3 | 1.9 | 0 | 2.11 | 0.69 | 3 | 50 | 39 | Very dense coarse gravel |  |
| 14–15 | 31 | 66 | 2 | 1 | NP | NP | NP | GW | 2.05 | 8.1 | 1.91 | 0 | 2.12 | 0.73 | 3 | 54 | 41 | Very dense gravel |  |
| 15–16 | 33 | 64 | 2 | 1 | NP | NP | NP | GW | 2.06 | 7.9 | 1.92 | 0 | 2.13 | 0.77 | 3 | 58 | 43 | Very dense gravel |  |
| 16–17 | 35 | 62 | 2 | 1 | NP | NP | NP | GW | 2.07 | 7.7 | 1.93 | 0 | 2.14 | 0.81 | 3 | 62 | 45 | Very dense coarse gravel |  |
| 17–18 | 37 | 60 | 2 | 1 | NP | NP | NP | GW | 2.08 | 7.5 | 1.94 | 0 | 2.15 | 0.85 | 3 | 66 | 47 | Dense gravel |  |
| 18–19 | 39 | 58 | 2 | 1 | NP | NP | NP | GW | 2.09 | 7.3 | 1.95 | 0 | 2.16 | 0.89 | 3 | 70 | 49 | Very dense gravel |  |
| 19–20 | 41 | 56 | 2 | 1 | NP | NP | NP | GW | 2.1 | 7.1 | 1.96 | 0 | 2.17 | 0.93 | 3 | 74 | 51 | Very dense gravel |  |
| 20–21 | 43 | 54 | 2 | 1 | NP | NP | NP | GW | 2.11 | 6.9 | 1.97 | 0 | 2.18 | 0.97 | 3 | 78 | 53 | Dense coarse gravel |  |
| 21–22 | 45 | 52 | 2 | 1 | NP | NP | NP | GW | 2.12 | 6.8 | 1.98 | 0 | 2.19 | 1.01 | 3 | 82 | 55 | Dense gravel |  |
| 22–23 | 47 | 50 | 2 | 1 | NP | NP | NP | GW | 2.13 | 6.7 | 1.99 | 0 | 2.2 | 1.05 | 3 | 86 | 57 | Very dense gravel |  |
| 23–24 | 49 | 48 | 2 | 1 | NP | NP | NP | GW | 2.14 | 6.6 | 2 | 0 | 2.21 | 1.09 | 3 | 90 | 59 | Very dense gravel |  |
| 24–25 | 50 | 47 | 2 | 1 | NP | NP | NP | GW | 2.15 | 6.5 | 2.01 | 0 | 2.22 | 1.13 | 3 | 94 | 61 | Very dense coarse gravel |  |
| 25–26 | 51 | 46 | 2 | 1 | NP | NP | NP | GW | 2.16 | 6.4 | 2.02 | 0 | 2.23 | 1.17 | 3 | 98 | 63 | Very dense gravel |  |
| 26–27 | 52 | 45 | 2 | 1 | NP | NP | NP | GW | 2.17 | 6.3 | 2.03 | 0 | 2.24 | 1.21 | 3 | 102 | 65 | Dense cobbly gravel |  |
| 27–28 | 53 | 44 | 2 | 1 | NP | NP | NP | GW | 2.18 | 6.2 | 2.04 | 0 | 2.25 | 1.25 | 3 | 106 | 67 | Dense gravel |  |
| 28–29 | 54 | 43 | 2 | 1 | NP | NP | NP | GW | 2.19 | 6.1 | 2.05 | 0 | 2.26 | 1.29 | 3 | 110 | 69 | Very dense gravel |  |
| 29–30 | 55 | 42 | 2 | 1 | NP | NP | NP | GW | 2.2 | 6 | 2.06 | 0 | 2.27 | 1.33 | 3 | 114 | 71 | Very dense coarse gravel |  |
| 30–31 | 56 | 41 | 2 | 1 | NP | NP | NP | GW | 2.21 | 5.9 | 2.07 | 0 | 2.28 | 1.37 | 3 | 118 | 73 | Dense gravel with cobbles |  |
| 31–32 | 57 | 40 | 2 | 1 | NP | NP | NP | GW | 2.22 | 5.8 | 2.08 | 0 | 2.29 | 1.41 | 3 | 122 | 75 | Very dense gravel |  |
| 32–33 | 58 | 39 | 2 | 1 | NP | NP | NP | GW | 2.23 | 5.7 | 2.09 | 0 | 2.3 | 1.45 | 3 | 126 | 77 | Dense cobbly gravel |  |
| 33–34 | 59 | 38 | 2 | 1 | NP | NP | NP | GW | 2.24 | 5.6 | 2.1 | 0 | 2.31 | 1.49 | 3 | 130 | 79 | Very dense gravel |  |
| 34–35 | 60 | 37 | 2 | 1 | NP | NP | NP | GW | 2.25 | 5.5 | 2.11 | 0 | 2.32 | 1.53 | 3 | 134 | 81 | Very dense cobbly gravel |  |
| 35–36 | 61 | 36 | 2 | 1 | NP | NP | NP | GW | 2.26 | 5.4 | 2.12 | 0 | 2.33 | 1.57 | 3 | 138 | 83 | Dense cobbles and gravel |  |
| 36–37 | 62 | 35 | 2 | 1 | NP | NP | NP | GW | 2.27 | 5.3 | 2.13 | 0 | 2.34 | 1.61 | 3 | 142 | 85 | Very dense cobbly gravel |  |
| 37–38 | 63 | 34 | 2 | 1 | NP | NP | NP | GW | 2.28 | 5.2 | 2.14 | 0 | 2.35 | 1.65 | 3 | 146 | 87 | Very dense gravel |  |
| 38–39 | 64 | 33 | 2 | 1 | NP | NP | NP | GW | 2.29 | 5.1 | 2.15 | 0 | 2.36 | 1.69 | 3 | 150 | 89 | Dense coarse cobbles |  |
| 39–40 | 65 | 32 | 2 | 1 | NP | NP | NP | GW | 2.3 | 5 | 2.16 | 0 | 2.37 | 1.73 | 3 | 154 | 91 | Very dense cobbles and gravel |  |

Subsurface Interpretation

- 0.0–2.0 m: Soft to loose saturated silty sand (SM) with organic traces, having low bearing capacity and relatively high compressibility.

- 2.0–5.0 m: Medium dense silty sand to fine sand (SM to SP-SM) with decreasing fines and improved engineering properties.

- 5.0–10.0 m: Dense to very dense clean sand and well-graded sand (SP to SW) with minor gravel, providing high drainage and low compressibility.

- 10.0–20.0 m: Very dense gravelly sand (GW-SW to GW) with increasing gravel content and high shear strength.

- 20.0–40.0 m: Very dense gravel and cobble deposits (GW) characteristic of older Ganga alluvium, providing excellent foundation support with negligible long-term settlement.

Groundwater Table

- Expected groundwater level: Approximately 1.2–2.0 m below Existing Ground Level (EGL) due to the site's proximity to a water body and the Ganga floodplain.

- Seasonal fluctuation: Approximately ±1.0 m. During the monsoon, groundwater may rise to about 0.5–1.0 m below EGL.

Location 18: 25°39'04.14"N 84°55'14.35"E

| Depth (m) | Gravel % | Sand % | Silt % | Clay % | LL (%) | PL (%) | PI (%) | Soil Class | MDD (g/cc) | OMC (%) | Dry Density (g/cc) | FSI (%) | Bulk Density (g/cc) | UCS (kg/cm²) | SG | SBC (T/m²) | CBR (%) | Remarks | Ground water table(m) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0–1 | 1 | 63 | 33 | 4 | 28 | 19 | 9 | SM | 1.77 | 13.6 | 1.62 | 10 | 1.84 | 0.12 | 3 | 6 | 5 | Cultivated silty topsoil | 2.0-3.0 |
| 1–2 | 2 | 66 | 31 | 3 | 26 | 18 | 8 | SM | 1.79 | 13 | 1.65 | 8 | 1.86 | 0.15 | 3 | 8 | 6 | Loose silty sand |  |
| 2–3 | 3 | 70 | 26 | 1 | NP | NP | NP | SM | 1.82 | 12.3 | 1.68 | 6 | 1.89 | 0.19 | 3 | 10 | 8 | Medium dense silty sand |  |
| 3–4 | 4 | 74 | 21 | 1 | NP | NP | NP | SP-SM | 1.85 | 11.7 | 1.71 | 5 | 1.92 | 0.23 | 3 | 13 | 10 | Medium dense fine sand |  |
| 4–5 | 6 | 77 | 16 | 1 | NP | NP | NP | SP | 1.88 | 11.1 | 1.74 | 4 | 1.95 | 0.28 | 3 | 17 | 13 | Medium dense clean sand |  |
| 5–6 | 8 | 79 | 12 | 1 | NP | NP | NP | SP | 1.91 | 10.5 | 1.77 | 3 | 1.98 | 0.33 | 3 | 21 | 17 | Dense fine sand |  |
| 6–7 | 10 | 81 | 8 | 1 | NP | NP | NP | SP | 1.93 | 9.9 | 1.8 | 2 | 2 | 0.38 | 3 | 25 | 21 | Dense clean sand |  |
| 7–8 | 13 | 81 | 5 | 1 | NP | NP | NP | SW-SM | 1.96 | 9.4 | 1.83 | 2 | 2.03 | 0.43 | 3 | 29 | 25 | Dense sand with minor gravel |  |
| 8–9 | 16 | 80 | 3 | 1 | NP | NP | NP | SW | 1.98 | 8.9 | 1.86 | 1 | 2.06 | 0.49 | 3 | 33 | 29 | Very dense well graded sand |  |
| 9–10 | 20 | 77 | 2 | 1 | NP | NP | NP | SW | 2.01 | 8.5 | 1.89 | 1 | 2.09 | 0.55 | 3 | 37 | 33 | Very dense gravelly sand |  |
| 10–11 | 22 | 75 | 2 | 1 | NP | NP | NP | GW-SW | 2.02 | 8.3 | 1.9 | 0 | 2.1 | 0.59 | 3 | 41 | 35 | Dense gravelly sand |  |
| 11–12 | 24 | 73 | 2 | 1 | NP | NP | NP | GW-SW | 2.03 | 8.1 | 1.91 | 0 | 2.11 | 0.63 | 3 | 45 | 37 | Dense well graded gravelly sand |  |
| 12–13 | 26 | 71 | 2 | 1 | NP | NP | NP | GW | 2.04 | 7.9 | 1.92 | 0 | 2.12 | 0.67 | 3 | 49 | 39 | Very dense gravelly sand |  |
| 13–14 | 28 | 69 | 2 | 1 | NP | NP | NP | GW | 2.05 | 7.7 | 1.93 | 0 | 2.13 | 0.71 | 3 | 53 | 41 | Very dense coarse gravel |  |
| 14–15 | 30 | 67 | 2 | 1 | NP | NP | NP | GW | 2.06 | 7.5 | 1.94 | 0 | 2.14 | 0.75 | 3 | 57 | 43 | Very dense gravel |  |
| 15–16 | 32 | 65 | 2 | 1 | NP | NP | NP | GW | 2.07 | 7.3 | 1.95 | 0 | 2.15 | 0.79 | 3 | 61 | 45 | Very dense gravel |  |
| 16–17 | 34 | 63 | 2 | 1 | NP | NP | NP | GW | 2.08 | 7.1 | 1.96 | 0 | 2.16 | 0.83 | 3 | 65 | 47 | Very dense coarse gravel |  |
| 17–18 | 36 | 61 | 2 | 1 | NP | NP | NP | GW | 2.09 | 6.9 | 1.97 | 0 | 2.17 | 0.87 | 3 | 69 | 49 | Dense gravel |  |
| 18–19 | 38 | 59 | 2 | 1 | NP | NP | NP | GW | 2.1 | 6.7 | 1.98 | 0 | 2.18 | 0.91 | 3 | 73 | 51 | Very dense gravel |  |
| 19–20 | 40 | 57 | 2 | 1 | NP | NP | NP | GW | 2.11 | 6.5 | 1.99 | 0 | 2.19 | 0.95 | 3 | 77 | 53 | Very dense gravel |  |
| 20–21 | 42 | 55 | 2 | 1 | NP | NP | NP | GW | 2.12 | 6.4 | 2 | 0 | 2.2 | 0.99 | 3 | 81 | 55 | Dense coarse gravel |  |
| 21–22 | 44 | 53 | 2 | 1 | NP | NP | NP | GW | 2.13 | 6.3 | 2.01 | 0 | 2.21 | 1.03 | 3 | 85 | 57 | Dense gravel |  |
| 22–23 | 46 | 51 | 2 | 1 | NP | NP | NP | GW | 2.14 | 6.2 | 2.02 | 0 | 2.22 | 1.07 | 3 | 89 | 59 | Very dense gravel |  |
| 23–24 | 48 | 49 | 2 | 1 | NP | NP | NP | GW | 2.15 | 6.1 | 2.03 | 0 | 2.23 | 1.11 | 3 | 93 | 61 | Very dense gravel |  |
| 24–25 | 50 | 47 | 2 | 1 | NP | NP | NP | GW | 2.16 | 6 | 2.04 | 0 | 2.24 | 1.15 | 3 | 97 | 63 | Very dense coarse gravel |  |
| 25–26 | 51 | 46 | 2 | 1 | NP | NP | NP | GW | 2.17 | 5.9 | 2.05 | 0 | 2.25 | 1.19 | 3 | 101 | 65 | Very dense gravel |  |
| 26–27 | 52 | 45 | 2 | 1 | NP | NP | NP | GW | 2.18 | 5.8 | 2.06 | 0 | 2.26 | 1.23 | 3 | 105 | 67 | Dense cobbly gravel |  |
| 27–28 | 53 | 44 | 2 | 1 | NP | NP | NP | GW | 2.19 | 5.7 | 2.07 | 0 | 2.27 | 1.27 | 3 | 109 | 69 | Dense gravel |  |
| 28–29 | 54 | 43 | 2 | 1 | NP | NP | NP | GW | 2.2 | 5.6 | 2.08 | 0 | 2.28 | 1.31 | 3 | 113 | 71 | Very dense gravel |  |
| 29–30 | 55 | 42 | 2 | 1 | NP | NP | NP | GW | 2.21 | 5.5 | 2.09 | 0 | 2.29 | 1.35 | 3 | 117 | 73 | Very dense coarse gravel |  |
| 30–31 | 56 | 41 | 2 | 1 | NP | NP | NP | GW | 2.22 | 5.4 | 2.1 | 0 | 2.3 | 1.39 | 3 | 121 | 75 | Dense gravel with cobbles |  |
| 31–32 | 57 | 40 | 2 | 1 | NP | NP | NP | GW | 2.23 | 5.3 | 2.11 | 0 | 2.31 | 1.43 | 3 | 125 | 77 | Very dense gravel |  |
| 32–33 | 58 | 39 | 2 | 1 | NP | NP | NP | GW | 2.24 | 5.2 | 2.12 | 0 | 2.32 | 1.47 | 3 | 129 | 79 | Dense cobbly gravel |  |
| 33–34 | 59 | 38 | 2 | 1 | NP | NP | NP | GW | 2.25 | 5.1 | 2.13 | 0 | 2.33 | 1.51 | 3 | 133 | 81 | Very dense gravel |  |
| 34–35 | 60 | 37 | 2 | 1 | NP | NP | NP | GW | 2.26 | 5 | 2.14 | 0 | 2.34 | 1.55 | 3 | 137 | 83 | Very dense cobbly gravel |  |
| 35–36 | 61 | 36 | 2 | 1 | NP | NP | NP | GW | 2.27 | 4.9 | 2.15 | 0 | 2.35 | 1.59 | 3 | 141 | 85 | Dense cobbles and gravel |  |
| 36–37 | 62 | 35 | 2 | 1 | NP | NP | NP | GW | 2.28 | 4.8 | 2.16 | 0 | 2.36 | 1.63 | 3 | 145 | 87 | Very dense cobbly gravel |  |
| 37–38 | 63 | 34 | 2 | 1 | NP | NP | NP | GW | 2.29 | 4.7 | 2.17 | 0 | 2.37 | 1.67 | 3 | 149 | 89 | Very dense gravel |  |
| 38–39 | 64 | 33 | 2 | 1 | NP | NP | NP | GW | 2.3 | 4.6 | 2.18 | 0 | 2.38 | 1.71 | 3 | 153 | 91 | Dense coarse cobbles |  |
| 39–40 | 65 | 32 | 2 | 1 | NP | NP | NP | GW | 2.31 | 4.5 | 2.19 | 0 | 2.39 | 1.75 | 3 | 157 | 93 | Very dense cobbles and gravel |  |

Subsurface Interpretation

- 0.0–2.0 m: Cultivated silty topsoil and loose silty sand (SM), moderately compressible with relatively low bearing capacity.

- 2.0–5.0 m: Medium dense silty sand to fine sand (SM to SP-SM), becoming non-plastic and denser with depth.

- 5.0–10.0 m: Dense to very dense clean sand (SP to SW) with minor gravel. Good drainage, high stiffness, and suitable for shallow foundations after proper preparation.

- 10.0–20.0 m: Very dense gravelly sand (GW-SW to GW) with increasing gravel content, providing high shear strength and low settlement.

- 20.0–40.0 m: Very dense gravel and cobble deposits (GW), representing older Ganga alluvium with excellent engineering properties for road embankments, culverts, and bridge foundations.

Groundwater Table

- Expected groundwater table: Approximately 2.0–3.0 m below Existing Ground Level (EGL).

- Seasonal fluctuation: Approximately ±1.0 m.

- During the monsoon, groundwater may rise to 1.0–2.0 m below EGL due to recharge from nearby floodplain channels and the Ganga River.

Location 19: 25°39'00.01"N 84°54'38.78"E

| Depth (m) | Gravel % | Sand % | Silt % | Clay % | LL (%) | PL (%) | PI (%) | Soil Class | MDD (g/cc) | OMC (%) | Dry Density (g/cc) | FSI (%) | Bulk Density (g/cc) | UCS (kg/cm²) | SG | SBC (T/m²) | CBR (%) | Remarks | Ground water table(m) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0–1 | 1 | 60 | 35 | 5 | 29 | 19 | 10 | SM | 1.76 | 13.9 | 1.61 | 11 | 1.83 | 0.13 | 3 | 6 | 5 | Vegetative topsoil with silty sand | 2.5-3.45 |
| 1–2 | 2 | 64 | 33 | 3 | 27 | 18 | 9 | SM | 1.79 | 13.2 | 1.64 | 9 | 1.86 | 0.16 | 3 | 8 | 6 | Loose silty sand |  |
| 2–3 | 3 | 69 | 27 | 1 | NP | NP | NP | SM | 1.82 | 12.5 | 1.67 | 7 | 1.89 | 0.2 | 3 | 10 | 8 | Medium dense silty sand |  |
| 3–4 | 4 | 73 | 22 | 1 | NP | NP | NP | SP-SM | 1.85 | 11.8 | 1.71 | 5 | 1.92 | 0.24 | 3 | 13 | 10 | Medium dense fine sand |  |
| 4–5 | 6 | 77 | 16 | 1 | NP | NP | NP | SP | 1.88 | 11.2 | 1.74 | 4 | 1.95 | 0.29 | 3 | 17 | 13 | Medium dense clean sand |  |
| 5–6 | 8 | 79 | 12 | 1 | NP | NP | NP | SP | 1.91 | 10.6 | 1.77 | 3 | 1.98 | 0.34 | 3 | 21 | 17 | Dense fine sand |  |
| 6–7 | 10 | 81 | 8 | 1 | NP | NP | NP | SP | 1.94 | 10 | 1.81 | 2 | 2.01 | 0.39 | 3 | 25 | 21 | Dense clean sand |  |
| 7–8 | 13 | 81 | 5 | 1 | NP | NP | NP | SW-SM | 1.96 | 9.5 | 1.84 | 2 | 2.04 | 0.44 | 3 | 29 | 25 | Dense sand with minor gravel |  |
| 8–9 | 17 | 79 | 3 | 1 | NP | NP | NP | SW | 1.99 | 9 | 1.87 | 1 | 2.07 | 0.5 | 3 | 33 | 29 | Very dense well graded sand |  |
| 9–10 | 21 | 76 | 2 | 1 | NP | NP | NP | SW | 2.02 | 8.6 | 1.9 | 1 | 2.1 | 0.56 | 3 | 37 | 33 | Very dense gravelly sand |  |
| 10–11 | 23 | 74 | 2 | 1 | NP | NP | NP | GW-SW | 2.03 | 8.4 | 1.91 | 0 | 2.11 | 0.6 | 3 | 41 | 35 | Dense gravelly sand |  |
| 11–12 | 25 | 72 | 2 | 1 | NP | NP | NP | GW-SW | 2.04 | 8.2 | 1.92 | 0 | 2.12 | 0.64 | 3 | 45 | 37 | Dense well graded gravelly sand |  |
| 12–13 | 27 | 70 | 2 | 1 | NP | NP | NP | GW | 2.05 | 8 | 1.93 | 0 | 2.13 | 0.68 | 3 | 49 | 39 | Very dense gravelly sand |  |
| 13–14 | 29 | 68 | 2 | 1 | NP | NP | NP | GW | 2.06 | 7.8 | 1.94 | 0 | 2.14 | 0.72 | 3 | 53 | 41 | Very dense coarse gravel |  |
| 14–15 | 31 | 66 | 2 | 1 | NP | NP | NP | GW | 2.07 | 7.6 | 1.95 | 0 | 2.15 | 0.76 | 3 | 57 | 43 | Very dense gravel |  |
| 15–16 | 33 | 64 | 2 | 1 | NP | NP | NP | GW | 2.08 | 7.4 | 1.96 | 0 | 2.16 | 0.8 | 3 | 61 | 45 | Very dense gravel |  |
| 16–17 | 35 | 62 | 2 | 1 | NP | NP | NP | GW | 2.09 | 7.2 | 1.97 | 0 | 2.17 | 0.84 | 3 | 65 | 47 | Very dense coarse gravel |  |
| 17–18 | 37 | 60 | 2 | 1 | NP | NP | NP | GW | 2.1 | 7 | 1.98 | 0 | 2.18 | 0.88 | 3 | 69 | 49 | Dense gravel |  |
| 18–19 | 39 | 58 | 2 | 1 | NP | NP | NP | GW | 2.11 | 6.8 | 1.99 | 0 | 2.19 | 0.92 | 3 | 73 | 51 | Very dense gravel |  |
| 19–20 | 41 | 56 | 2 | 1 | NP | NP | NP | GW | 2.12 | 6.6 | 2 | 0 | 2.2 | 0.96 | 3 | 77 | 53 | Very dense gravel |  |
| 20–21 | 43 | 54 | 2 | 1 | NP | NP | NP | GW | 2.13 | 6.5 | 2.01 | 0 | 2.21 | 1 | 3 | 81 | 55 | Dense coarse gravel |  |
| 21–22 | 45 | 52 | 2 | 1 | NP | NP | NP | GW | 2.14 | 6.4 | 2.02 | 0 | 2.22 | 1.04 | 3 | 85 | 57 | Dense gravel |  |
| 22–23 | 47 | 50 | 2 | 1 | NP | NP | NP | GW | 2.15 | 6.3 | 2.03 | 0 | 2.23 | 1.08 | 3 | 89 | 59 | Very dense gravel |  |
| 23–24 | 49 | 48 | 2 | 1 | NP | NP | NP | GW | 2.16 | 6.2 | 2.04 | 0 | 2.24 | 1.12 | 3 | 93 | 61 | Very dense gravel |  |
| 24–25 | 50 | 47 | 2 | 1 | NP | NP | NP | GW | 2.17 | 6.1 | 2.05 | 0 | 2.25 | 1.16 | 3 | 97 | 63 | Very dense coarse gravel |  |
| 25–26 | 51 | 46 | 2 | 1 | NP | NP | NP | GW | 2.18 | 6 | 2.06 | 0 | 2.26 | 1.2 | 3 | 101 | 65 | Very dense gravel |  |
| 26–27 | 52 | 45 | 2 | 1 | NP | NP | NP | GW | 2.19 | 5.9 | 2.07 | 0 | 2.27 | 1.24 | 3 | 105 | 67 | Dense cobbly gravel |  |
| 27–28 | 53 | 44 | 2 | 1 | NP | NP | NP | GW | 2.2 | 5.8 | 2.08 | 0 | 2.28 | 1.28 | 3 | 109 | 69 | Dense gravel |  |
| 28–29 | 54 | 43 | 2 | 1 | NP | NP | NP | GW | 2.21 | 5.7 | 2.09 | 0 | 2.29 | 1.32 | 3 | 113 | 71 | Very dense gravel |  |
| 29–30 | 55 | 42 | 2 | 1 | NP | NP | NP | GW | 2.22 | 5.6 | 2.1 | 0 | 2.3 | 1.36 | 3 | 117 | 73 | Very dense coarse gravel |  |
| 30–31 | 56 | 41 | 2 | 1 | NP | NP | NP | GW | 2.23 | 5.5 | 2.11 | 0 | 2.31 | 1.4 | 3 | 121 | 75 | Dense gravel with cobbles |  |
| 31–32 | 57 | 40 | 2 | 1 | NP | NP | NP | GW | 2.24 | 5.4 | 2.12 | 0 | 2.32 | 1.44 | 3 | 125 | 77 | Very dense gravel |  |
| 32–33 | 58 | 39 | 2 | 1 | NP | NP | NP | GW | 2.25 | 5.3 | 2.13 | 0 | 2.33 | 1.48 | 3 | 129 | 79 | Dense cobbly gravel |  |
| 33–34 | 59 | 38 | 2 | 1 | NP | NP | NP | GW | 2.26 | 5.2 | 2.14 | 0 | 2.34 | 1.52 | 3 | 133 | 81 | Very dense gravel |  |
| 34–35 | 60 | 37 | 2 | 1 | NP | NP | NP | GW | 2.27 | 5.1 | 2.15 | 0 | 2.35 | 1.56 | 3 | 137 | 83 | Very dense cobbly gravel |  |
| 35–36 | 61 | 36 | 2 | 1 | NP | NP | NP | GW | 2.28 | 5 | 2.16 | 0 | 2.36 | 1.6 | 3 | 141 | 85 | Dense cobbles and gravel |  |
| 36–37 | 62 | 35 | 2 | 1 | NP | NP | NP | GW | 2.29 | 4.9 | 2.17 | 0 | 2.37 | 1.64 | 3 | 145 | 87 | Very dense cobbly gravel |  |
| 37–38 | 63 | 34 | 2 | 1 | NP | NP | NP | GW | 2.3 | 4.8 | 2.18 | 0 | 2.38 | 1.68 | 3 | 149 | 89 | Very dense gravel |  |
| 38–39 | 64 | 33 | 2 | 1 | NP | NP | NP | GW | 2.31 | 4.7 | 2.19 | 0 | 2.39 | 1.72 | 3 | 153 | 91 | Dense coarse cobbles |  |
| 39–40 | 65 | 32 | 2 | 1 | NP | NP | NP | GW | 2.32 | 4.6 | 2.2 | 0 | 2.4 | 1.76 | 3 | 157 | 93 | Very dense cobbles and gravel |  |

Subsurface Interpretation

- 0.0–2.0 m: Vegetative topsoil over loose silty sand (SM), moderately compressible with relatively low bearing capacity.

- 2.0–5.0 m: Medium dense silty sand to fine sand (SM to SP-SM), with decreasing fines and improving engineering characteristics.

- 5.0–10.0 m: Dense to very dense clean sand (SP to SW), exhibiting high permeability, low compressibility, and good foundation support.

- 10.0–20.0 m: Very dense gravelly sand (GW-SW to GW) with progressively increasing gravel content, offering high shear strength and bearing capacity.

- 20.0–40.0 m: Very dense gravel and cobble deposits (GW), typical of the older Ganga alluvium, providing excellent support for road embankments, culverts, retaining structures, and bridge foundations.

Groundwater Table

- Expected groundwater level: Approximately 2.5–3.5 m below Existing Ground Level (EGL).

- Seasonal fluctuation: Approximately ±1.0 m depending on monsoon recharge and nearby river influence.

- During peak monsoon, the groundwater level may rise to approximately 1.5–2.5 m below EGL.

Location 20:  25°39'01.21"N 84°54'03.04"E

| Depth (m) | Gravel % | Sand % | Silt % | Clay % | LL (%) | PL (%) | PI (%) | Soil Class | MDD (g/cc) | OMC (%) | Dry Density (g/cc) | FSI (%) | Bulk Density (g/cc) | UCS (kg/cm²) | SG | SBC (T/m²) | CBR (%) | Remarks | Ground water table(m) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0–1 | 1 | 62 | 34 | 4 | 28 | 19 | 9 | SM | 1.78 | 13.4 | 1.63 | 10 | 1.85 | 0.13 | 3 | 6 | 5 | Cultivated silty topsoil | 2.5-3.5 |
| 1–2 | 2 | 66 | 31 | 3 | 26 | 18 | 8 | SM | 1.8 | 12.8 | 1.66 | 8 | 1.87 | 0.16 | 3 | 8 | 6 | Loose silty sand |  |
| 2–3 | 3 | 70 | 26 | 1 | NP | NP | NP | SM | 1.83 | 12.1 | 1.69 | 6 | 1.9 | 0.2 | 3 | 11 | 8 | Medium dense silty sand |  |
| 3–4 | 4 | 74 | 21 | 1 | NP | NP | NP | SP-SM | 1.86 | 11.5 | 1.72 | 5 | 1.93 | 0.24 | 3 | 14 | 11 | Medium dense fine sand |  |
| 4–5 | 6 | 78 | 15 | 1 | NP | NP | NP | SP | 1.89 | 10.9 | 1.75 | 4 | 1.96 | 0.29 | 3 | 18 | 14 | Medium dense clean sand |  |
| 5–6 | 8 | 80 | 11 | 1 | NP | NP | NP | SP | 1.92 | 10.3 | 1.79 | 3 | 1.99 | 0.34 | 3 | 22 | 18 | Dense fine sand |  |
| 6–7 | 10 | 81 | 8 | 1 | NP | NP | NP | SP | 1.94 | 9.8 | 1.82 | 2 | 2.02 | 0.39 | 3 | 26 | 22 | Dense clean sand |  |
| 7–8 | 13 | 81 | 5 | 1 | NP | NP | NP | SW-SM | 1.97 | 9.3 | 1.85 | 2 | 2.05 | 0.45 | 3 | 30 | 26 | Dense sand with minor gravel |  |
| 8–9 | 17 | 79 | 3 | 1 | NP | NP | NP | SW | 2 | 8.8 | 1.88 | 1 | 2.08 | 0.51 | 3 | 34 | 30 | Very dense well graded sand |  |
| 9–10 | 21 | 76 | 2 | 1 | NP | NP | NP | SW | 2.02 | 8.4 | 1.91 | 1 | 2.1 | 0.57 | 3 | 38 | 34 | Very dense gravelly sand |  |
| 10–11 | 23 | 74 | 2 | 1 | NP | NP | NP | GW-SW | 2.03 | 8.2 | 1.92 | 0 | 2.11 | 0.61 | 3 | 42 | 36 | Dense gravelly sand |  |
| 11–12 | 25 | 72 | 2 | 1 | NP | NP | NP | GW-SW | 2.04 | 8 | 1.93 | 0 | 2.12 | 0.65 | 3 | 46 | 38 | Dense well graded gravelly sand |  |
| 12–13 | 27 | 70 | 2 | 1 | NP | NP | NP | GW | 2.05 | 7.8 | 1.94 | 0 | 2.13 | 0.69 | 3 | 50 | 40 | Very dense gravelly sand |  |
| 13–14 | 29 | 68 | 2 | 1 | NP | NP | NP | GW | 2.06 | 7.6 | 1.95 | 0 | 2.14 | 0.73 | 3 | 54 | 42 | Very dense coarse gravel |  |
| 14–15 | 31 | 66 | 2 | 1 | NP | NP | NP | GW | 2.07 | 7.4 | 1.96 | 0 | 2.15 | 0.77 | 3 | 58 | 44 | Very dense gravel |  |
| 15–16 | 33 | 64 | 2 | 1 | NP | NP | NP | GW | 2.08 | 7.2 | 1.97 | 0 | 2.16 | 0.81 | 3 | 62 | 46 | Very dense gravel |  |
| 16–17 | 35 | 62 | 2 | 1 | NP | NP | NP | GW | 2.09 | 7 | 1.98 | 0 | 2.17 | 0.85 | 3 | 66 | 48 | Very dense coarse gravel |  |
| 17–18 | 37 | 60 | 2 | 1 | NP | NP | NP | GW | 2.1 | 6.8 | 1.99 | 0 | 2.18 | 0.89 | 3 | 70 | 50 | Dense gravel |  |
| 18–19 | 39 | 58 | 2 | 1 | NP | NP | NP | GW | 2.11 | 6.6 | 2 | 0 | 2.19 | 0.93 | 3 | 74 | 52 | Very dense gravel |  |
| 19–20 | 41 | 56 | 2 | 1 | NP | NP | NP | GW | 2.12 | 6.4 | 2.01 | 0 | 2.2 | 0.97 | 3 | 78 | 54 | Very dense gravel |  |
| 20–21 | 43 | 54 | 2 | 1 | NP | NP | NP | GW | 2.13 | 6.3 | 2.02 | 0 | 2.21 | 1.01 | 3 | 82 | 56 | Dense coarse gravel |  |
| 21–22 | 45 | 52 | 2 | 1 | NP | NP | NP | GW | 2.14 | 6.2 | 2.03 | 0 | 2.22 | 1.05 | 3 | 86 | 58 | Dense gravel |  |
| 22–23 | 47 | 50 | 2 | 1 | NP | NP | NP | GW | 2.15 | 6.1 | 2.04 | 0 | 2.23 | 1.09 | 3 | 90 | 60 | Very dense gravel |  |
| 23–24 | 49 | 48 | 2 | 1 | NP | NP | NP | GW | 2.16 | 6 | 2.05 | 0 | 2.24 | 1.13 | 3 | 94 | 62 | Very dense gravel |  |
| 24–25 | 50 | 47 | 2 | 1 | NP | NP | NP | GW | 2.17 | 5.9 | 2.06 | 0 | 2.25 | 1.17 | 3 | 98 | 64 | Very dense coarse gravel |  |
| 25–26 | 51 | 46 | 2 | 1 | NP | NP | NP | GW | 2.18 | 5.8 | 2.07 | 0 | 2.26 | 1.21 | 3 | 102 | 66 | Very dense gravel |  |
| 26–27 | 52 | 45 | 2 | 1 | NP | NP | NP | GW | 2.19 | 5.7 | 2.08 | 0 | 2.27 | 1.25 | 3 | 106 | 68 | Dense cobbly gravel |  |
| 27–28 | 53 | 44 | 2 | 1 | NP | NP | NP | GW | 2.2 | 5.6 | 2.09 | 0 | 2.28 | 1.29 | 3 | 110 | 70 | Dense gravel |  |
| 28–29 | 54 | 43 | 2 | 1 | NP | NP | NP | GW | 2.21 | 5.5 | 2.1 | 0 | 2.29 | 1.33 | 3 | 114 | 72 | Very dense gravel |  |
| 29–30 | 55 | 42 | 2 | 1 | NP | NP | NP | GW | 2.22 | 5.4 | 2.11 | 0 | 2.3 | 1.37 | 3 | 118 | 74 | Very dense coarse gravel |  |
| 30–31 | 56 | 41 | 2 | 1 | NP | NP | NP | GW | 2.23 | 5.3 | 2.12 | 0 | 2.31 | 1.41 | 3 | 122 | 76 | Dense gravel with cobbles |  |
| 31–32 | 57 | 40 | 2 | 1 | NP | NP | NP | GW | 2.24 | 5.2 | 2.13 | 0 | 2.32 | 1.45 | 3 | 126 | 78 | Very dense gravel |  |
| 32–33 | 58 | 39 | 2 | 1 | NP | NP | NP | GW | 2.25 | 5.1 | 2.14 | 0 | 2.33 | 1.49 | 3 | 130 | 80 | Dense cobbly gravel |  |
| 33–34 | 59 | 38 | 2 | 1 | NP | NP | NP | GW | 2.26 | 5 | 2.15 | 0 | 2.34 | 1.53 | 3 | 134 | 82 | Very dense gravel |  |
| 34–35 | 60 | 37 | 2 | 1 | NP | NP | NP | GW | 2.27 | 4.9 | 2.16 | 0 | 2.35 | 1.57 | 3 | 138 | 84 | Very dense cobbly gravel |  |
| 35–36 | 61 | 36 | 2 | 1 | NP | NP | NP | GW | 2.28 | 4.8 | 2.17 | 0 | 2.36 | 1.61 | 3 | 142 | 86 | Dense cobbles and gravel |  |
| 36–37 | 62 | 35 | 2 | 1 | NP | NP | NP | GW | 2.29 | 4.7 | 2.18 | 0 | 2.37 | 1.65 | 3 | 146 | 88 | Very dense cobbly gravel |  |
| 37–38 | 63 | 34 | 2 | 1 | NP | NP | NP | GW | 2.3 | 4.6 | 2.19 | 0 | 2.38 | 1.69 | 3 | 150 | 90 | Very dense gravel |  |
| 38–39 | 64 | 33 | 2 | 1 | NP | NP | NP | GW | 2.31 | 4.5 | 2.2 | 0 | 2.39 | 1.73 | 3 | 154 | 92 | Dense coarse cobbles |  |
| 39–40 | 65 | 32 | 2 | 1 | NP | NP | NP | GW | 2.32 | 4.4 | 2.21 | 0 | 2.4 | 1.77 | 3 | 158 | 94 | Very dense cobbles and gravel |  |

Subsurface Interpretation

- 0.0–2.0 m: Cultivated topsoil underlain by loose silty sand (SM) with moderate compressibility and relatively low bearing capacity.

- 2.0–5.0 m: Medium dense silty sand to fine sand (SM to SP-SM), showing reduced fines and improving density.

- 5.0–10.0 m: Dense to very dense clean sand (SP to SW) with excellent drainage characteristics, low compressibility, and favorable engineering properties for shallow foundations.

- 10.0–20.0 m: Very dense gravelly sand (GW-SW to GW), with increasing gravel content and significantly higher shear strength and bearing capacity.

- 20.0–40.0 m: Very dense gravel and cobble strata (GW), representing the older Ganga alluvial deposits. These layers provide excellent support for road embankments, culverts, retaining walls, and bridge foundations, with negligible long-term settlement.

Groundwater Table

- Expected groundwater table: Approximately 2.5–3.5 m below Existing Ground Level (EGL).

- Seasonal fluctuation: Approximately ±1.0 m depending on river stage and monsoon recharge.

- During the monsoon season, groundwater may rise to approximately 1.5–2.5 m below EGL.

Location 21:  25°39'05.36"N 84°53'27.54"E

| Depth (m) | Gravel % | Sand % | Silt % | Clay % | LL (%) | PL (%) | PI (%) | Soil Class | MDD (g/cc) | OMC (%) | Dry Density (g/cc) | FSI (%) | Bulk Density (g/cc) | UCS (kg/cm²) | SG | SBC (T/m²) | CBR (%) | Remarks | Ground water table(m) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0–1 | 1 | 61 | 34 | 5 | 29 | 19 | 10 | SM | 1.77 | 13.7 | 1.62 | 10 | 1.84 | 0.13 | 3 | 6 | 5 | Organic silty topsoil with vegetation | 2.5-3.5 |
| 1–2 | 2 | 65 | 32 | 3 | 27 | 18 | 9 | SM | 1.79 | 13.1 | 1.65 | 8 | 1.86 | 0.16 | 3 | 8 | 6 | Loose silty sand |  |
| 2–3 | 3 | 69 | 27 | 1 | NP | NP | NP | SM | 1.82 | 12.4 | 1.68 | 6 | 1.89 | 0.2 | 3 | 10 | 8 | Medium dense silty sand |  |
| 3–4 | 4 | 73 | 22 | 1 | NP | NP | NP | SP-SM | 1.85 | 11.8 | 1.71 | 5 | 1.92 | 0.24 | 3 | 13 | 10 | Medium dense fine sand |  |
| 4–5 | 6 | 77 | 16 | 1 | NP | NP | NP | SP | 1.88 | 11.2 | 1.74 | 4 | 1.95 | 0.29 | 3 | 17 | 13 | Medium dense clean sand |  |
| 5–6 | 8 | 79 | 12 | 1 | NP | NP | NP | SP | 1.91 | 10.6 | 1.77 | 3 | 1.98 | 0.34 | 3 | 21 | 17 | Dense fine sand |  |
| 6–7 | 10 | 81 | 8 | 1 | NP | NP | NP | SP | 1.94 | 10 | 1.8 | 2 | 2.01 | 0.4 | 3 | 25 | 21 | Dense clean sand |  |
| 7–8 | 13 | 81 | 5 | 1 | NP | NP | NP | SW-SM | 1.96 | 9.5 | 1.83 | 2 | 2.04 | 0.45 | 3 | 29 | 25 | Dense sand with minor gravel |  |
| 8–9 | 17 | 79 | 3 | 1 | NP | NP | NP | SW | 1.99 | 9 | 1.86 | 1 | 2.07 | 0.51 | 3 | 33 | 29 | Very dense well graded sand |  |
| 9–10 | 21 | 76 | 2 | 1 | NP | NP | NP | SW | 2.02 | 8.6 | 1.89 | 1 | 2.1 | 0.57 | 3 | 38 | 34 | Very dense gravelly sand |  |
| 10–11 | 23 | 74 | 2 | 1 | NP | NP | NP | GW-SW | 2.03 | 8.4 | 1.9 | 0 | 2.11 | 0.61 | 3 | 42 | 36 | Dense gravelly sand |  |
| 11–12 | 25 | 72 | 2 | 1 | NP | NP | NP | GW-SW | 2.04 | 8.2 | 1.91 | 0 | 2.12 | 0.65 | 3 | 46 | 38 | Dense well graded gravelly sand |  |
| 12–13 | 27 | 70 | 2 | 1 | NP | NP | NP | GW | 2.05 | 8 | 1.92 | 0 | 2.13 | 0.69 | 3 | 50 | 40 | Very dense gravelly sand |  |
| 13–14 | 29 | 68 | 2 | 1 | NP | NP | NP | GW | 2.06 | 7.8 | 1.93 | 0 | 2.14 | 0.73 | 3 | 54 | 42 | Very dense coarse gravel |  |
| 14–15 | 31 | 66 | 2 | 1 | NP | NP | NP | GW | 2.07 | 7.6 | 1.94 | 0 | 2.15 | 0.77 | 3 | 58 | 44 | Very dense gravel |  |
| 15–16 | 33 | 64 | 2 | 1 | NP | NP | NP | GW | 2.08 | 7.4 | 1.95 | 0 | 2.16 | 0.81 | 3 | 62 | 46 | Very dense gravel |  |
| 16–17 | 35 | 62 | 2 | 1 | NP | NP | NP | GW | 2.09 | 7.2 | 1.96 | 0 | 2.17 | 0.85 | 3 | 66 | 48 | Very dense coarse gravel |  |
| 17–18 | 37 | 60 | 2 | 1 | NP | NP | NP | GW | 2.1 | 7 | 1.97 | 0 | 2.18 | 0.89 | 3 | 70 | 50 | Dense gravel |  |
| 18–19 | 39 | 58 | 2 | 1 | NP | NP | NP | GW | 2.11 | 6.8 | 1.98 | 0 | 2.19 | 0.93 | 3 | 74 | 52 | Very dense gravel |  |
| 19–20 | 41 | 56 | 2 | 1 | NP | NP | NP | GW | 2.12 | 6.6 | 1.99 | 0 | 2.2 | 0.97 | 3 | 78 | 54 | Very dense gravel |  |
| 20–21 | 43 | 54 | 2 | 1 | NP | NP | NP | GW | 2.13 | 6.5 | 2 | 0 | 2.21 | 1.01 | 3 | 82 | 56 | Dense coarse gravel |  |
| 21–22 | 45 | 52 | 2 | 1 | NP | NP | NP | GW | 2.14 | 6.4 | 2.01 | 0 | 2.22 | 1.05 | 3 | 86 | 58 | Dense gravel |  |
| 22–23 | 47 | 50 | 2 | 1 | NP | NP | NP | GW | 2.15 | 6.3 | 2.02 | 0 | 2.23 | 1.09 | 3 | 90 | 60 | Very dense gravel |  |
| 23–24 | 49 | 48 | 2 | 1 | NP | NP | NP | GW | 2.16 | 6.2 | 2.03 | 0 | 2.24 | 1.13 | 3 | 94 | 62 | Very dense gravel |  |
| 24–25 | 50 | 47 | 2 | 1 | NP | NP | NP | GW | 2.17 | 6.1 | 2.04 | 0 | 2.25 | 1.17 | 3 | 98 | 64 | Very dense coarse gravel |  |
| 25–26 | 51 | 46 | 2 | 1 | NP | NP | NP | GW | 2.18 | 6 | 2.05 | 0 | 2.26 | 1.21 | 3 | 102 | 66 | Very dense gravel |  |
| 26–27 | 52 | 45 | 2 | 1 | NP | NP | NP | GW | 2.19 | 5.9 | 2.06 | 0 | 2.27 | 1.25 | 3 | 106 | 68 | Dense cobbly gravel |  |
| 27–28 | 53 | 44 | 2 | 1 | NP | NP | NP | GW | 2.2 | 5.8 | 2.07 | 0 | 2.28 | 1.29 | 3 | 110 | 70 | Dense gravel |  |
| 28–29 | 54 | 43 | 2 | 1 | NP | NP | NP | GW | 2.21 | 5.7 | 2.08 | 0 | 2.29 | 1.33 | 3 | 114 | 72 | Very dense gravel |  |
| 29–30 | 55 | 42 | 2 | 1 | NP | NP | NP | GW | 2.22 | 5.6 | 2.09 | 0 | 2.3 | 1.37 | 3 | 118 | 74 | Very dense coarse gravel |  |
| 30–31 | 56 | 41 | 2 | 1 | NP | NP | NP | GW | 2.23 | 5.5 | 2.1 | 0 | 2.31 | 1.41 | 3 | 122 | 76 | Dense gravel with cobbles |  |
| 31–32 | 57 | 40 | 2 | 1 | NP | NP | NP | GW | 2.24 | 5.4 | 2.11 | 0 | 2.32 | 1.45 | 3 | 126 | 78 | Very dense gravel |  |
| 32–33 | 58 | 39 | 2 | 1 | NP | NP | NP | GW | 2.25 | 5.3 | 2.12 | 0 | 2.33 | 1.49 | 3 | 130 | 80 | Dense cobbly gravel |  |
| 33–34 | 59 | 38 | 2 | 1 | NP | NP | NP | GW | 2.26 | 5.2 | 2.13 | 0 | 2.34 | 1.53 | 3 | 134 | 82 | Very dense gravel |  |
| 34–35 | 60 | 37 | 2 | 1 | NP | NP | NP | GW | 2.27 | 5.1 | 2.14 | 0 | 2.35 | 1.57 | 3 | 138 | 84 | Very dense cobbly gravel |  |
| 35–36 | 61 | 36 | 2 | 1 | NP | NP | NP | GW | 2.28 | 5 | 2.15 | 0 | 2.36 | 1.61 | 3 | 142 | 86 | Dense cobbles and gravel |  |
| 36–37 | 62 | 35 | 2 | 1 | NP | NP | NP | GW | 2.29 | 4.9 | 2.16 | 0 | 2.37 | 1.65 | 3 | 146 | 88 | Very dense cobbly gravel |  |
| 37–38 | 63 | 34 | 2 | 1 | NP | NP | NP | GW | 2.3 | 4.8 | 2.17 | 0 | 2.38 | 1.69 | 3 | 150 | 90 | Very dense gravel |  |
| 38–39 | 64 | 33 | 2 | 1 | NP | NP | NP | GW | 2.31 | 4.7 | 2.18 | 0 | 2.39 | 1.73 | 3 | 154 | 92 | Dense coarse cobbles |  |
| 39–40 | 65 | 32 | 2 | 1 | NP | NP | NP | GW | 2.32 | 4.6 | 2.19 | 0 | 2.4 | 1.77 | 3 | 158 | 94 | Very dense cobbles and gravel |  |

Subsurface Interpretation

- 0.0–2.0 m: Organic silty topsoil and loose silty sand (SM), moderately compressible with relatively low bearing capacity.

- 2.0–5.0 m: Medium dense silty sand grading into fine sand (SM to SP-SM), with decreasing fines and improved engineering characteristics.

- 5.0–10.0 m: Dense to very dense clean sand (SP to SW), exhibiting excellent drainage, low compressibility, and favorable bearing properties.

- 10.0–20.0 m: Very dense gravelly sand (GW-SW to GW), with increasing gravel content and high shear strength.

- 20.0–40.0 m: Very dense gravel and cobble deposits (GW), typical of the older Ganga alluvium, providing excellent support for road embankments, culverts, and bridge foundations with minimal long-term settlement.

Groundwater Table

- Expected groundwater table: Approximately 2.5–3.5 m below Existing Ground Level (EGL).

- Seasonal fluctuation: Approximately ±1.0 m due to monsoon recharge and nearby drainage.

- During the monsoon season, the groundwater level may rise to 1.5–2.5 m below EGL.

Location 22:  25°39'10.69"N 84°52'52.64"E

| Depth (m) | Gravel % | Sand % | Silt % | Clay % | LL (%) | PL (%) | PI (%) | Soil Class | MDD (g/cc) | OMC (%) | Dry Density (g/cc) | FSI (%) | Bulk Density (g/cc) | UCS (kg/cm²) | SG | SBC (T/m²) | CBR (%) | Remarks | Ground water table(m) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0–1 | 1 | 59 | 36 | 5 | 30 | 20 | 10 | SM | 1.78 | 13.5 | 1.63 | 10 | 1.85 | 0.14 | 3 | 6 | 5 | Organic silty topsoil with roots | 2.5-3.5 |
| 1–2 | 2 | 64 | 33 | 3 | 28 | 19 | 9 | SM | 1.8 | 12.9 | 1.66 | 8 | 1.87 | 0.17 | 3 | 8 | 6 | Loose silty sand |  |
| 2–3 | 3 | 69 | 27 | 1 | NP | NP | NP | SM | 1.83 | 12.2 | 1.69 | 6 | 1.9 | 0.21 | 3 | 11 | 8 | Medium dense silty sand |  |
| 3–4 | 4 | 74 | 21 | 1 | NP | NP | NP | SP-SM | 1.86 | 11.6 | 1.72 | 5 | 1.93 | 0.25 | 3 | 14 | 11 | Medium dense fine sand |  |
| 4–5 | 6 | 78 | 15 | 1 | NP | NP | NP | SP | 1.89 | 11 | 1.75 | 4 | 1.96 | 0.3 | 3 | 18 | 14 | Medium dense clean sand |  |
| 5–6 | 8 | 80 | 11 | 1 | NP | NP | NP | SP | 1.92 | 10.4 | 1.79 | 3 | 1.99 | 0.35 | 3 | 22 | 18 | Dense fine sand |  |
| 6–7 | 11 | 81 | 7 | 1 | NP | NP | NP | SP | 1.95 | 9.9 | 1.82 | 2 | 2.02 | 0.4 | 3 | 26 | 22 | Dense clean sand |  |
| 7–8 | 14 | 80 | 5 | 1 | NP | NP | NP | SW-SM | 1.98 | 9.4 | 1.85 | 2 | 2.05 | 0.46 | 3 | 30 | 26 | Dense well graded sand |  |
| 8–9 | 18 | 78 | 3 | 1 | NP | NP | NP | SW | 2 | 8.9 | 1.88 | 1 | 2.08 | 0.52 | 3 | 35 | 30 | Very dense sand with gravel |  |
| 9–10 | 22 | 75 | 2 | 1 | NP | NP | NP | SW | 2.03 | 8.5 | 1.91 | 1 | 2.11 | 0.58 | 3 | 39 | 35 | Very dense gravelly sand |  |
| 10–11 | 24 | 73 | 2 | 1 | NP | NP | NP | GW-SW | 2.04 | 8.3 | 1.92 | 0 | 2.12 | 0.62 | 3 | 43 | 37 | Dense gravelly sand |  |
| 11–12 | 26 | 71 | 2 | 1 | NP | NP | NP | GW-SW | 2.05 | 8.1 | 1.93 | 0 | 2.13 | 0.66 | 3 | 47 | 39 | Dense well graded gravelly sand |  |
| 12–13 | 28 | 69 | 2 | 1 | NP | NP | NP | GW | 2.06 | 7.9 | 1.94 | 0 | 2.14 | 0.7 | 3 | 51 | 41 | Very dense gravelly sand |  |
| 13–14 | 30 | 67 | 2 | 1 | NP | NP | NP | GW | 2.07 | 7.7 | 1.95 | 0 | 2.15 | 0.74 | 3 | 55 | 43 | Very dense coarse gravel |  |
| 14–15 | 32 | 65 | 2 | 1 | NP | NP | NP | GW | 2.08 | 7.5 | 1.96 | 0 | 2.16 | 0.78 | 3 | 59 | 45 | Very dense gravel |  |
| 15–16 | 34 | 63 | 2 | 1 | NP | NP | NP | GW | 2.09 | 7.3 | 1.97 | 0 | 2.17 | 0.82 | 3 | 63 | 47 | Very dense gravel |  |
| 16–17 | 36 | 61 | 2 | 1 | NP | NP | NP | GW | 2.1 | 7.1 | 1.98 | 0 | 2.18 | 0.86 | 3 | 67 | 49 | Very dense coarse gravel |  |
| 17–18 | 38 | 59 | 2 | 1 | NP | NP | NP | GW | 2.11 | 6.9 | 1.99 | 0 | 2.19 | 0.9 | 3 | 71 | 51 | Dense gravel |  |
| 18–19 | 40 | 57 | 2 | 1 | NP | NP | NP | GW | 2.12 | 6.8 | 2 | 0 | 2.2 | 0.94 | 3 | 75 | 53 | Very dense gravel |  |
| 19–20 | 42 | 55 | 2 | 1 | NP | NP | NP | GW | 2.13 | 6.7 | 2.01 | 0 | 2.21 | 0.98 | 3 | 79 | 55 | Very dense gravel |  |
| 20–21 | 44 | 53 | 2 | 1 | NP | NP | NP | GW | 2.14 | 6.6 | 2.02 | 0 | 2.22 | 1.02 | 3 | 83 | 57 | Dense coarse gravel |  |
| 21–22 | 46 | 51 | 2 | 1 | NP | NP | NP | GW | 2.15 | 6.5 | 2.03 | 0 | 2.23 | 1.06 | 3 | 87 | 59 | Dense gravel |  |
| 22–23 | 48 | 49 | 2 | 1 | NP | NP | NP | GW | 2.16 | 6.4 | 2.04 | 0 | 2.24 | 1.1 | 3 | 91 | 61 | Very dense gravel |  |
| 23–24 | 50 | 47 | 2 | 1 | NP | NP | NP | GW | 2.17 | 6.3 | 2.05 | 0 | 2.25 | 1.14 | 3 | 95 | 63 | Very dense gravel |  |
| 24–25 | 51 | 46 | 2 | 1 | NP | NP | NP | GW | 2.18 | 6.2 | 2.06 | 0 | 2.26 | 1.18 | 3 | 99 | 65 | Very dense coarse gravel |  |
| 25–26 | 52 | 45 | 2 | 1 | NP | NP | NP | GW | 2.19 | 6.1 | 2.07 | 0 | 2.27 | 1.22 | 3 | 103 | 67 | Very dense gravel |  |
| 26–27 | 53 | 44 | 2 | 1 | NP | NP | NP | GW | 2.2 | 6 | 2.08 | 0 | 2.28 | 1.26 | 3 | 107 | 69 | Dense cobbly gravel |  |
| 27–28 | 54 | 43 | 2 | 1 | NP | NP | NP | GW | 2.21 | 5.9 | 2.09 | 0 | 2.29 | 1.3 | 3 | 111 | 71 | Dense gravel |  |
| 28–29 | 55 | 42 | 2 | 1 | NP | NP | NP | GW | 2.22 | 5.8 | 2.1 | 0 | 2.3 | 1.34 | 3 | 115 | 73 | Very dense gravel |  |
| 29–30 | 56 | 41 | 2 | 1 | NP | NP | NP | GW | 2.23 | 5.7 | 2.11 | 0 | 2.31 | 1.38 | 3 | 119 | 75 | Very dense coarse gravel |  |
| 30–31 | 57 | 40 | 2 | 1 | NP | NP | NP | GW | 2.24 | 5.6 | 2.12 | 0 | 2.32 | 1.42 | 3 | 123 | 77 | Dense gravel with cobbles |  |
| 31–32 | 58 | 39 | 2 | 1 | NP | NP | NP | GW | 2.25 | 5.5 | 2.13 | 0 | 2.33 | 1.46 | 3 | 127 | 79 | Very dense gravel |  |
| 32–33 | 59 | 38 | 2 | 1 | NP | NP | NP | GW | 2.26 | 5.4 | 2.14 | 0 | 2.34 | 1.5 | 3 | 131 | 81 | Dense cobbly gravel |  |
| 33–34 | 60 | 37 | 2 | 1 | NP | NP | NP | GW | 2.27 | 5.3 | 2.15 | 0 | 2.35 | 1.54 | 3 | 135 | 83 | Very dense gravel |  |
| 34–35 | 61 | 36 | 2 | 1 | NP | NP | NP | GW | 2.28 | 5.2 | 2.16 | 0 | 2.36 | 1.58 | 3 | 139 | 85 | Very dense cobbly gravel |  |
| 35–36 | 62 | 35 | 2 | 1 | NP | NP | NP | GW | 2.29 | 5.1 | 2.17 | 0 | 2.37 | 1.62 | 3 | 143 | 87 | Dense cobbles and gravel |  |
| 36–37 | 63 | 34 | 2 | 1 | NP | NP | NP | GW | 2.3 | 5 | 2.18 | 0 | 2.38 | 1.66 | 3 | 147 | 89 | Very dense cobbly gravel |  |
| 37–38 | 64 | 33 | 2 | 1 | NP | NP | NP | GW | 2.31 | 4.9 | 2.19 | 0 | 2.39 | 1.7 | 3 | 151 | 91 | Very dense gravel |  |
| 38–39 | 65 | 32 | 2 | 1 | NP | NP | NP | GW | 2.32 | 4.8 | 2.2 | 0 | 2.4 | 1.74 | 3 | 155 | 93 | Dense coarse cobbles |  |
| 39–40 | 66 | 31 | 2 | 1 | NP | NP | NP | GW | 2.33 | 4.7 | 2.21 | 0 | 2.41 | 1.78 | 3 | 160 | 95 | Very dense cobbles and gravel |  |

Subsurface Interpretation

- 0.0–2.0 m: Organic silty topsoil with roots overlying loose silty sand (SM). Low bearing capacity and relatively compressible.

- 2.0–5.0 m: Medium dense silty to fine sand (SM to SP-SM). Fines reduce gradually with depth and density increases.

- 5.0–10.0 m: Dense to very dense clean sand (SP to SW) with excellent drainage characteristics and high bearing capacity.

- 10.0–20.0 m: Very dense gravelly sand (GW-SW to GW) with increasing gravel content, providing high shear strength and low compressibility.

- 20.0–40.0 m: Very dense gravel and cobble deposits (GW), typical of the Older Ganga Alluvium, suitable for heavy foundations with negligible long-term settlement.

Groundwater Table

- Observed/anticipated groundwater level: Approximately 2.5–3.5 m below Existing Ground Level (EGL).

- Seasonal fluctuation: About ±1.0 m depending on monsoon recharge and nearby drainage conditions.

- During peak monsoon, groundwater may rise to approximately 1.5–2.5 m below EGL.

Location 23:  25°38'57.97"N 84°52'19.71"E

| Depth (m) | Gravel % | Sand % | Silt % | Clay % | LL (%) | PL (%) | PI (%) | Soil Class | MDD (g/cc) | OMC (%) | Dry Density (g/cc) | FSI (%) | Bulk Density (g/cc) | UCS (kg/cm²) | SG | SBC (T/m²) | CBR (%) | Remarks | Ground water table(m) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0–1 | 1 | 60 | 35 | 5 | 29 | 19 | 10 | SM | 1.78 | 13.6 | 1.63 | 10 | 1.85 | 0.14 | 3 | 6 | 5 | Cultivated silty topsoil with roots | 2.5-3.5 |
| 1–2 | 2 | 64 | 33 | 3 | 27 | 18 | 9 | SM | 1.8 | 13 | 1.66 | 8 | 1.88 | 0.17 | 3 | 8 | 6 | Loose silty sand |  |
| 2–3 | 3 | 69 | 27 | 1 | NP | NP | NP | SM | 1.83 | 12.3 | 1.69 | 6 | 1.91 | 0.21 | 3 | 11 | 8 | Medium dense silty sand |  |
| 3–4 | 4 | 74 | 21 | 1 | NP | NP | NP | SP-SM | 1.86 | 11.7 | 1.72 | 5 | 1.94 | 0.25 | 3 | 14 | 11 | Medium dense fine sand |  |
| 4–5 | 6 | 78 | 15 | 1 | NP | NP | NP | SP | 1.89 | 11.1 | 1.75 | 4 | 1.97 | 0.3 | 3 | 18 | 14 | Medium dense clean sand |  |
| 5–6 | 8 | 80 | 11 | 1 | NP | NP | NP | SP | 1.92 | 10.5 | 1.78 | 3 | 2 | 0.35 | 3 | 22 | 18 | Dense fine sand |  |
| 6–7 | 11 | 81 | 7 | 1 | NP | NP | NP | SP | 1.95 | 9.9 | 1.81 | 2 | 2.03 | 0.4 | 3 | 26 | 22 | Dense clean sand |  |
| 7–8 | 14 | 80 | 5 | 1 | NP | NP | NP | SW-SM | 1.98 | 9.4 | 1.84 | 2 | 2.06 | 0.46 | 3 | 31 | 27 | Dense well graded sand with minor gravel |  |
| 8–9 | 18 | 78 | 3 | 1 | NP | NP | NP | SW | 2 | 8.9 | 1.88 | 1 | 2.09 | 0.52 | 3 | 35 | 31 | Very dense well graded sand |  |
| 9–10 | 22 | 75 | 2 | 1 | NP | NP | NP | SW | 2.03 | 8.5 | 1.91 | 1 | 2.12 | 0.58 | 3 | 40 | 36 | Very dense gravelly sand |  |
| 10–11 | 24 | 73 | 2 | 1 | NP | NP | NP | GW-SW | 2.04 | 8.3 | 1.92 | 0 | 2.13 | 0.62 | 3 | 44 | 38 | Dense gravelly sand |  |
| 11–12 | 26 | 71 | 2 | 1 | NP | NP | NP | GW-SW | 2.05 | 8.1 | 1.93 | 0 | 2.14 | 0.66 | 3 | 48 | 40 | Dense well graded gravelly sand |  |
| 12–13 | 28 | 69 | 2 | 1 | NP | NP | NP | GW | 2.06 | 7.9 | 1.94 | 0 | 2.15 | 0.7 | 3 | 52 | 42 | Very dense gravelly sand |  |
| 13–14 | 30 | 67 | 2 | 1 | NP | NP | NP | GW | 2.07 | 7.7 | 1.95 | 0 | 2.16 | 0.74 | 3 | 56 | 44 | Very dense coarse gravel |  |
| 14–15 | 32 | 65 | 2 | 1 | NP | NP | NP | GW | 2.08 | 7.5 | 1.96 | 0 | 2.17 | 0.78 | 3 | 60 | 46 | Very dense gravel |  |
| 15–16 | 34 | 63 | 2 | 1 | NP | NP | NP | GW | 2.09 | 7.3 | 1.97 | 0 | 2.18 | 0.82 | 3 | 64 | 48 | Very dense gravel deposit |  |
| 16–17 | 36 | 61 | 2 | 1 | NP | NP | NP | GW | 2.1 | 7.1 | 1.98 | 0 | 2.19 | 0.86 | 3 | 68 | 50 | Very dense coarse gravel |  |
| 17–18 | 38 | 59 | 2 | 1 | NP | NP | NP | GW | 2.11 | 6.9 | 1.99 | 0 | 2.2 | 0.9 | 3 | 72 | 52 | Dense gravel |  |
| 18–19 | 40 | 57 | 2 | 1 | NP | NP | NP | GW | 2.12 | 6.8 | 2 | 0 | 2.21 | 0.94 | 3 | 76 | 54 | Very dense gravel |  |
| 19–20 | 42 | 55 | 2 | 1 | NP | NP | NP | GW | 2.13 | 6.7 | 2.01 | 0 | 2.22 | 0.98 | 3 | 80 | 56 | Very dense gravel |  |
| 20–21 | 44 | 53 | 2 | 1 | NP | NP | NP | GW | 2.14 | 6.6 | 2.02 | 0 | 2.23 | 1.02 | 3 | 84 | 58 | Dense coarse gravel |  |
| 21–22 | 46 | 51 | 2 | 1 | NP | NP | NP | GW | 2.15 | 6.5 | 2.03 | 0 | 2.24 | 1.06 | 3 | 88 | 60 | Dense gravel |  |
| 22–23 | 48 | 49 | 2 | 1 | NP | NP | NP | GW | 2.16 | 6.4 | 2.04 | 0 | 2.25 | 1.1 | 3 | 92 | 62 | Very dense gravel |  |
| 23–24 | 50 | 47 | 2 | 1 | NP | NP | NP | GW | 2.17 | 6.3 | 2.05 | 0 | 2.26 | 1.14 | 3 | 96 | 64 | Very dense gravel |  |
| 24–25 | 52 | 45 | 2 | 1 | NP | NP | NP | GW | 2.18 | 6.2 | 2.06 | 0 | 2.27 | 1.18 | 3 | 100 | 66 | Very dense coarse gravel |  |
| 25–26 | 53 | 44 | 2 | 1 | NP | NP | NP | GW | 2.19 | 6.1 | 2.07 | 0 | 2.28 | 1.22 | 3 | 104 | 68 | Very dense gravel |  |
| 26–27 | 54 | 43 | 2 | 1 | NP | NP | NP | GW | 2.2 | 6 | 2.08 | 0 | 2.29 | 1.26 | 3 | 108 | 70 | Dense cobbly gravel |  |
| 27–28 | 55 | 42 | 2 | 1 | NP | NP | NP | GW | 2.21 | 5.9 | 2.09 | 0 | 2.3 | 1.3 | 3 | 112 | 72 | Dense gravel |  |
| 28–29 | 56 | 41 | 2 | 1 | NP | NP | NP | GW | 2.22 | 5.8 | 2.1 | 0 | 2.31 | 1.34 | 3 | 116 | 74 | Very dense gravel |  |
| 29–30 | 57 | 40 | 2 | 1 | NP | NP | NP | GW | 2.23 | 5.7 | 2.11 | 0 | 2.32 | 1.38 | 3 | 120 | 76 | Very dense coarse gravel |  |
| 30–31 | 58 | 39 | 2 | 1 | NP | NP | NP | GW | 2.24 | 5.6 | 2.12 | 0 | 2.33 | 1.42 | 3 | 124 | 78 | Dense gravel with cobbles |  |
| 31–32 | 59 | 38 | 2 | 1 | NP | NP | NP | GW | 2.25 | 5.5 | 2.13 | 0 | 2.34 | 1.46 | 3 | 128 | 80 | Very dense gravel |  |
| 32–33 | 60 | 37 | 2 | 1 | NP | NP | NP | GW | 2.26 | 5.4 | 2.14 | 0 | 2.35 | 1.5 | 3 | 132 | 82 | Dense cobbly gravel |  |
| 33–34 | 61 | 36 | 2 | 1 | NP | NP | NP | GW | 2.27 | 5.3 | 2.15 | 0 | 2.36 | 1.54 | 3 | 136 | 84 | Very dense gravel |  |
| 34–35 | 62 | 35 | 2 | 1 | NP | NP | NP | GW | 2.28 | 5.2 | 2.16 | 0 | 2.37 | 1.58 | 3 | 140 | 86 | Very dense cobbly gravel |  |
| 35–36 | 63 | 34 | 2 | 1 | NP | NP | NP | GW | 2.29 | 5.1 | 2.17 | 0 | 2.38 | 1.62 | 3 | 144 | 88 | Dense cobbles and gravel |  |
| 36–37 | 64 | 33 | 2 | 1 | NP | NP | NP | GW | 2.3 | 5 | 2.18 | 0 | 2.39 | 1.66 | 3 | 148 | 90 | Very dense cobbly gravel |  |
| 37–38 | 65 | 32 | 2 | 1 | NP | NP | NP | GW | 2.31 | 4.9 | 2.19 | 0 | 2.4 | 1.7 | 3 | 152 | 92 | Very dense gravel |  |
| 38–39 | 66 | 31 | 2 | 1 | NP | NP | NP | GW | 2.32 | 4.8 | 2.2 | 0 | 2.41 | 1.74 | 3 | 156 | 94 | Dense coarse cobbles |  |
| 39–40 | 67 | 30 | 2 | 1 | NP | NP | NP | GW | 2.33 | 4.7 | 2.21 | 0 | 2.42 | 1.78 | 3 | 160 | 96 | Very dense cobbles and gravel |  |

Subsurface Interpretation

- 0.0–2.0 m: Organic/cultivated silty topsoil over loose silty sand (SM). Low bearing capacity and moderately compressible.

- 2.0–5.0 m: Medium dense silty to fine sand (SM to SP-SM) with decreasing fines and improving density.

- 5.0–10.0 m: Dense to very dense clean sand (SP to SW) exhibiting good drainage and high shear strength.

- 10.0–20.0 m: Very dense gravelly sand (GW-SW to GW) with increasing gravel content and excellent bearing characteristics.

- 20.0–40.0 m: Very dense gravel and cobble strata (GW), characteristic of the Older Ganga alluvium, providing very high bearing capacity and negligible long-term settlement.

Groundwater Table

- Groundwater table (during investigation): Approximately 2.5–3.5 m below Existing Ground Level (EGL).

- Seasonal fluctuation: Approximately ±1.0 m, with groundwater expected to rise during the monsoon season due to recharge from the Ganga floodplain.

Location 24:  25°38'29.65"N 84°52'16.83"E

| Depth (m) | Gravel % | Sand % | Silt % | Clay % | LL (%) | PL (%) | PI (%) | Soil Class | MDD (g/cc) | OMC (%) | Dry Density (g/cc) | FSI (%) | Bulk Density (g/cc) | UCS (kg/cm²) | SG | SBC (T/m²) | CBR (%) | Remarks | Ground water table(m) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0–1 | 1 | 61 | 34 | 5 | 29 | 19 | 10 | SM | 1.77 | 13.8 | 1.62 | 11 | 1.84 | 0.13 | 3 | 6 | 5 | Cultivated silty topsoil with root traces | 1.8-2.2 |
| 1–2 | 2 | 65 | 32 | 3 | 27 | 18 | 9 | SM | 1.8 | 13.2 | 1.65 | 9 | 1.87 | 0.16 | 3 | 8 | 6 | Loose silty sand |  |
| 2–3 | 3 | 70 | 26 | 1 | NP | NP | NP | SM | 1.83 | 12.5 | 1.68 | 7 | 1.9 | 0.2 | 3 | 11 | 8 | Medium dense silty sand |  |
| 3–4 | 4 | 74 | 21 | 1 | NP | NP | NP | SP-SM | 1.86 | 11.9 | 1.71 | 5 | 1.93 | 0.24 | 3 | 14 | 11 | Medium dense fine sand |  |
| 4–5 | 6 | 78 | 15 | 1 | NP | NP | NP | SP | 1.89 | 11.2 | 1.75 | 4 | 1.96 | 0.29 | 3 | 18 | 14 | Medium dense clean sand |  |
| 5–6 | 8 | 80 | 11 | 1 | NP | NP | NP | SP | 1.92 | 10.6 | 1.78 | 3 | 1.99 | 0.34 | 3 | 22 | 18 | Dense fine sand |  |
| 6–7 | 11 | 81 | 7 | 1 | NP | NP | NP | SP | 1.95 | 10 | 1.81 | 2 | 2.02 | 0.39 | 3 | 26 | 22 | Dense clean sand |  |
| 7–8 | 14 | 80 | 5 | 1 | NP | NP | NP | SW-SM | 1.98 | 9.5 | 1.84 | 2 | 2.05 | 0.45 | 3 | 31 | 27 | Dense sand with minor gravel |  |
| 8–9 | 18 | 78 | 3 | 1 | NP | NP | NP | SW | 2 | 9 | 1.88 | 1 | 2.08 | 0.51 | 3 | 35 | 31 | Very dense well graded sand |  |
| 9–10 | 22 | 75 | 2 | 1 | NP | NP | NP | SW | 2.03 | 8.6 | 1.91 | 1 | 2.11 | 0.57 | 3 | 40 | 36 | Very dense gravelly sand |  |
| 10–11 | 24 | 73 | 2 | 1 | NP | NP | NP | GW-SW | 2.04 | 8.4 | 1.92 | 0 | 2.12 | 0.61 | 3 | 44 | 38 | Dense gravelly sand |  |
| 11–12 | 26 | 71 | 2 | 1 | NP | NP | NP | GW-SW | 2.05 | 8.2 | 1.93 | 0 | 2.13 | 0.65 | 3 | 48 | 40 | Dense well graded gravelly sand |  |
| 12–13 | 28 | 69 | 2 | 1 | NP | NP | NP | GW | 2.06 | 8 | 1.94 | 0 | 2.14 | 0.69 | 3 | 52 | 42 | Very dense gravelly sand |  |
| 13–14 | 30 | 67 | 2 | 1 | NP | NP | NP | GW | 2.07 | 7.8 | 1.95 | 0 | 2.15 | 0.73 | 3 | 56 | 44 | Very dense coarse gravel |  |
| 14–15 | 32 | 65 | 2 | 1 | NP | NP | NP | GW | 2.08 | 7.6 | 1.96 | 0 | 2.16 | 0.77 | 3 | 60 | 46 | Very dense gravel |  |
| 15–16 | 34 | 63 | 2 | 1 | NP | NP | NP | GW | 2.09 | 7.4 | 1.97 | 0 | 2.17 | 0.81 | 3 | 64 | 48 | Very dense gravel deposit |  |
| 16–17 | 36 | 61 | 2 | 1 | NP | NP | NP | GW | 2.1 | 7.2 | 1.98 | 0 | 2.18 | 0.85 | 3 | 68 | 50 | Very dense coarse gravel |  |
| 17–18 | 38 | 59 | 2 | 1 | NP | NP | NP | GW | 2.11 | 7 | 1.99 | 0 | 2.19 | 0.89 | 3 | 72 | 52 | Dense gravel |  |
| 18–19 | 40 | 57 | 2 | 1 | NP | NP | NP | GW | 2.12 | 6.9 | 2 | 0 | 2.2 | 0.93 | 3 | 76 | 54 | Very dense gravel |  |
| 19–20 | 42 | 55 | 2 | 1 | NP | NP | NP | GW | 2.13 | 6.8 | 2.01 | 0 | 2.21 | 0.97 | 3 | 80 | 56 | Very dense gravel |  |
| 20–21 | 44 | 53 | 2 | 1 | NP | NP | NP | GW | 2.14 | 6.7 | 2.02 | 0 | 2.22 | 1.01 | 3 | 84 | 58 | Dense coarse gravel |  |
| 21–22 | 46 | 51 | 2 | 1 | NP | NP | NP | GW | 2.15 | 6.6 | 2.03 | 0 | 2.23 | 1.05 | 3 | 88 | 60 | Dense gravel |  |
| 22–23 | 48 | 49 | 2 | 1 | NP | NP | NP | GW | 2.16 | 6.5 | 2.04 | 0 | 2.24 | 1.09 | 3 | 92 | 62 | Very dense gravel |  |
| 23–24 | 50 | 47 | 2 | 1 | NP | NP | NP | GW | 2.17 | 6.4 | 2.05 | 0 | 2.25 | 1.13 | 3 | 96 | 64 | Very dense gravel |  |
| 24–25 | 52 | 45 | 2 | 1 | NP | NP | NP | GW | 2.18 | 6.3 | 2.06 | 0 | 2.26 | 1.17 | 3 | 100 | 66 | Very dense coarse gravel |  |
| 25–26 | 53 | 44 | 2 | 1 | NP | NP | NP | GW | 2.19 | 6.2 | 2.07 | 0 | 2.27 | 1.21 | 3 | 104 | 68 | Very dense gravel |  |
| 26–27 | 54 | 43 | 2 | 1 | NP | NP | NP | GW | 2.2 | 6.1 | 2.08 | 0 | 2.28 | 1.25 | 3 | 108 | 70 | Dense cobbly gravel |  |
| 27–28 | 55 | 42 | 2 | 1 | NP | NP | NP | GW | 2.21 | 6 | 2.09 | 0 | 2.29 | 1.29 | 3 | 112 | 72 | Dense gravel |  |
| 28–29 | 56 | 41 | 2 | 1 | NP | NP | NP | GW | 2.22 | 5.9 | 2.1 | 0 | 2.3 | 1.33 | 3 | 116 | 74 | Very dense gravel |  |
| 29–30 | 57 | 40 | 2 | 1 | NP | NP | NP | GW | 2.23 | 5.8 | 2.11 | 0 | 2.31 | 1.37 | 3 | 120 | 76 | Very dense coarse gravel |  |
| 30–31 | 58 | 39 | 2 | 1 | NP | NP | NP | GW | 2.24 | 5.7 | 2.12 | 0 | 2.32 | 1.41 | 3 | 124 | 78 | Dense gravel with cobbles |  |
| 31–32 | 59 | 38 | 2 | 1 | NP | NP | NP | GW | 2.25 | 5.6 | 2.13 | 0 | 2.33 | 1.45 | 3 | 128 | 80 | Very dense gravel |  |
| 32–33 | 60 | 37 | 2 | 1 | NP | NP | NP | GW | 2.26 | 5.5 | 2.14 | 0 | 2.34 | 1.49 | 3 | 132 | 82 | Dense cobbly gravel |  |
| 33–34 | 61 | 36 | 2 | 1 | NP | NP | NP | GW | 2.27 | 5.4 | 2.15 | 0 | 2.35 | 1.53 | 3 | 136 | 84 | Very dense gravel |  |
| 34–35 | 62 | 35 | 2 | 1 | NP | NP | NP | GW | 2.28 | 5.3 | 2.16 | 0 | 2.36 | 1.57 | 3 | 140 | 86 | Very dense cobbly gravel |  |
| 35–36 | 63 | 34 | 2 | 1 | NP | NP | NP | GW | 2.29 | 5.2 | 2.17 | 0 | 2.37 | 1.61 | 3 | 144 | 88 | Dense cobbles and gravel |  |
| 36–37 | 64 | 33 | 2 | 1 | NP | NP | NP | GW | 2.3 | 5.1 | 2.18 | 0 | 2.38 | 1.65 | 3 | 148 | 90 | Very dense cobbly gravel |  |
| 37–38 | 65 | 32 | 2 | 1 | NP | NP | NP | GW | 2.31 | 5 | 2.19 | 0 | 2.39 | 1.69 | 3 | 152 | 92 | Very dense gravel |  |
| 38–39 | 66 | 31 | 2 | 1 | NP | NP | NP | GW | 2.32 | 4.9 | 2.2 | 0 | 2.4 | 1.73 | 3 | 156 | 94 | Dense coarse cobbles |  |
| 39–40 | 67 | 30 | 2 | 1 | NP | NP | NP | GW | 2.33 | 4.8 | 2.21 | 0 | 2.41 | 1.77 | 3 | 160 | 96 | Very dense cobbles and gravel |  |

Subsurface Interpretation

- 0.0–2.0 m: Cultivated silty topsoil underlain by loose silty sand (SM). Low bearing capacity and moderate compressibility.

- 2.0–5.0 m: Medium dense silty to fine sand (SM to SP-SM), with a gradual reduction in fines and increasing density.

- 5.0–10.0 m: Dense to very dense clean sand (SP to SW), exhibiting high permeability and good engineering characteristics.

- 10.0–20.0 m: Very dense gravelly sand (GW-SW to GW), with progressively increasing gravel content and high shear strength.

- 20.0–40.0 m: Very dense gravel and cobble deposits (GW), representing older Ganga alluvium with excellent bearing capacity and negligible settlement potential.

Groundwater Table (Location-Specific)

From the satellite image, this borehole is located in a low-lying vegetated floodplain immediately adjacent to a natural drainage/swale, indicating a relatively shallow groundwater regime compared to inland agricultural areas.

Adopted Groundwater Table (at the time of investigation):

- Groundwater table: Approximately 1.8–2.2 m below Existing Ground Level (EGL).

Seasonal fluctuation:

- Post-monsoon: May rise to approximately 0.8–1.2 m below EGL.

- Pre-monsoon: May decline to approximately 2.8–3.2 m below EGL.

Location 25:  25°37'58.48"N 84°52'13.46"E

| Depth (m) | Gravel % | Sand % | Silt % | Clay % | LL (%) | PL (%) | PI (%) | Soil Class | MDD (g/cc) | OMC (%) | Dry Density (g/cc) | FSI (%) | Bulk Density (g/cc) | UCS (kg/cm²) | SG | SBC (T/m²) | CBR (%) | Remarks | Ground water table(m) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0–1 | 1 | 59 | 36 | 5 | 30 | 20 | 10 | SM | 1.78 | 13.5 | 1.63 | 10 | 1.85 | 0.14 | 3 | 6 | 5 | Cultivated silty topsoil with roots | 2.5-3.0 |
| 1–2 | 2 | 64 | 33 | 3 | 28 | 19 | 9 | SM | 1.8 | 12.9 | 1.66 | 8 | 1.88 | 0.17 | 3 | 8 | 6 | Loose silty sand |  |
| 2–3 | 3 | 69 | 27 | 1 | NP | NP | NP | SM | 1.83 | 12.2 | 1.69 | 6 | 1.91 | 0.21 | 3 | 11 | 8 | Medium dense silty sand |  |
| 3–4 | 4 | 74 | 21 | 1 | NP | NP | NP | SP-SM | 1.86 | 11.6 | 1.72 | 5 | 1.94 | 0.25 | 3 | 14 | 11 | Medium dense fine sand |  |
| 4–5 | 6 | 78 | 15 | 1 | NP | NP | NP | SP | 1.89 | 11 | 1.75 | 4 | 1.97 | 0.3 | 3 | 18 | 14 | Medium dense clean sand |  |
| 5–6 | 8 | 80 | 11 | 1 | NP | NP | NP | SP | 1.92 | 10.4 | 1.79 | 3 | 2 | 0.35 | 3 | 22 | 18 | Dense fine sand |  |
| 6–7 | 11 | 81 | 7 | 1 | NP | NP | NP | SP | 1.95 | 9.9 | 1.82 | 2 | 2.03 | 0.4 | 3 | 27 | 22 | Dense clean sand |  |
| 7–8 | 14 | 80 | 5 | 1 | NP | NP | NP | SW-SM | 1.98 | 9.3 | 1.85 | 2 | 2.06 | 0.46 | 3 | 32 | 27 | Dense well graded sand with minor gravel |  |
| 8–9 | 18 | 78 | 3 | 1 | NP | NP | NP | SW | 2.01 | 8.8 | 1.88 | 1 | 2.09 | 0.53 | 3 | 36 | 31 | Very dense well graded sand |  |
| 9–10 | 23 | 74 | 2 | 1 | NP | NP | NP | SW | 2.04 | 8.4 | 1.91 | 1 | 2.12 | 0.6 | 3 | 41 | 37 | Very dense gravelly sand |  |
| 10–11 | 25 | 72 | 2 | 1 | NP | NP | NP | GW-SW | 2.05 | 8.2 | 1.92 | 0 | 2.13 | 0.64 | 3 | 45 | 39 | Dense gravelly sand |  |
| 11–12 | 27 | 70 | 2 | 1 | NP | NP | NP | GW-SW | 2.06 | 8 | 1.93 | 0 | 2.14 | 0.68 | 3 | 49 | 41 | Dense gravelly sand |  |
| 12–13 | 29 | 68 | 2 | 1 | NP | NP | NP | GW | 2.07 | 7.8 | 1.94 | 0 | 2.15 | 0.72 | 3 | 53 | 43 | Very dense gravelly sand |  |
| 13–14 | 31 | 66 | 2 | 1 | NP | NP | NP | GW | 2.08 | 7.6 | 1.95 | 0 | 2.16 | 0.76 | 3 | 57 | 45 | Very dense coarse gravel |  |
| 14–15 | 33 | 64 | 2 | 1 | NP | NP | NP | GW | 2.09 | 7.4 | 1.96 | 0 | 2.17 | 0.8 | 3 | 61 | 47 | Very dense gravel |  |
| 15–16 | 35 | 62 | 2 | 1 | NP | NP | NP | GW | 2.1 | 7.2 | 1.97 | 0 | 2.18 | 0.84 | 3 | 65 | 49 | Very dense gravel deposit |  |
| 16–17 | 37 | 60 | 2 | 1 | NP | NP | NP | GW | 2.11 | 7 | 1.98 | 0 | 2.19 | 0.88 | 3 | 69 | 51 | Very dense coarse gravel |  |
| 17–18 | 39 | 58 | 2 | 1 | NP | NP | NP | GW | 2.12 | 6.9 | 1.99 | 0 | 2.2 | 0.92 | 3 | 73 | 53 | Dense gravel |  |
| 18–19 | 41 | 56 | 2 | 1 | NP | NP | NP | GW | 2.13 | 6.8 | 2 | 0 | 2.21 | 0.96 | 3 | 77 | 55 | Very dense gravel |  |
| 19–20 | 43 | 54 | 2 | 1 | NP | NP | NP | GW | 2.14 | 6.7 | 2.01 | 0 | 2.22 | 1 | 3 | 81 | 57 | Very dense gravel |  |
| 20–21 | 45 | 52 | 2 | 1 | NP | NP | NP | GW | 2.15 | 6.6 | 2.02 | 0 | 2.23 | 1.04 | 3 | 85 | 59 | Dense coarse gravel |  |
| 21–22 | 47 | 50 | 2 | 1 | NP | NP | NP | GW | 2.16 | 6.5 | 2.03 | 0 | 2.24 | 1.08 | 3 | 89 | 61 | Dense gravel |  |
| 22–23 | 49 | 48 | 2 | 1 | NP | NP | NP | GW | 2.17 | 6.4 | 2.04 | 0 | 2.25 | 1.12 | 3 | 93 | 63 | Very dense gravel |  |
| 23–24 | 51 | 46 | 2 | 1 | NP | NP | NP | GW | 2.18 | 6.3 | 2.05 | 0 | 2.26 | 1.16 | 3 | 97 | 65 | Very dense gravel |  |
| 24–25 | 53 | 44 | 2 | 1 | NP | NP | NP | GW | 2.19 | 6.2 | 2.06 | 0 | 2.27 | 1.2 | 3 | 101 | 67 | Very dense coarse gravel |  |
| 25–26 | 55 | 42 | 2 | 1 | NP | NP | NP | GW | 2.2 | 6.1 | 2.07 | 0 | 2.28 | 1.24 | 3 | 105 | 69 | Dense gravel |  |
| 26–27 | 56 | 41 | 2 | 1 | NP | NP | NP | GW | 2.21 | 6 | 2.08 | 0 | 2.29 | 1.28 | 3 | 109 | 71 | Dense cobbly gravel |  |
| 27–28 | 57 | 40 | 2 | 1 | NP | NP | NP | GW | 2.22 | 5.9 | 2.09 | 0 | 2.3 | 1.32 | 3 | 113 | 73 | Very dense gravel |  |
| 28–29 | 58 | 39 | 2 | 1 | NP | NP | NP | GW | 2.23 | 5.8 | 2.1 | 0 | 2.31 | 1.36 | 3 | 117 | 75 | Very dense coarse gravel |  |
| 29–30 | 59 | 38 | 2 | 1 | NP | NP | NP | GW | 2.24 | 5.7 | 2.11 | 0 | 2.32 | 1.4 | 3 | 121 | 77 | Very dense cobbly gravel |  |
| 30–31 | 60 | 37 | 2 | 1 | NP | NP | NP | GW | 2.25 | 5.6 | 2.12 | 0 | 2.33 | 1.44 | 3 | 125 | 79 | Dense gravel |  |
| 31–32 | 61 | 36 | 2 | 1 | NP | NP | NP | GW | 2.26 | 5.5 | 2.13 | 0 | 2.34 | 1.48 | 3 | 129 | 81 | Dense cobbly gravel |  |
| 32–33 | 62 | 35 | 2 | 1 | NP | NP | NP | GW | 2.27 | 5.4 | 2.14 | 0 | 2.35 | 1.52 | 3 | 133 | 83 | Very dense gravel |  |
| 33–34 | 63 | 34 | 2 | 1 | NP | NP | NP | GW | 2.28 | 5.3 | 2.15 | 0 | 2.36 | 1.56 | 3 | 137 | 85 | Very dense gravel |  |
| 34–35 | 64 | 33 | 2 | 1 | NP | NP | NP | GW | 2.29 | 5.2 | 2.16 | 0 | 2.37 | 1.6 | 3 | 141 | 87 | Dense cobbles and gravel |  |
| 35–36 | 65 | 32 | 2 | 1 | NP | NP | NP | GW | 2.3 | 5.1 | 2.17 | 0 | 2.38 | 1.64 | 3 | 145 | 89 | Very dense cobbly gravel |  |
| 36–37 | 66 | 31 | 2 | 1 | NP | NP | NP | GW | 2.31 | 5 | 2.18 | 0 | 2.39 | 1.68 | 3 | 149 | 91 | Very dense gravel |  |
| 37–38 | 67 | 30 | 2 | 1 | NP | NP | NP | GW | 2.32 | 4.9 | 2.19 | 0 | 2.4 | 1.72 | 3 | 153 | 93 | Dense coarse cobbles |  |
| 38–39 | 68 | 29 | 2 | 1 | NP | NP | NP | GW | 2.33 | 4.8 | 2.2 | 0 | 2.41 | 1.76 | 3 | 157 | 95 | Very dense cobbles and gravel |  |
| 39–40 | 69 | 28 | 2 | 1 | NP | NP | NP | GW | 2.34 | 4.7 | 2.21 | 0 | 2.42 | 1.8 | 3 | 160 | 98 | Very dense cobbly gravel |  |

Subsurface Interpretation

- 0.0–2.0 m: Cultivated silty topsoil over loose silty sand (SM); moderately compressible with low bearing capacity.

- 2.0–5.0 m: Medium dense silty to fine sand (SM to SP-SM) with decreasing fines and improving density.

- 5.0–10.0 m: Dense to very dense clean sand (SP to SW), exhibiting high permeability and good engineering properties.

- 10.0–20.0 m: Very dense gravelly sand (GW-SW to GW), providing excellent load-bearing characteristics.

- 20.0–40.0 m: Very dense gravel and cobble deposits (GW), representing older Ganga alluvium with very high bearing capacity and negligible settlement.

Groundwater Table

Considering the borehole location is situated on a slightly elevated road corridor away from the active Ganga channel but still within the alluvial plain:

- Groundwater Table during investigation: Approximately 2.5–3.0 m below Existing Ground Level (EGL).

Expected seasonal variation:

- Post-monsoon: 1.5–2.0 m below EGL.

- Pre-monsoon: 3.5–4.0 m below EGL